## Slide 1: E4 Reduction & DTS Change Proposal
Agostino & DerChang, WW07.4/18
E4 Reduction Strategy
Analysis
Change Proposal and Ratification Process

## Slide 2: E4 Reduction Strategy
VT,set: no impact to Vsel−Vinh window; reducing VT,set degrades inhibiting ratio  will keep constant
∆VT: exhibits higher with Alloy6/CR5.3
𝛔rst: exhibits reduction with Alloy6/CR5.3.
dftrst: lower than SXP due to SD only (no amorphous PM drift)
Vpara: Constant; no change to WL/BL resistance and cell leakage (inhibit ratio)
Voltage [V]
Set@1us
Reset@1us
0s
3.54s
E2
Vinh
E1
E3
E4
Vsel
3.54s
VT,set
VT,rst
∆Vwlr
dftset
Gbendu,RD
dftrst
∆Vinh
Vpara
∆VT
Vsel = VT,set + ∆VT + 3.54∙𝛔rst + dftrst + Vpara
V+,Local = Vsel − Vinh
V−,Local = − Vinh

## Slide 3: RWB and Vsel−Vinh Window Analysis
All unit in mV | S15 Rev3.12.1 | S26A Rev 2.2 | SSM Rev 0.3 | SSM Pre R 0.4 (Single VDM) | SSM Pre R 0.4 (Dual VDM) | Change (PreR.4 - R.3) | Change (Dual - Single)
Decoder | Unipolar | Unipolar | Bipolar Option 1 | Bipolar Option 2 | Bipolar Option 2 |  | 
Set Vt mean @ 1usec | 4410 | 4410 | 4530 | 4410 | 4410 | -120 | 
Set Sigma | 105 | 105 | 105 | 80 | 80 | -25 | 
Reset Sigma | 90 | 90 | 105 | 100 | 100 | -5 | 
E3 shift (cycling window) | 100 | 100 | 0 | 100 | 100 | 100 | 
E3 RD | 0 | 0 | 250 | 250 | 250 |  | 
x'tile | 30 | 30 | 30 | 30 | 30 |  | 
E2 drift Dual VDM: 1usto 10s Single VDM: 1us to 2d | 240 | 240 | 450 | 450 | 240 |  | -210
Read bias Variation | 50 | 50 | 50 | 50 | 50 |  | 
Other(?) | 70 | 70 | 0 | 70 | 70 | 70 | 
Reset Vt mean @ 1us (DTS) | 5590 | 5590 | 6030 | 6000 | 5790 | -30 | -210
delta Vt (DTS) | 1180 | 1180 | 1500 | 1590 | 1380 | 90 | -210
Max Reset Drift (1us-2d) | 1000 | 1000 | 500 | 400 | 400 | -100 | 
Reseet 3.54 sigma to E4 | 319 | 319 | 372 | 354 | 354 | -18 | 
Leakage IR (20uA×20K) | 400 | 400 | 400 | 400 | 400 |  | 
Selection Voltage | 7309 | 7309 | 7302 | 7154 | 6944 | -148 | -210
Negative VDM (WL VDM) | 3500 | 3500 | 3500 | 3500 | 3500 |  | 
Postive VDM (AXN) | 3809 | 3809 | 3802 | 3654 | 3444 | -148 | -210
Posistive VDM requirement | 3800 | 3800 | 3800 | 3540 | 3540 |  | 
Gap (25mV error bar) |  |  |  | 114 |  |  | 
Match S15/S26
Empirical
Match S15/S26
Dual VDM
Dual VDM
-σ, +RD, +(?)
Empirical

## Slide 4: Change and Ratification
Proposed DTS changes
Ratification
  RA/RM based on Alloy6/CR5.3 (ECD WW10)
  PrePOR DTS and experimental collateral for Design impact assessment (ECD WW10)
All unit in mV | POR Rev 0.3 | PrePOR Rev 0.4
Drift Tracker | Single VDM | Dual VDM
Set Vt mean @ 1usec | 4530 | 4410
Set Sigma | 105 | 80
Reset Sigma | 105 | 100
E3 shift (cycling window) | 0 | 100
E2 drift | 450 | 240
Other(?) | 0 | 70
Reset Vt mean @ 1us | 6030 | 5790
delta Vt | 1500 | 1380
Max Reset Drift (1us-2d) | 500 | 400
Selection Voltage | 7300 | 6950