## Slide 1: SD Characterization Update
Dan Gealy, Enrico Varesi, Folsom TEMlab, Boise TEM lab, Mattia Robustelli, Umberto Meotto, Brady Jenkins, Brian Gerhard
1 31 2018

## Slide 2: Summary – work in progress
PFA on SD1 (only)
  SR71 X-cut (no grounded) Folsom (pos/neg/virgin program) – 0024732/wf16
  SR71 Y-cut (no grounded) Boise (pos/neg/virgin program) - 0024732/wf16
  S26 Y-cut (grounded) Boise (pos program) - 0024732/wf2
    Thickness changes not prominent
    SR71: some segregation detected on opposite programmed cells moving opposite compared to virgin (not all data are in to have full correspondence), in addition to a main modulation by cut direction (as usual for ungrounded samples).
    Grounded positive only prog S26 indicates Se enrichment at top.
  Not much consistent with initial work on SD1 (it was much higher)
PFM work at the PFM/AFM
  No data yet
Raman from probed arrays

## Slide 3
PFA-396 (SD1)
SD1:
Stronger As/Se segregation
for SET vs RESET (time dominating)
1us
50ns
1us
50ns
50 ns | 1000 ns | 50 ns | 1000 ns
50 uA |  | 150 uA | 
1k cycles
Hefei, Enrico
  Elemental segregation with SD1
    Consistent with current direction (as with PM)
      Opposite electromigration behavior on D0 & D1
SD1 Elemental Migration
Back

## Slide 4
W BLs were not grounded.
W BLs were grounded.
WL-BL grounding
SR71 Boise
Y-cut
S26 Boise
Y-cut

## Slide 5: Stem Images: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
Folsom
X-cut SR71 ungrounded
Significant Se enrichment at bottom for one of the two programmed cell
Opposite smooth segregation for opposite prog, compared to virgin
Prog assignment to be confirmed
Prog sequence:
pos,/neg prog seasoning
chkb positive prog (4 pulses)
line pattern:
adjacent pos and neg prog between 6 not programmable cells

## Slide 6: Filtered normalized composition profiles
Virgin #11
Virgin #12
#16
#24
#32
#40
#48
Folsom
X-cut SR71 ungrounded
bottom
top

## Slide 7
EDS Element Mapping
Se map
Ge map
Even
neg
Odd
pos
RS71 SD1
TL171222001 – Boise
WL cut (Y) not grounded
http://edcfab4.micron.com/fab4/RTL010/_layouts/15/osssearchresults.aspx?k=TL171222001
As map

## Slide 8
SI= (Se/As)top / (Se/As)bottom
RS71 SD1
TL171222001 – Boise
WL cut (Y) not grounded
Due to the difficulty of de-processing for specific location samples, in this sample, W BLs were not connected together. Therefore, sample prep would cause element segregation. Here it is assumed that the effect of sample prep on element segregation is at the same extent for all the bits.
Odd and even bits were fired oppositely.
For oppositely fired bits, the As/Se segregation behavior is also opposite.
http://edcfab4.micron.com/fab4/RTL010/_layouts/15/osssearchresults.aspx?k=TL171222001
neg
pos

## Slide 9
Top
Se-rich
Bottom
As-rich
RS71 SD1
TL171222001 – Boise
WL cut (Y) not grounded

## Slide 10
S26
SR71 even
SR71 odd
SR71 virgin
top
bottom
SR71-even = neg prog ?
SR71-odd => pos prog ?
S26 => pos prog
SD1
summary
Boise, Y-cuts
Folsom
X-cut, ungrounded
(usually Se-bottom)
ungrounded
grounded
ungrounded
(usually Se-top)
grounded

## Slide 11
D1
D0
D0, X-cut=Se bottom
D1, X-cut=Se bottom
D1, Y-cut=Se top
D1, Y-cut=Se top
X-cut=Se bottom
Y-cut=Se top
Typical
Ungrounded result

## Slide 12
device | TEM lab | cut | line | Grounding WL-BL | prog | Se/As top/bottom | Se-rich
SR71 | Folsom | X | BL 9 | no | Pos | 1.06 | 
 |  |  |  |  | Neg | 0.75 | 
 |  |  |  |  | virgin | 0.95 | bottom
SR71 | Boise | Y | WL 14 | no | Pos | 1.10 | 
 |  |  |  |  | Neg | 1.77 | 
 |  |  |  |  | virgin | 1.33 | top
S26 | Boise | Y |  | yes | Pos | 1.63 | 
Typically ungrounded:
X-cut=Se-rich at bottom
Y-cut=Se-rich at top
SR71 (ungrounded):
  Overall (virgin) main segregation modulated by cut direction (as usual)
  Opposite segregation for opposite programming compared to virgin
  Programming assignment to be confirmed
S26 (grounded pos prog): Se enrichment at top
SD1 PFA summary

## Slide 13: Raman on Probed arrays (SDv12 SD-only, S26)
Laser treated was not bake recoverable
Differences observed between front-side deprocessed virgin & probed
Backside deprocessed not completed
Frontside deprocessed
Red: virgin
Black: programmed