## Slide 1: K* campaign: S26 data
Deeper insights, potential warnings and expectations
Lidia, Ago and Paolo

## Slide 2: Upsides from S26
2 Lots out of the K* camp (In-SAG and In-SiSAG)
S26 main array probe confirms SR71 trends with In
Main upsides of the In-SAG matrix:
  FF reduction
  Lower sigma
  Good drift performances
  Higher Memory Effect
  Higher SSM window (just from SR71 and 2xCMOS)
Drift vs. Sigma
Split | Ge | Si | In
1C | 13 | 6 | 2
2E | 16 | 0 | 0
3E | 21 | 0 | 0
4E | 25 | 0 | 0
5E | 16 | 0 | 2
6E | 16 | 0 | 5
7E | 19 | 0 | 2
Normalized Sigma vs. VT
Golden alloy
Memory effect vs Composition
10s
Drift Rate vs 10s SET sigma @ 85C
>1 Volt!
In-SAG alloys
FF reduction
Probe no visib at higher Vt

## Slide 3: Potential warning of In-SAG: Lower Tg
Lower Tg/lower thermal stability have not impact on opens on these alloys
SDv12
Thermal stability
by Swap
Filtered from zone E and railed WLICS
Opens (log) model
Si major driver
Residual after fitting by BLBL

## Slide 4: Potential warning of In-SAG: Leakage – S26 data
Full Stack
5% SDonly
2% SDonly
4% SD only w/ T&B lamina
VL at 3.6V nominal;
4K cells
50-50% SET/RST back pattern
SD at 22nm for SD only
+15-20% VL from 2% to 5% In
Adding lamina
Inc In%
85C

## Slide 5: Camp J*: “Normalized” I-V curves (x-axis bias is from 0 to 85%VT)
The progressive In addition tends to increase the sub-VT P-F conduction. See here the comparison with SDv13.
Leakage increase consistent with what observed on array
Ge 13%
Ge 13%
Ge 13%
In 6%
In 9%
In 11%
SDv13
From the K camp
In addition
Ge 15%
In 5%
~4E alloy!

## Slide 6: SiSAG vs In-SAG/In-SiSAG benchmarking for SxP
Better Drift, Sigma higher Memory effect can be capitalized for PM scalability
In-SAG will require higher SD thickness (~4 nm) than Si-SAG to get the same VT
Thus, In-SAG can be of interest for SxP also
Si-SAG
In-SAG
In
Si
@ 22 nm thickness
DVT~0.5V
POR
To get the same POR VT with In-SAG (4E), we need to increase tSD by ~ 4 nm
Better Sigma (<100mV for In-SAG) wrt ~120 mV for POR, better Drift (240 mV wrt 280 mV in the ~ VDM3 from SR71), higher Memory Effect (280 mV) represent a RWB improvement that could be capitalized as PM scaling
Actual 30S
30S w/ In-SAG
Recommendation:
SxP trial with In-SAG centered on 16%Ge and 5%In

## Slide 7: Back-up

## Slide 8: Upsides from S26
2 Lots out of the K* camp (In-SAG and In-SiSAG)
Main upsides of the In-SAG matrix:
  FF reduction
  Lower sigma
  Good drift performances
  Higher Memory Effect
  Higher SSM window (just from SR71 and 2xCMOS)
>1 Volt!
In-SAG alloys
FF reduction
Drift vs. Sigma
Split | Ge | Si | In
1C | 13 | 6 | 2
2E | 16 | 0 | 0
3E | 21 | 0 | 0
4E | 25 | 0 | 0
5E | 16 | 0 | 2
6E | 16 | 0 | 5
7E | 19 | 0 | 2
Normalized Sigma vs. VT
Golden alloy
Memory effect vs Composition
SSM window - 3.54s projected
In
Si
SSM window
Note: Memory Effect reliability to be verified

## Slide 9
ILEAK
VT

## Slide 10: Recommendations:
2nd Lot confirmed the recommendation to purchase of In-SAG alloy with Ge16% and In 5% mono-tg as SSM pre-POR  ETA for tg arrival end-Jan
Preliminary analysis of K* pushes to consider In-SAG for 30S too  opportunity to run it on 3DXP when the 30S perspectives will be clarified
In-SAG results reinforce the roadmap for Ga-SAG
1.6
1.7
1.8
2.4
In line with the III-group exploration we can check if the the Electronegativity contrast wrt Se the important parameter for the SSM window?
    GaSe tg in house, more suitable for this campaign is the Ga2Se3 tg  just ordered (ETA ~ wk 8)

## Slide 11: Towards a Treasure Map of the In-SAG based SD3 (including also In-SiSAG)
2 further A0 Lots planned to complete the treasure map exploration of the In-SAG (and In-SiSAG) system (split tables) + some selected alloys on A1  Next read: wk 04
Main open question we need to answer: what is the maximum In% we can tolerate w/o segregation and leakage issues?

## Slide 12
Area of further interest:
  +In, +Ge
  verify Si role