## Slide 1: PM speed
Samples for RWTH POT

## Slide 2: purpose
Measurement of PM transformation speed @RWTH by POT (pulsed optical tested)
Availability to measure a few alloys
Interest for Te-rich, Sb-rich and contaminated

## Slide 3: Reflectivity measurements
Wuttig group built a Phase Change Optical Tester (POT), with also time resolved capability
Within this collaboration there is also the request to characterize some alloys from Micron.
  Planned measurement on top/bottom segregated alloys (Te-rich, Sb-rich), w/w-o contaminant – target available from next Jan.

## Slide 4: Standard RWTH stack for POT measurement

## Slide 5: Status: simulation on Si (wafer)/SiO2 (550nm)/GST-like (120nm)/carbon (20nm)
=658 nm
Suggested best stack:
GST= 70-90 nm
Carbon= 10-20 nm

## Slide 6: Proposed samples (final stack to be defined)
PM(Sb-rich) + buffers
  THOX
  THOX preann
  TEOS (or CSOD) asdep
  TEOS (or CSOD) preann
PM(Te-rich)
  THOX
  THOX preann
  TEOS (or CSOD) asdep
  TEOS (or CSOD) preann