## Slide 1: SD Characterization Update
Dan Gealy, Enrico Varesi
1 24 2018

## Slide 2: Summary – work in progress
PFA 1357 in progress – SD1 split
  Some segregation observed
    Primarily As motion
    No grounding
    Thickness changes not prominent
    Not all data is in
  Not consistent with initial work on SD1
PFM work at the PFM/AFM
  No data yet
Raman from probed arrays

## Slide 3: Stem Images: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
15
15
22
24
32
16
23
31

## Slide 4: Filtered normalized composition profiles
Virgin #11
Virgin #12
#16
#24
#32
#40
#48

## Slide 5: Linescan: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
Bit 11 virgin
Bit 12 virgin
Bit 16
Bit 24
Bit 12 virgin
Bit 32
Bit 40
Bit 48

## Slide 6
PFA-396 (SD1)
SD1:
Stronger As/Se segregation
for SET vs RESET (time dominating)
1us
50ns
1us
50ns
50 ns | 1000 ns | 50 ns | 1000 ns
50 uA |  | 150 uA | 
1k cycles
Hefei, Enrico
  Elemental segregation with SD1
    Consistent with current direction (as with PM)
      Opposite electromigration behavior on D0 & D1
SD1 Elemental Migration
Back

## Slide 7: Raman on Probed arrays
Laser treated was not bake recoverable
Differences observed between front-side deprocessed virgin & probed
Backside deprocessed not completed