## Slide 1: SD Characterization Update
Feb 14, 2018
Dan Gealy, Enrico Varesi, Folsom TEMlab, Boise TEM lab, Mattia Robustelli, Umberto Meotto

## Slide 2: PFA on SD1
Goal: to verify element segregation on a SD material more thermally stable than POR SD, to confirm previous PFA results addressing Se/As segregation similarly to Te/Sb for PM.
SD1 (only) samples
  S26 (pos program) – post probe 0024732/wf2
  S26 (virgin) 0024732/wf2
  SR71 (pos/neg/virgin program) 0024732/wf16
    Prog sequence: pos,/neg prog seasoning + CHKBD positive prog (4 pulses)
    line pattern: adjacent pos and neg prog between 6 not programmable cells

## Slide 3: Summary – TEM PFA Work SD1
TL180206001 – S26 virgin die - SD1 split
  WL cut (Y-dir)
    Grounded WL/BL
      Little segregation observed. SI ≈ 1
    Ungrounded
      Se/As segregation observed – top is Se rich, bottom is As rich. SI > 1
  BL cut (X-dir)
    Ungrounded
      Se/As segregation observed – top is As rich, bottom is Se rich. SI < 1
TL180108002 – S26 probed die - SD1 split
  WL cut (Y-dir) - Grounded WL/BL. “Positive” programming
  Se/As segregation observed – top is Se rich, bottom is As rich. SI > 1
S26a
Virgin bits
S26a
Pos/Virgin bits
Consistent with selenium tendency to enrich (by migration) toward positive electrode, either if poled by program or by ungrounding charging

## Slide 4: Summary – TEM PFA Work SD1 (2)
PFA1357
TL1721222001 SR71b with bit placement - SD1 split
  WL cut (WL14). No grounding
  Strong Se/As segregation trending
    Even/odd bit placement is opposite
    SI: “even bits” > virgin bits > “odd bits” observed – top is Se rich, bottom is As rich. SI > 1
    Thickness changes not prominent
PFA 1357– SR71b SD1 split
  BL cut (X-dir)
    Ungrounded
      Se/As segregation observed – top is As rich, bottom is Se rich
    Se/As segregation trending
      “odd bits”> virgin bits >”odd bits” – top is Se rich, bottom is As rich
      Thickness changes not prominent
  PFA 1357/TL180206001 ungrounded BL cut are consistent
  Prog assignment to be confirmed
TL172122001

## Slide 5
Job | device | Lot/wf | status | GND | Cut_dir | type | Se rich | Se/As (top/bottom)
Pfa-1357 | SR71 | 0024732/wf16 | Done | No | X | Prog2 | Bottom | 0.75
 |  |  |  |  |  | Virgin | Bottom | 0.95
 |  |  |  |  |  | Prog1 | no | 1.06
 | SR71 | 0024732/wf16 |  | Yes | Y | Neg |  | 
 |  |  |  |  |  | Virgin |  | 
 |  |  |  |  |  | Pos |  | 
TL171222001 | SR71 | 0024732/wf16 | Done | No | Y | Neg (odd) | Top | 1.11
 |  |  |  |  |  | Virgin | Top | 1.31
 |  |  |  |  |  | Pos (even) | Top | 1.75
TL180108002 | S26 | 0024732/wf2 | Done | Yes | Y | Pos | Top | 1.62
TL180206001 | S26 | 0024732/wf2 | Done | Yes | Y | Virgin | no | 1.02
 | S26 | 0024732/wf2 | Done | No | X | Virgin | bottom | 0.86
 | S26 | 0024732/wf2 | Done | No | Y | Virgin | Top | 1.2
Pfa-1385 | S26 | 0024732/wf2 |  | Yes | Y | Pos |  | 
PFA on SD1 – Summary Table

## Slide 6
pfa-1357
PFA on SD1 – Summary; Segregation Index Boxplots
SI = (Se/As)top/ (Se/As)bottom
negative
positive
Selenium tends to enrich (by migration) toward positive electrode, either if poled by program or by ungrounding charging

## Slide 7
PFA-396 (SD1)
SD1:
Stronger As/Se segregation
for SET vs RESET (time dominating)
1us
50ns
1us
50ns
50 ns | 1000 ns | 50 ns | 1000 ns
50 uA |  | 150 uA | 
1k cycles
Hefei, Enrico
  Elemental segregation with SD1
    Consistent with current direction (as with PM)
      Opposite electromigration behavior on D0 & D1
Previous SD1 Elemental Migration Work
Back

## Slide 8
D1
D0
D0, X-cut=Se bottom
D1, X-cut=Se bottom
D1, Y-cut=Se top
D1, Y-cut=Se top
X-cut=Se bottom
Y-cut=Se top
Previous typical ungrounded result:
- grounded= WL-BL grounding
- ungrounded = just the line inside lamella is grounded, the other metals can charge positively during FIB cut.
+
+
+
+
Consistent with Se moving toward positive electrode

## Slide 9
W BLs were not grounded.
W BLs were grounded.
WL-BL grounding
SR71 WL cut
(Y-dir)
S26 WL cut
(Y-dir)
metal

## Slide 10
Virgin Bits – S26a TL180206001
SD1 split4E, w02 Ungrounded WL/BL cuts
  Grounded WL cut shows little segregation
  Ungrounded show segregation
  Opposite segregation between WL & BL cuts
Virgin array -ungrounded BL cut
Virgin array - ungrounded WL cut
Virgin array -grounded WL cut
Hongqi

## Slide 11
Pos prog TL180108002
Fired/Virgin Bits – S26A TL180108002, TL180206001
Grounded WL Cuts
Hongqi
Virgin Array TL180206001
SD1 split4E, Grounded WL cuts
  w02 S26A
    Programed
    Virgin array
  Segregation on programming observed
    Se rich top, As rich bottom
  Little preparation bias

## Slide 12
Odd (Neg prog?)
Fired/Virgin Bits – SR71b TL1712222001
Even (Pos prog?)
Virgin
SD1 split4E w16
  WL Cut. No grounding
    WL 14/multiple BL’s
    Se/As segregation trending
      SI “even bits”> virgin bits >”odd bits” – top is Se rich, bottom is As rich
Hongqi
Ungrounded WL cut overlays a preparation segregation bias that adds to D0 positive programming but subtracts from D0 negative programming
TL172122001

## Slide 13
Pos prog
S26a
Fired Bits – SR71b TL1712222001, S26a TL180108002
SD1 split4E
  w16 SR71b
    WL Cut. No grounding
    WL 14/multiple BL’s
  w02 S26a
    WL cut. Grounded
  Data is consistent if we assume pos. programing on even bits
    Logical interpretation is that even lines are probed negatively
Even (Pos prog?) SR71b
Hongqi

## Slide 14
Virgin Bit Comparison – SR71b/S26a
Virgin Bits – SR71b ungrounded BL cut PFA 1357
SD1 split4E w16
  BL Cut. No grounding
  SI < 1
Virgin Bits S26a -ungrounded BL cut

## Slide 15
Odd (Neg prog?)
Fired/Unfired Bits – PFA 1357
Even (Pos prog?)
Virgin
SD1 split4E w16
  BL Cut. No grounding
Hefei

## Slide 16: PFA 1357 / TL122122001 Comparison
TL172122001
  WL Cut. WL14 (1st active) - verifiied
PFA1357
  BL Cut. BL 9
Trends are opposite between PFA 1357 & TL122122001
Actual placement needs to be better understood
Assuming even bits are positively programed (not intended) WL cuts on SR71b & S26a not grounded v. grounded are consistent
TL172122001
PFA1357

## Slide 17
EDS Element Line Scan TL171222001 Oppositely Fired Bits (SR71)
33
35
34
36
37
38
33
35
34
36
37
38
Linescans not normalized

## Slide 18
EDS Element Line Scan TL171222001 Not Fired Bits (SR71)
33
35
34
36
37
38
33
35
34
36
37
38
Linescans not normalized

## Slide 19
EDS Element Line Scan TL80108002 (S26)
Grounded WL/BL
Consistent with SR71B
As/Se motion
Linescans not normalized

## Slide 20: Stem Images: 0024732.003, split 4E SD1 SAG, wafer16 SR71B
Folsom
X-cut SR71 ungrounded
Significant Se enrichment at bottom for one of the two programmed cell
Opposite smooth segregation for opposite prog, compared to virgin
Prog assignment to be confirmed
Prog sequence:
pos,/neg prog seasoning
chkb positive prog (4 pulses)
line pattern:
adjacent pos and neg prog between 6 not programmable cells

## Slide 21
S26
SR71 even
SR71 odd
SR71 virgin
top
bottom
SD1
summary
Boise, Y-cuts
Folsom
X-cut, ungrounded
(usually Se-bottom)
ungrounded
grounded
ungrounded
(usually Se-top)
grounded