## Slide 1: S26A SD only K* wave2 probe summary
ww8
Lidia

## Slide 2: Summary
Main advantage found from SD only lot SWR (different integration, different probe flow, S26 product)
  Consistent memory effect increase in trend with In content; +100mV between SET/RST from POR SD to In-SAG at 5%  to demonstrate the transfer to full stack window
  SET sigma improvement, might be -10mV
Possible downside and warning, how far with In concentration?
  Cell
    Drift increase, data are noisy and collected with long sense time (PG4 spec)
    VL increase minor
  Structure
    SWL WLICS increase, not intrinsic but due to damage by seasoning (pending PFA)
  Unknown metrics
    E1 knee not available
  Given downsides, recommendation is to limit to 5% In
Full stack integration concern
  SD thickness adjustment and etch.
    To match SET Vt, SD thickness has to be higher than FS POR. Imply etch adjustment with possibly different response of the new alloy to the chemistry.
  SD liner protection: all the exp here shown have the so called 2-step WL etch with PL to preserve SD and give a straight CD profile

## Slide 3: SWR/Lots considered for this presentation (S26 2nd wave K* SD only campaign)
PR 28 at 50C
A0 reticle
Explores In from 5 to 11%
PR 28 at 85C
A0 reticle
1E has forward looking alloy for SSM project
Other exp are not today focus too high Ge or Si addition
PR 29 at 85C
A1 reticle
Explores In from 5 to 7%
No significant change with probe rev; IRST fixed at 120uA and SET pulse fixed at P1=22.5uA, P3 = 25uA, P4 = 22.5uA
One lot has been probed at 50C unintentionally

## Slide 4: 85C probe 0173982.013 + a repetition of Alloy 6 on 0057102.003
Zone A/B
median after filtering from structure fail
ED3
All the metrics have been corrected for the access transistor and refer to the voltage across the cell
Need to evaluate the impact on the array with proper access transistor contribution that differs between S15C and S26A
The lowest SET Vt can be over- estimated by the sweep range with current DAC. In general 10s SET Vt is properly extracted. Other metrics that uses 1us SET Vt can be also affected (memory effect is eventually under-estimated)

## Slide 5: 0024692.003 full lot (50C)
Fail at periph

## Slide 6: Vt sigma (10s)
In SAG
In Si-SAG
Alloys with much different composition have been intentionally excluded from this plot
In-SAG: SET sigma improvement
no clear worsening from 5% to 7%
Carefully evaluate L2L
wave2 results better than wave1, that was structurally compromised
Norm Vt sigma vs Vt 10s
Vt sigma vs Vt 10s
0057102
0024692
K* lots have 22nm thick SD
Line is roughly where S15C CR 7.72 full stack is (corrected Vt by -400mV)
Eventually skew SD thickness lower than 22nm to match Vt

## Slide 7: Drift
7% InSAG
PG4 sensing time (75ns) One of the two lots is neutral for drift comparison POR vs 5% InSAG; the other one shows +70mV
All SD only lots have lower drift than full stack S26 ref
POR
5% InSAG
WLR 3H-1us 85C
Probe 100s -1us 85C
Also from Probe, downside with In%

## Slide 8: VL vs SET Vt
+25%

## Slide 9: Structural

## Slide 10: WLICS SWL increase with high In post Seasoning
9%
9%
11%
In%
WLICS huge increase after Seasoning for highest In composition, two worst grp 5E/7E have also tails of high VL, suspecting damage (IRST for seasoning at 120uA). Upon retest degradation continue and 3E is hit also
WLICS pre is clean
SWL at re-probe vs SWL after 1st seasoning

## Slide 11: Opens SBIT
Single bit after filtering from WLICS
Zone A-C
No toggle for opens
9%

## Slide 12: Back up

## Slide 13: WLICS
WLICS huge increase after Seasoning VL for 2E; 6E railed for SWL already before Seasoning
0057102.003
WLICS –pre seasoning
SWL
With re-probe SWL increase extends to other alloys
SWL Re-probe/ 1st season
SWL after 1st season
SWL at re-probe
Grp in order of gravity:
6E>2E>4E>7E>5E=1E>3E
Difficult to find a toggle with alloy composition

## Slide 14: 0173982 WLICS
4E is minimally marginal
No re-probe data for this lot
SWL PRE/POST

## Slide 15: Other Structure BLBL
Some marginal grps than from WLICS
SBL Ecats

## Slide 16: VT OFFSET (Balaji/John)

## Slide 17: VT OFFSET (Balaji/John)