## Slide 1: SSM Memory Switching F2F @ WW23.5
DerChang and SSM device team, WW18.3
Agenda
RWB
Cell and Array Characterization Matrix

## Slide 2: Agenda
# | Topics | Owners | Coverage
1 | RWB | Agostino | SR71 CR5.3, PR3 Quantification
2 | Basics | Fuga | Transfer Curves
3 | Drift | Enzo | UnBias vs. biased drift of set vs. reset states
4 | Disturb | Enzo | Reset and Set State
5 | Imprint | Enzo | Imprint Char: SRS, RSR, SSR, RRS
6 | Endurance | Enzo | Cycling Bathtub Curve
7 | RWB | Agostino | DTS Rev 1.0, S24S S/R gap and Strategy to Qual

## Slide 3: RWB Assessment
RWB Model
PR3
CR5.3 and Alloy14

## Slide 4: Cell Basics
Four Quadrant Transfer curve characterization: Write Polarity vs. Read Polarity
Write:
  Stimulus # 1: On-state contour based on On-state current and Duration from -30C to +110C
  Stimulus # 2: SubVt bias and duration from 25C to 300C
Read:
  VTH
  SubVt I-V scan: V@10nA, S1, S2, I0, ITH
  On-State I-V: VON@ION, rON, VOFFSET, V*, I*

## Slide 5: Array Char Flow
 | PreCon | Stess | RO Prep | RO
UD | Reset vs. Set | 1us to 48Hr | No | Vt Histo
BD | Reset vs. Set | ±SubVt bias, 1us to 10s | No | Vt Histo
RD | Reset vs. Set | VDM, 1 to 1M reads | No | Vt Histo
Imprint | Reset vs. Set | SoS vs. RoR, 1 to 1M writes | SRS vs. RSR vs. SSR vs. RRS | Vt Histo
Endurance | ±FF | 1 to 10M FW (±W cycling) | Set vs. Reset | Vt Histo

## Slide 6: Array Characterization, detailed
 | Group | PreCondition | Relaiability Stress | Read Prep. | Read Out | Description
Drift -- Unbiased | 3 | Write+ | unbiased from 1us to 48Hr@ 85C |  | Vt Histo- | UD Reset VtHisto-
Drift -- Unbiased | 4 | Write- | unbiased from 1us to 48Hr@ 85C |  | Vt Histo- | UD Set VtHisto-
Drift -- Biased | 3 | Write+ | SubVt bias+ from 1us to 10s@ 85C |  | Vt Histo- | BD Reset Bias+ VtHisto-
Drift -- Biased | 4 | Write- | SubVt bias+ from 1us to 10s@ 85C |  | Vt Histo- | BD Set Bias+ VtHisto-
Drift -- Biased | 7 | Write+ | SubVt bias- from 1us to 10s@ 85C |  | Vt Histo- | BD Reset Bias- VtHisto-
Drift -- Biased | 8 | Write- | SubVt bias- from 1us to 10s@ 85C |  | Vt Histo- | BD Set Bias- VtHisto-
Read Disturb -- Reset | 3 | Write+ | Vdm- from 1 to 1M read |  | Vt Histo- | RD Reset Read- Vt Histo-
Read Disturb -- Set | 4 | Write- | Vdm- from 1 to 1M read |  | Vt Histo- | RD Set Read+ Vt Histo-
Imprint -- Forward | 3.a | Write+ | Write+ from 1 to 1M write |  | Vt Histo- | Imprint RESET RSR (1) VtHisto-
Imprint -- Forward | 4.a | Write- | Write- from 1 to 1M write |  | Vt Histo- | Imprint SET SRS (1) VtHisto-
Imprint -- Forward | 3.b | Write+ | Write+ from 1 to 1M write | 1 W - | Vt Histo- | Imprint RESET RSR (2) VtHisto-
Imprint -- Forward | 4.b | Write- | Write- from 1 to 1M write | 1 W + | Vt Histo- | Imprint SET SRS (2) VtHisto-
Imprint -- Forward | 3.c | Write+ | Write+ from 1 to 1M write | 1 W - / 1W+ | Vt Histo- | Imprint RESET RSR (3) VtHisto-
Imprint -- Forward | 4.c | Write- | Write- from 1 to 1M write | 1 W + /1 W- | Vt Histo- | Imprint SET SRS (3) VtHisto-
Imprint -- Reverse | 3.a | Write+ | Write+ from 1 to 1M write |  | Vt Histo- | Imprint RESET RRS (1) VtHisto-
Imprint -- Reverse | 4.a | Write- | Write- from 1 to 1M write |  | Vt Histo- | Imprint SET SSR (1) VtHisto-
Imprint -- Reverse | 3.b | Write+ | Write+ from 1 to 1M write | 1 W + | Vt Histo- | Imprint RESET RRS (2) VtHisto-
Imprint -- Reverse | 4.b | Write- | Write- from 1 to 1M write | 1 W - | Vt Histo- | Imprint SET SSR (2) VtHisto-
Imprint -- Reverse | 3.c | Write+ | Write+ from 1 to 1M write | 1 W + /1 W- | Vt Histo- | Imprint RESET RRS (3) VtHisto-
Imprint -- Reverse | 4.c | Write- | Write- from 1 to 1M write | 1 W - / 1W+ | Vt Histo- | Imprint SET SSR (3) VtHisto-
Endurance -- FF+ | 3.a | FF+ | FW from 1 to 10M (End +) |  | Vt Histo- | Endruance FF+ Reset VtHisto-
Endurance -- FF- | 4.a | FF- | FW from 1 to 10M (End -) |  | Vt Histo- | Endruance FF- Set VtHisto-
Endurance -- FF+ | 3.b | FF+ | FW from 1 to 10M (End -) |  | Vt Histo- | Endruance FF+ Set VtHisto-
Endurance -- FF- | 4.b | FF- | FW from 1 to 10M (End +) |  | Vt Histo- | Endruance FF- Reset VtHisto-

## Slide 7: Backup

## Slide 8: Drift
Unbiased Drift
Do ti from 1us to 48hr {
  GP1,3: PreCon+
  GP2,4: PreCon–
  Wait ti
  GP1,2: Read+
  GP3,4: Read–
}
Unbiased Drift
Do Vinh from 3.2V to 3.8V {
  Do ti from 1us to 10s
  {
    GP1,3,5,7: PreCon+
    GP2,4,6,8: PreCon–
    Vinh+ Bias on GP1~4 for ti
    Vinh− Bias on GP5~8 for ti
    GP1,2,5,6: Read+
    GP3,4,7,8: Read–
  }

## Slide 9: Read Disturb
Reset Read Disturb
Do VDMi : from VDM to VDM-400mV {
  Do Ci from 1 to 1M Read pulses
  {
    GP1,3 : PreCon+
    GP2,4 : PreCon–
    Read– VDMi on GP1,3 for Ci
    Read+ VDMi on GP2,4 for Ci
    GP1,2: Read+
    GP3,4: Read–
  }
SET Read Disturb
Do Ci from 1 to 1M Read pulses
{
  GP1,3 : PreCon+
  GP2,4 : PreCon–
  Read+ VDM on GP1,3 for Ci
  Read– VDM on GP2,4 for Ci
  GP1,2: Read+
  GP3,4: Read–
}

## Slide 10: Imprint
“Forward” Imprint – SRS or RSR
Do PA : from PAi to 30 to 100uA {
  Do Ci from 1 to 1M Write pulses
  {
    Write+ PAi on GP1,3 for Ci
    Write– PAi on GP2,4 for Ci
    GP1a,2a: Read+
    GP3a,4a: Read–
    One Write– PAi on GP1b,3b
    One Write+ PAi on GP2b,4b
    GP1b,2b: Read+
    GP3b,4b: Read–
    One cycle –/+ PAi on GP1c,3c
    One cycle +/– PAi on GP2c,4c
    GP1c,2c: Read+
    GP3c,4c: Read–
  }
“Reverse” Imprint – SSR or RRS
Do PA : from PAi to 30 to 100uA {
  Do Ci from 1 to 1M Write pulses
  {
    Write+ PAi on GP1,3 for Ci
    Write– PAi on GP2,4 for Ci
    GP1a,2a: Read+
    GP3a,4a: Read–
    One Write+ PAi on GP1b,3b
    One Write– PAi on GP2b,4b
    GP1b,2b: Read+
    GP3b,4b: Read–
    One cycle +/– PAi on GP1c,3c
    One cycle –/+ PAi on GP2c,4c
    GP1c,2c: Read+
    GP3c,4c: Read–
  }

## Slide 11: Endurance
Do Ci from 1 to 10M FW pulses
{
  GP1,3 : FF+
  GP2,4 : FF-
  FW GP1~4 for Ci
  1 W+ on GP1a,2b,3a,4b
  1 W- on GP1b,2a,3b,4a
  GP1,2: Read+
  GP3,4: Read–
}