## Slide 1: Polarity measurements using 2xNMOS single cell devices in S15B Unbiased & Biased Induced Drift
Christina P., Koushik, Paolo, Stephen
11/25/2014

## Slide 2: Summary
Unbiased Drift:
  Drift rate is small, as expected for SDdV4.
  Voltage drop due to polarity reversal does not depend on wait time.
Biased Drift:
  Drift can be minimized when stress is applied in opposite polarity than the read pulses.
Drift dependence on polarity suggest that drift is not only bulk related effect, but interface component is present.

## Slide 3: Un-biased Drift
Flow: FFRRFFRRFFRRFF
    Where F,R : 10 read pulses with FRW & REV polarity.
WT during set up is skewed between “0” (~11sec actual), 100sec and 300sec.
The effect of the WT and Read pulses used will be quantified.
WT
10 read pulses
…
…
10 read pulses

## Slide 4: Sequence: Vary Wait time at set up
FF
FR
RF
RR
The effect of wait time will be quantified:
DeltaVT=VT_Post Wait Time_1 – VT_pre Wait Time_10

## Slide 5: Unbiased Drift: VT_shift Vs WT
All measurements show small delta VT Vs WT.
FR & RF: apart from the effect of wait time, there is an additional voltage drop due to polarity reversal.

## Slide 6: Unbiased Drift: VT_shift Vs WT (cont.)
Due to limited number of repetitions, slope cannot be measured with confidence. Devices do show drift (~30-50mV/dec for SDdV4).
Intercept captures the Delta VT due to polarity reversal; which does not depend on time. Data match well previous results (thk dependence, and FR ≥ RF).

## Slide 7: Biased-Drift
A 3.6V, 4V, 4.4V _10sec stress is introduced either in FRW or REV polarity.
    Flow: FFR FfF FfF FrF FrF FrR FrR FfR FfR,
    Where: F,R : 10 read pulses with FRW & REV polarity &
    f,r : stress with FRW & REV polarity.
f
r
DeltaVT=VT_Post Stress_1 – VT_pre Stress_10

## Slide 8: 12sec Unbiased & (3.6V-10s)Biased Drift
Please note that the stress data include 12sec of unbiased drift (this is set up time).
After 3.6V-10sec stress, drift is observable, but DeltaVt decreases as SDdV4 thickness is increased.
Lowest Drift in FrF; Stress is opposite polarity that the read pulse.
Pre-Stress read pulse: FRW POL
Additional voltage drop due to polarity reversal.

## Slide 9: Unbiased & (~72%VT_10s)Biased Drift
Pre-Stress read pulse: FRW POL
The smallest Delta VT is measured when stress is applied at REV polarity, and device is read in FRW polarity (FrF) Stress and Read should be in opposite polarities.

## Slide 11: Pad Connections for S15B_2xNMOS_Sampling Stress
Pad | Desc | Device ID
1 | Cascode | All
2 | BL-Dev1 | All
3 | PW_BOT_D1 | All
4 | Top_Gate_dev2 | All
5 | DBL | 1
6 | Gate | All
7 | DNW | 2
8 | Source | All
9 | Top Gate | All
10 | DWL | All
11 | PW_top | 1
12 | Top Cascode | 5
13 | PSUB | 2
14 | Gate-2 | All
15 | PW_BOT_D2 | 1
16 | Source-2 | All
4
3
11
9
12
15
14
2
3
6
16
8
1
1
1
12
DNW=7 globally SMU2
Des BL=5
Des WL=10
2
6
8
11
SMU1
SMU2
SMU2
SMU4
SMU3
SMU4
Gate pulser
SMU1= VBL
SMU2=6.5V
SMU3=VBL/2
SMU4=0V
scope2
FRW
SMU2
Pad 4 is connected to pad11
SMU4

## Slide 12: Details on Stress Applied
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 13: Effect of Polarity Reversal (cont.)
When devices are formed in FRW polarity, larger differences are observed. Larger differences in SDV4.
Weak thickness dependence is seen.

## Slide 14: Details on Stress Applied
As bias increases larger number of bits/per split have leakage ratio >1.
Please note that stress applied will stop if Leakage ratio>=5 or Leakage>60nA.
We will need to filter out the devices that stress was not applied.
Filtering criteria: T_stress>9.9sec, and leakage ratio<1.
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 15: Stress Applied Vs Time
Filter out all VT data where Stress was not applied for t=10sec.
REV POL
Pre-Stress read pulse: FRW POL

## Slide 16: VT_shift due to applied sub-VT stress
Lowest DeltaVT (due to bias induced drift): FrF.
FrF: REV stress shows negligible drift!
FrR: Bias induced drift + Polarity Reversal (FRW to REV).
FfF: Bias induced drift (positive)
FfR: Bias induced drift + POL Reversal (FRW to REV).
This delta is due to polarity reversal FRW to REV: for this split is expected ~0.9V
Lowest DeltaVT (due to bias induced drift): RfR.
RfR: Small drift with FRW stress.
RrR: Reverse Stress shows positive stress.
RfF: Bias induced drift + POL Reversal (REV to FRW).
RrF: Bias induced drift + POL Reversal (REV to FRW).
This delta is due to polarity reversal REV to FRW: ~0.7V
Filter out for Leakage Ratio<1: Bias induced drift.
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 17: Unbiased & Biased Drift (all data)

## Slide 18: Unbiased & (~70-75%VT)Biased Drift
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 19: Unbiased DeltaVT Vs SD thk
If first pulse is FRW, intercept is ~0, while if
First pulse is REV intercept is ~0.4-0.5V.
FR VS RF:
Thickness sensitivity ~5x higher in FR; 50mV/nm vs 10mV/nm
Intercept ~0.44V in RF, & ~0 in FR case.

## Slide 20: Effect of polarity on Bias induced Drift