## Slide 1: Polarity measurements using 2xNMOS single cell devices in S15B Test Development & Plan
Christina P., Koushik, Paolo, Stephen
11/19/2014

## Slide 2: Summary
Drift can be cancelled out when opposite polarity stress is applied.

## Slide 3: Experiment
FRW Precondition : V4STR2
REV Precondition : V4STR3
Stress 3.6V, 4V, 4.4V for 10sec
  Effect of sub-threshold stress on polarity
    Flow1: FFR FfF FfF FrF FrF FrR FrR FfR FfR,
    Flow2: FFR RfF RfF RrF RrF RrR RrR RfR RfR,
    Where f, r=stress in FRW(f), and REV(r) polarity, and
    F,R: 10 VT read pulses with Iclamp=120uA, RR=1V/us in FRW(F), and REV(R) polarity.
    F: precondition; 10 read pulses with FRW polarity.

## Slide 4: Details on Stress Applied
As bias increases larger number of bits/per split have leakage ratio >1.
Please note that stress applied will stop if Leakage ratio>=5 or Leakage>60nA.
We will need to filter out the devices that stress was not applied.
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 5: Stress Applied Vs Time
Filter out all VT data where Stress was not applied for t=10sec.
REV POL
Pre-Stress read pulse: FRW POL

## Slide 6: VT_shift due to applied sub-VT stress
Please note, we have filtered out any data where stress was not applied for 10sec.
VT measured after the stress exceeds detection limit. Devices are not open.
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 7: VT_shift due to applied sub-VT stress
Please note, we have filtered out any data where stress was not applied for 10sec.
We also filtered any high VT bits (VT>9.5V; VT detection limit).
Lowest drift: FrF
Lowest drift: RfR
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 8: VT_shift due to applied sub-VT stress
Lowest DeltaVT (due to bias induced drift): FrF.
FrF: REV stress shows negligible drift!
FrR: Bias induced drift + Polarity Reversal (FRW to REV).
FfF: Bias induced drift (positive)
FfR: Bias induced drift + POL Reversal (FRW to REV).
This delta is due to polarity reversal FRW to REV: for this split is expected ~0.9V
Lowest DeltaVT (due to bias induced drift): RfR.
RfR: Small drift with FRW stress.
RrR: Reverse Stress shows positive stress.
RfF: Bias induced drift + POL Reversal (REV to FRW).
RrF: Bias induced drift + POL Reversal (REV to FRW).
This delta is due to polarity reversal REV to FRW: ~0.7V
Filter out for Leakage Ratio<1: Bias induced drift.
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 9: Summary
Drift can be cancelled out when opposite polarity stress is applied.

## Slide 11: Pad Connections for S15B_2xNMOS_Sampling Stress
Pad | Desc | Device ID
1 | Cascode | All
2 | BL-Dev1 | All
3 | PW_BOT_D1 | All
4 | Top_Gate_dev2 | All
5 | DBL | 1
6 | Gate | All
7 | DNW | 2
8 | Source | All
9 | Top Gate | All
10 | DWL | All
11 | PW_top | 1
12 | Top Cascode | 5
13 | PSUB | 2
14 | Gate-2 | All
15 | PW_BOT_D2 | 1
16 | Source-2 | All
4
3
11
9
12
15
14
2
3
6
16
8
1
1
1
12
DNW=7 globally SMU2
Des BL=5
Des WL=10
2
6
8
11
SMU1
SMU2
SMU2
SMU4
SMU3
SMU4
Gate pulser
SMU1= VBL
SMU2=6.5V
SMU3=VBL/2
SMU4=0V
scope2
FRW
SMU2
Pad 4 is connected to pad11
SMU4

## Slide 12: VT_shift due to applied sub-VT stress
Lowest DeltaVT (due to bias induced drift): FrF.
FrF: REV stress shows negative drift!
FrR: Bias induced (negative!) + Polarity Reversal (FRW to REV).
FfF: Bias induced drift (positive)
FfR: Bias induced drift + POL Reversal (FRW to REV).
This delta is due to polarity reversal FRW to REV: for this split is expected ~0.9V
Lowest DeltaVT (due to bias induced drift): RfR.
RfR: FRW stress shows positive drift!
RrR: Reverse Stress shows negative stress.
RfF: Bias induced drift + POL Reversal (REV to FRW).
RrF: Bias induced drift + POL Reversal (REV to FRW).
This delta is due to polarity reversal REV to FRW: ~0.7V
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL

## Slide 13: Details on Stress Applied
Pre-Stress read pulse: FRW POL
Pre-Stress read pulse: REV POL