## Slide 1: What SSM gains if RWB works
DerChang, Fabio & Sandeep, WW45, 2017
Process Simplification
Performance Improvement
CMOS requirement
The big picture: Metric for EoQ4 assessment
  RWB Principles and Strategy
  Bipolar Array Architecture
  RRAM Research Benchmarking

## Slide 2: Potential Process Simplification (20nm Comparison)
SSM
SXP
SSM Potentially overcomes several SXP issues
  No cross-contamination between PM and SD
    Today: Etch done in 2 steps (First & Last Partial Etches: FP, LP) with liners deposited in between
  Lower cell aspect-ratio simplifies the cell sealing
  Lower programming current  relaxes metal (WL/BL) requirements and associated array capacitance
Aspect Ratios, including hardmask resist are estimates – useful for comparative purposes
 | 1st Cut |  | 2nd Cut | 
 | SXP | SSM | SXP | SSM
Stack height [nm] | 141 | 69 | 152 | 85
Stack Height, inc. HM [nm] | 296 | 142.6 | 297 | 191.7
Height/ Space for FP [nm] | 212.5/25.5 |  | 261/21.7 | 
Height/ Space for LP [nm] | 246/19.6 | 142.6/19.6 | 182/18.4 | 191.7/18.4
Space Aspect Ratio for FP | 6.4 |  | 6.7 | 
Space Aspect Ratio for LP | 8.4 | 4.8 | 9.1 | 5.4

## Slide 3: Preliminary Analysis on Performance Gain (20nm Comparison)
SSM
SXP
Potential for improving one of the key limiters of 3DXP: low write bandwidth (vs read and vs. DRAM)
Write latency will improve (more balanced)
Write bandwidth is only slightly improved (<10%) normalized for power, but potential headroom (~3X) for improvement, if increased power can be supported
 |  | Read |  | Write | 
 |  | SXP | SSM | SXP | SSM
Latency | ns | 105 | 105 | 465 | 175
Energy | pJ/b | 52 | 52 | 118 | 109
Latency limited BW | MB/s | 4876 | 4876 | 1101 | 2926
Power limited BW | MB/s | 1601 | 1601 | 800 | 866

## Slide 4: Circuit topology comparisons – Physical geometry insensitive RWB
WL2
WL1
BL
WL2
WL1
BL
 | READ |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | 0 | − | 0 | +
BL | + | + | − | −
WL1 | − | 0 | + | 0
 | SET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | -Vcc | +
BL | + | + | − | −
WL1 | − | +Vcc | + | -Vcc
 | RESET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | +Vcc | −
BL | + | + | + | +
WL1 | − | +Vcc | − | +Vcc
SSM
3DXP

## Slide 5: Circuit topology comparisons – Profile dependent RWB
 | READ |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | 0 | − | 0 | −
BL | + | + | − | +
WL1 | − | 0 | + | 0
 | SET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | -Vcc | −
BL | + | + | − | +
WL1 | − | +Vcc | + | +Vcc
 | RESET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | +Vcc | +
BL | + | + | + | −
WL1 | − | +Vcc | − | -Vcc
WL2
WL1
BL
WL2
WL1
BL
SSM
3DXP

## Slide 6: The Big Picture
The Metric for SSM assessment and The Expected Outcome in EoQ4 Proposal

## Slide 7: Principle of 3DXP RWB
VDM1
Window generation:
  mean to mean shift at 1us
Window consumption:
  0 to 3.54 of E2 and E3
  E2 drift from 1us to 10s (retention tacking)
  E3 shift at 12.5K FW (wear management)
VDM3 tracking (net expansion)
Window generation:
  E3 expansion from 1us to 3s
Window consumption:
  E2 drift from 10sec to
No additional consumption after drift
Developing SSM RWB Strategy
New ideas needed for VDM
Window generation:
  mean to mean shift at 1us
Window consumption:
  0 to 3.54 of E2 and E3
  Retention management
  Wear management on E2 and E3
Key Characterizations for RWB
∆VT physics – transport mechanisms, constituents vs. contaminants, interface vs. bulk
E2, E3 variability – repeatability, PA/PW (slope-1/2/3 characteristics), snapback effects (ED), bit-2-bit
E2 / E3 retention: Drift, RD, WD
Bathtub characteristics – including IPD

## Slide 8: Three Array Architecture Benchmark
Metric based on Die size, Energy and Latency Projection
S26-SXP
SR71B
S26 based - SSM

## Slide 9: Switching mechanism adjacency and Benchmark
Best Known Resistive Change Mechanism
  Interfacial barrier (VCMO, MIEC)
  Filamentation (Metal Oxide or Solid Electrolyte)
  Ferroelectricity (FeRAM, ϵeff change  EG change)
  Phase Change
  Mechanical Switches (NRAM)
Literature searches on
  “EA” of retention and electrical conductivity of states (S/R)
  “Forces” to change states