## Slide 1: Potential Process Simplification (20nm Comparison)
SSM
SXP
SSM Potentially overcomes several SXP issues
  No cross-contamination between PM and SD
    Today: Etch done in 2 steps (First & Last Partial Etches: FP, LP) with liners deposited in between
  Lower cell aspect-ratio simplifies the cell sealing
  Lower programming current  relaxes metal (WL/BL) requirements and associated array capacitance
Aspect Ratios, including hardmask resist are estimates – useful for comparative purposes
 | 1st Cut |  | 2nd Cut | 
 | SXP | SSM | SXP | SSM
Stack height [nm] | 141 | 69 | 152 | 85
Stack Height, inc. HM [nm] | 296 | 142.6 | 297 | 191.7
Height/ Space for FP [nm] | 212.5/25.5 |  | 261/21.7 | 
Height/ Space for LP [nm] | 246/19.6 | 142.6/19.6 | 182/18.4 | 191.7/18.4
Space Aspect Ratio for FP | 6.4 |  | 6.7 | 
Space Aspect Ratio for LP | 8.4 | 4.8 | 9.1 | 5.4

## Slide 2: Preliminary Analysis on Bipolar Array architecture (20nm Comparison)
SSM
SXP
Potential for improving one of the key limiters of 3DXP: low write bandwidth (vs read and vs. DRAM)
Write latency will need to also consider spike mitigation and pulse termination, up to 50ns adder. (Worst case latency limited BW: 3GB/s)
 |  | Read |  | Write | 
 |  | SXP | SSM | SXP | SSM
Die Size | mm2 | Same (200) |  |  | 
HVTs Gate oxide |  |  |  | 100Å | 100/200Å
Algo |  | Same |  | N.Write | F.Write
Latency | ns | 105 | 105 | 465 | 105~125
Energy | pJ/b | 52 | 52 | 118 | 118
Latency limited BW | MB/s | 4876 | 4876 | 1101 | 4096+
Power limited BW | MB/s | 1601 | 1601 | 800 | 800

## Slide 3: SSM POR RWB
∆VT=900mV, 1usec mean to mean shift
Sigma – limited by “intrinsic”
  SET=115mV
  Reset=125mV
Drift: (Similar to SXP)
  Single VDM – 1us~48Hr@ 85C
  550mV
20K E3 shift: 150mV (similar to SXP)
Cross Tile: 50mV (Follow SXP BKM)
Reset Read Disturb: (SSM uniquely required)
  300mV
RWB: -1V; Recovery ideas include
  Vertical Profile engineering: 300 to 600mV
  Composition optimization: 200~300mV
  Electrode Selection: ~100mV
  Program Algo such as Amplitude, Width and Termination: 100 to 300mV
  (RWB Strategy: ∆VT – 3.54∙(σSET+ σRESET) – E2 Drift – Cross Tile – E3 Shift – Reset RD GB)
Rev/ReV
For/Rev
Write/Read
Polarity
900mV
22nm 2% In-doped V12
5Å Al2O3 lamina
5Å Al2O3 lamina
15nm HUC TE
3nm HUC/7nm CNx BE
45nm BL W
37nm WL W
New x’sec SEM will be provide

## Slide 4: The Understanding of Window Components for RWB Synthesis
∆VT surviving physics: an interfacial modulation effects with bipolar operations
  Bipolar Read exhibiting parallel subVth I-V shift suggests ∆VT due to carrier injection but not bulk transport
  Bipolar Write supports mass transport model between interfaces
  Modulated by Composition skew, Etch/Vertical profile, Electrode types and Algorithm
  Insensitive to 2nd cut clean, Seal types, Pre-/Post-2nd cut anneal and passivation anneal
  VT vs. PA/PW results not matching expectation (window expansion/saturation) need to be understood
E2/E3 Variability: Intrinsically, VT repeatability of SSM is expected equal to or worse than SXP due to interface atomic fluctuations in addition to ovonic threshold bounce.
  Best exhibited VT Sigma: σSet is 115mV (105mV bounce) and σReset is 125mV (125mV bounce)
Drift: Set drift is similar to SXP; however, reset drift is ½ of Set’s.
  Dual VDM strategy of SXP is not applicable. Single VDM is POR; new VDM tracker ideas needed
Read Disturb: Immunity to Set while Reset disturb requires additional RWB margin
  Reset: ~0.3V Margin is needed to protect from 20K reads. Mechanism to be segmented
No Write Disturb issues
Endurance: Bathtub shape of E2 and E3 is similar of SXP with lower VT turnaround (detailed quantification is WIP)
Retention: WIP

## Slide 5: 2017-2018 Focus Topics
Processes: RWB understanding and Improvement
  Composition Exploration (for ∆VT & sigma)
  Profile Engineering
  SXP POR Porting
Algo and Additional S26 Stepping: improve multi-deck cell Yield interaction with Tests
  Pulse Shapes (Spike mitigation learnings comes from S26 Array)
  Dual-deck (Quad-Deck is in idea stage)
New Vehicle: SSM Product Feasibility Assessment
  20nm 256Gb/200mm2 design

## Slide 6: Backup

## Slide 7: Generation: ∆VT physics
Transport mechanisms:
  Filament (Parallel) or Bulk (Serial)
    If bulk, local movement (Å) or mass transport (nm)
  Constituents or Contaminants
Key exhibits
  for./rev. program X for./rev. read
    Subthreshold I-V  –40℃ WIP
    SR71 VT/∆VT distribution
  Temp Co, EA of subVth conduction  WIP
  TTT to establish migration models (with temp or time)  limited data, wip
  ∆VT subject to composition vs. Integration (clean, seal, bake)
  Vt-I on 2XCMOS (in 4 quadrants)
The evidences of forward vs. reverse I-V and Vt indicate an interfacial modulation effects with bipolar operations
  Not a parallel resistor network as exhibited with bipolar read  Refute filament model
  Parallel subVth I-V shift suggests carrier injection but bulk transport  Refute local structure (electronic configuration) changes (–40℃ WIP)
  Supporting mass transport model between interfaces
∆VT is
  Insensitive to 2nd cut clean, Seal type, and Pre-/Post-2nd cut & passivation anneal
  Modulated by In/Ge/Se composition skew  composition vs. 1st/2nd cut profile segmentation needed
  A function of Electrode process (HUC vs. HBC BE or C vs. CNx TE)
Inconsistency yet to be understood
  Window expansion or saturation is expected as PW/PA increases
  Negative slope on VT-PW and positive slope on VT-PA
  Follow up with
    “subVth window” vs. PA/PW
    Threshold “Point” (VTH@ITH)
    Spike Effects

## Slide 8: Consumption: E2, E3 Variability
Variability including
  Same bit: Repeatability (analog to Bounce of SXP)
  Bit-2-Bit
    circuit/device interaction such as PA/PW (slope-1/2/3 characteristics),
    Cross Tile (ED) such as snapback effects
    Deck-2-Deck offset
    Device physical differences
  Ambient: temperature
Key exhibits
  Intrinsic sigma such as bounce
  S2R “TTT” – PA, PW, and number of pulse
  R2S “TTT” – PA, PW, and number of pulse
  “ED” or cross tile
  Geometric impact: lateral, vertical and profile
  Composition learnings
  Cross vs. extrinsic contamination learnings
  Temperature effects, thermal co and EA of Vt
“corner” definitions
Intrinsically, VT repeatability of SSM is expected equal to or higher than SXP due to interface atomic fluctuations in addition to ovonic threshold bounce
  VT σSet is ~25mV and σReset is ~45mV higher than SXP’s (80mV)
  Higher PA lower VT σ; insensitive to PW
ED dependence: systematic – near ED lower Vt
  Follow-up: Spike Mitigation, BL/WL RC skew and Electrode (local R) experiment
Physical Geometry
  Strong correlation on vertical profile – lower window with straight profile but insensitive to thickness and CD
Integration  Lower sensitivity to foreign containment if any
  52, 69 or 80 anneal is insensitive to ∆VT (2XCMOS data, SR71 WIP)
  BL clean, Seal thickness, temp or treat shows low impact to ∆Vt
SD Composition
  In and Ge doping increases ∆VT
  Convoluted with vertical profile, to be segmented
Corner definition is yet to be developed

## Slide 9: Retention/Disturb: Drift, RD, WD
Drift characterization
  Set and Reset states
  UD and BD
  1u up to 48Hrs
  EA
Read Disturb and more
  Set State: Analog to Set on Set (or Reset on Reset?)
    PW vs. number of pulses
  Reset State: RD retention
Write Disturb
  Set and Reset state
  EA
Rainbow characteristics
  EA of Set and Reset state retention
Drift
  Reset UnBias Drift is ~½ of Set’s
  Bias Drift of E2 is similar to SXP
  SXP drift Tracker cannot be deployed
Read Disturb
  Reset Retention: ~0.3V Reset Margin is needed to protect from 20K reads.
    Mechanism to be segmented
  Tolerant to Set state:
    ~100mV@10M reads (Iclamp=30uA);
    Higher spike and/or read current, higher shift
No Write Disturb issues
WIP: EA of drift and Retention

## Slide 10: Endurance: Bathtub characteristics
Interlaced cycling (+60/-60 uA):
Median Vth evolution
Interlaced cycling is not time cumulative but spike (# of cycle) driven
Bathtub shape is similar of unipolar cycling
~100mV/dec
IPD
Pulses #
Interlaced cycling (+60/-60 uA): Median Vth evolution
20ms
2s
20s
RESET
SET
Vth evolution with unipolar cycling,
+60uA 140ns square pulses
Median Vth evolution
Vth goes down increasing IPD but sigma goes up

## Slide 11: Supporting Materials

## Slide 12: Critical path for SSM Strategy development Plan18 of SOW Approval Need date: WW47
SSM Physics
  Models of memory windows at first principle and the ranking.
  Each model must examine the following attributes against the best known memory research with a self-consistent rigor .
  Drift fundamentals such as constituents vs. contaminants actions in window evolutions
  Read/Write disturb mechanisms
  Corner case understanding
  Window subject to pulsing (polarity, amplitude, transient and duty)
  Solidify window budget principles to establish pathfinding strategy
  Scalability in window budget, disturbs, energy, physical dimensions and speed
  Algorithm learning in device physics and circuit interactions
Complete data collection in benchmarking/referencing to 3DXP, including
  S26 Array probe
  S26 Array WLR
  Bath-Tub curves of cycling/bake/re-cycling
  Probe platform, data collection and infrastructure