## Slide 1: Self Selector Memory (SSM)
Al Fazio
October 2017
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 2: Self Selector Memory (SSM)
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 3: 3D XPoint™: Memory + Selector Device
WL: Tungsten Wordline
BL: Tungsten Bitline
PM: Phase Change Memory
SD: Ovonic Threshold Device Select Device
Vprog
0 V
Vprog/2
Vprog/2
Vprog/2
Vprog/2
Isolation
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
1 BL Sockets
2 WL Sockets
WL
WL
WL
WL
WL
WL
BL
BL
1st Generation (20nm): 2 Decks 128Gbit
+V
-V
Isolation
2 BL Sockets
2 WL Sockets
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
PM
SD
WL
WL
WL
BL
WL
WL
WL
BL
WL
WL
WL
BL
WL
WL
WL
BL
2nd Generation (20nm): 4-Decks 256Gbit
+V
-V
3rd Generation (14nm): 4 Decks 512Gbit
Selector Device ensures high performance in terms of leakage and single cell selection
Memory element permits to store information using two stable states
Each deck is a repeat (process) of lower deck, but operated in reverse polarity
Each deck is always operated in the same uni-polar bias for read/write (not bi-polar per deck)
Cross point requires very good selector

## Slide 4: Ovonic Threshold Switch (SD) Polarity Effect
A VT window has been observed by applying programming pulses to the SD device with opposite polarity
Positive programming pulse
Negative VT detection  VT=5.6V  VTHigh
Negative programming pulse
Negative VT detection  VT=4.7V  VTLow
VT_High
VT_Low
S15B SD-only, lot 8792062, 18nm SDd ver 4
SxP
W WL
Carbon
SD
Carbon
PM
Carbon
W BL
W lamina
W WL
Carbon
SD
Carbon
W BL
SSM
Leads to possibility of a self-select-memory (SSM) of a single chalcogenide layer that has low field leakage, cell selection and stores information

## Slide 5: Self Selector Memory (SSM)
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 6: Potential Process Simplification (20nm Comparison)
SSM
SXP
SSM Potentially overcomes several SXP issues
  No cross-contamination between PM and SD
    Today: Etch done in 2 steps (First & Last Partial Etches: FP, LP) with liners deposited in between
  Lower cell aspect-ratio simplifies the cell sealing
  Lower programming current  relaxes metal (WL/BL) requirements and associated array capacitance
Aspect Ratios, including hardmask resist are estimates – useful for comparative purposes
 | 1st Cut |  | 2nd Cut | 
 | SXP | SSM | SXP | SSM
Stack height [nm] | 141 | 69 | 152 | 85
Stack Height, inc. HM [nm] | 296 | 142.6 | 297 | 191.7
Height/ Space for FP [nm] | 212.5/25.5 |  | 261/21.7 | 
Height/ Space for LP [nm] | 246/19.6 | 142.6/19.6 | 182/18.4 | 191.7/18.4
Space Aspect Ratio for FP | 6.4 |  | 6.7 | 
Space Aspect Ratio for LP | 8.4 | 4.8 | 9.1 | 5.4

## Slide 7: Process simplification  Lower Cost & Further Opportunities
Definite: Removes all the PM related process cost (deposition, etch, liner, etc)
Possibility #1: Further Lower Cost Opportunities become potentially viable
  Lower mask count process: N+1 critical masks (vs. 2N) for N decks (use 2 step SXP-like etch/liner for 2 SSM decks)
Possibility #2: Potential for “3D-NAND-like” Cross-point array architecture, for lower cost
  Thinner/simpler stack might be possible for lateral cell (vs planar / subtractive in SXP)
  ALD required for SD switch (does not exist)
  Power/Performance unknown w/ larger array RC
    3D NAND-like architecture for RRAM was not as good as our present SXP approach when we explored in past
    Never as low cost as 3D NAND (NAND = MLC/TLC/QLC)
Replace floating gate Transistor of 3D NAND with SSM;
Replace channel with metal.
We think can work with FG NAND flow, but may require RG??

## Slide 8: Performance Gain (20nm Comparison)
SSM
SXP
Potential for improving one of the key limiters of 3DXP: low write bandwidth (vs read and vs. DRAM)
Write latency will improve (more balanced, with typical compute workload of 2:1 read:write)
Write bandwidth is only slightly improved (<10%) normalized for power, but potential headroom (~3X) for improvement, if increased power can be supported
 |  | Read |  | Write | 
 |  | SXP | SSM | SXP | SSM
Latency | ns | 105 | 105 | 465 | 175
Energy | pJ/b | 52 | 52 | 118 | 109
Latency limited BW | MB/s | 4876 | 4876 | 1101 | 2926
Power limited BW | MB/s | 1601 | 1601 | 800 | 866

## Slide 9: Self Selector Memory (SSM)
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 10: Recently attained Array Testing (vs previous single cell) confirming distributions
SD-polarity effect deeply investigated on S15 silicon single cells
Main vehicle for the assessment is the SR71B test chip on S26A test pattern
  2x256kb test chip arrays (active cells are spread inside a 2x4Mb physical arrays) with dual polarity program capability and single polarity read
  Experiments are usually run on 32x32 cells sub-arrays (1kb statistics, 3 sigma visibility)
SSM flow is based on S26A SxP process  24 SSM lots out and tested up to now
New revision of SR71B with full bipolar capabilities (programming and reading) on A1 mask set
256kb active array
(physical array is 4Mb)

## Slide 11: Endurance & Distributions
Good endurance preliminary results up to 9Mcycles
1C
1C

## Slide 12: SSM Research Key Issue Summary
+ (good news)
  Write Disturb (Thermal heating of adjacent cell), issue on SXP, demonstrated not present on SSM
- (bad news)
  Read Disturb of high Vt state – new mechanism for SSM, not present in SXP – has to be comprehended in Vt window budgeting
  Drift is as anticipated, but also means we can’t exploit physics on SXP, where RESET state has two amorphous states (SD + PM), that drift faster and opens window  SSM is a smaller window.
    Drift tracker concept we use on SXP System ASICs not directly usable
512K cycles Write Disturb
Reset Read Disturb
Set/Reset Drift

## Slide 13: Self Selector Memory (SSM)
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 14: Don’t Know Basic Physics…yet
Switching mechanism not know  lack the physics to guide our risk assessments / understanding
  Several speculations, but only speculations, e.g. ferroelectric-like atomic movement, contaminant movement causing interface barrier modulation, is it similar to ReRAMs (which we do not favor)???
  SD difficult to atomically probe (TEM energy changes distribution); electrical fingerprinting has been limited thus far
Scalability not known, nor can we speculate without a basic physical model or empirical data
Can 1’s0’s Vt window be made large enough to be manufacturable?
Multi-deck results not yet attained: Are the effects solely due to geometry effects?

## Slide 15: Don’t Know Circuit Topology to Fit CMOS under Array…yet
SXP has all CMOS under array for each sub-tile (decoders, sense circuits, etc).
Not fitting CMOS  blows up die size??
Bi-polar operation adds transistors to critical pitch circuits under the array
Design / CMOS analysis has not yet started
SXP cross section: array + circuits under tile

## Slide 16: Self Selector Memory (SSM)
Basic Concept Intro
Assuming it works, what do we gain?
Key things we know
Key things we DON’T know
Next Steps

## Slide 17: Next Steps
Intel-Micron JDP looking to step-up SSM activities (from low level research)
Attempt to “fail fast”…or succeed fast
“POR is POR until we change the POR”
  POR roadmap for 3rd generation = SXP POR
    Scaled to 14nm

## Slide 18: Backup

## Slide 19: Circuit topology comparisons – Physical geometry insensitive
WL2
WL1
BL
WL2
WL1
BL
 | READ |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | 0 | − | 0 | +
BL | + | + | − | −
WL1 | − | 0 | + | 0
 | SET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | -Vcc | +
BL | + | + | − | −
WL1 | − | +Vcc | + | -Vcc
 | RESET |  |  | 
 | 3DXP |  | SSM | 
 | Lower Deck | Upper Deck | Lower Deck | Upper Deck
WL2 | +Vcc | − | +Vcc | −
BL | + | + | + | +
WL1 | − | +Vcc | − | +Vcc
SSM
3DXP

## Slide 20
(120nm)2
(45nm)2
J [A/nm2]
V [Volts]
Full-STACK
Electrode only
V [Volts]
J [MA/cm2]
48
32
16
64
Bottom
Electrode
Top
Electrode
BE
TE
Near Threshold
BE
TE
Threshold,
(positive feedback)
Snapback Regime
TE
BE
On-state
1.7
BE
TE
3.0eV
4.4eV
φB=.85eV
EF
1.7eV
TE
BE
SubThreshold
PF conduction
3D XPointTM Selector Element : Ovonics Threshold Switch
Selector
Amorphous Semiconductor