## Slide 1: SSM and Bipolar Architecture
DerChang & Balaji, WW15.4/2018
What is SSM and what we (think we) know
How is it different from SXP
How does it benchmark with other RRAM
Bipolar decoder and architecture

## Slide 2: Content
What is SSM and what we (think we) know
How is it different from SXP
How does it benchmark with other RRAM
Bipolar decoder and architecture

## Slide 3: Introduction to SSM
VT,High
VT,Low
S15B SD-only, lot 8792062, 18nm SDd ver 4
Positive
Write
Negative
read
Negative
Write
Negative
read
Pulse Polarity
TE
BE
SD
Self Select Memory, a.k.a. SSM, is a SD only memory cell.
Physical construction of SSM is X-Y cross point array BEOL stackable, compatible with mainstream CMOS.
Read/write is to threshold a cell in a tile while the rest of cells are inhibited in subthreshold bias.
It exhibits a window (∆VT) by applying programming pulses with opposite polarity.
The best known ∆VT physics is an electrochemical potential modulation due to mass transport by polarity.
Since the memory and selector are built-in with single elelement, hence Self-Select Memory is coined.
−/−
+/−
Write/Read
Polarity
900mV
+/+
−/+
VTH [mV]
σ of bit distribution

## Slide 4: Electrical Equivalent Circuit and Possible Underline Physics
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. The best known ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Near parallel shift on SubVt I-V between opposite polarities
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
From empirical to physical
  Write –Band offset switching subject to mass transport.
  Read – Space Charge modulation results in voltage shift
SD Resistor
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Post
Neg
Write
0V
(−)
Read Polarity

## Slide 5: Content
What is SSM and what we (think we) know
How is it different from SXP
How does it benchmark with other RRAM
Bipolar decoder and architecture

## Slide 6: SXP vs. SSM – Cell Architecture (20nm Comparison)
SSM
SXP
SSM potentially overcomes several SXP issues
  No cross-contamination between PM and SD
  Lower cell aspect-ratio simplifies the cell sealing
  Lower programming current  relaxes metal (WL/BL) requirements and associated array capacitance
 | 1st Cut |  | 2nd Cut | 
 | SXP | SSM | SXP | SSM
Stack height [nm] | 141 | 69 | 152 | 85
Stack Height, inc. HM [nm] | 296 | 142.6 | 297 | 191.7
Height/ Space for FP [nm] | 212.5/25.5 |  | 261/21.7 | 
Height/ Space for LP [nm] | 246/19.6 | 142.6/19.6 | 182/18.4 | 191.7/18.4
Space Aspect Ratio for FP | 6.4 |  | 6.7 | 
Space Aspect Ratio for LP | 8.4 | 4.8 | 9.1 | 5.4

## Slide 7: SXP vs. SSM – Array Architecture (20nm Comparison, Sharing Partition Architecture)
SSM
SXP
Potential for improving one of the key limiters of SXP: High Write completion time (vs Read latency)
Write latency may need to also consider spike mitigation and pulse termination, up to 50ns adder. (Worst case latency limited BW: 3GB/s)
No MLC capability identified with demarcation read algorithm
 |  | Read |  | Write | 
 |  | SXP | SSM | SXP | SSM
Die Size | mm2 | 197 |  |  | 
Algo |  | Same |  | N.Write | F.Write
Latency | ns | 95 | 95 | 465 | 95~125
Energy | pJ/b | 52 | 52 | 118 | 118
Latency limited BW | MB/s | 5389 | 5389 | 1101 | 4096+
Power limited BW | MB/s | 1601 | 1601 | 800 | 800

## Slide 8: SXP vs. SSM – Algorithm
PW
T0 - Selection
T1 – nucleation
T3 growth
T4
P1
P3
T0 - Selection
T1
T4
P1
P4
Sense
Data transfer to IO
essr
Setback
Occupancy
TSENSE
Sense
Data transfer to IO
Occupancy
TSENSE
SSM
SXP
READ
SET
RESET
T0 - Selection
T1
T4
P1
P4

## Slide 9: 3DXP Projects
Project | Architecture |  | PLC
S15 | Cell | 20nm SXP, Unipolar, SLC | α-product 128Gb PG4 Qual’d, PG1 Q1/18 Qual
 | Tile | 2-deck 2Kx4K, 1b/tile | 
 | Core | 128b/partition, 4-slice, 16-partition | 
 | Component | R1600/W550 MB/s, DDR4 | 
S26 | Cell | 20nm SXP, Unipolar, SLC | α-product 256Gb Q2/18 PG4 Qual Q3/18 PG1 Qual Chop = low cost S15
 | Tile | 4-deck 4Kx4K Quilt, 1b/tile | 
 | Core | 128b/partition, 1-slice, 32-partition | 
 | Component | R1600/W800 MB/s, DDR4 | 
S37 | Cell | 14nm SXP, Unipolar, SLC | XP03: CMOS/BEOL development S36X: Spider based on S26 CMOS α-product 512Gb DBR Q4/18 Chop = DDR5 low cost S26 Phase 2: R4800/W1600 MB/s
 | Tile | 4-deck 4Kx4K Quilt, 1b/tile | 
 | Core | 128b/partition, 2-slice, 32-partition | 
 | Component | R3200/W1100 MB/s, DDR5 | 
SSM (S26S as placeholder) | Cell | 20nm SSM, Bipolar, SLC | SR71B for cell fundamental learning S24S for array feature development α-Product decision pending on design and process development
 | Tile | 4-deck 4Kx4K Quilt, 1b/tile | 
 | Core | 128b/partition, 1-slice, 32-partition | 
 | Component | R1600/W800 MB/s, DDR4 | 

## Slide 10: An possibility into 3D-NAND Like Scaling
Scaling Expectation
  Density: doubling every generation
  Latency: equal or reduce
  Bandwidth/GB: Equal or improve
Expected Roadmap
Beyond S48S
  Reference architecture: SXP stack vs. 3D-NAND tier
  Scalable architecture development starts when 1. Switching mechanism is manageable and 2. 20nm Product Vehicle is DBR’d
3D-tier
3D-stack
 | S26S | S37S | S48S
Density/Die Size | 256Gb / 197mm2 | 512Gb / 195mm2 | 1Tb /<200mm2
half pitch | 20.5nm | 14nm | 10.25nm
Read/Write Latency | 95/240 ns | 80/240 ns | 80/80~120 ns
Read/Write Energy | 52/118 pJ/b | 26/59 pJ/b | 13/30 pJ/b
Read/Write Thruput | 1600/800 MB/s | 3200/1600 MB/s | 6400/3200 MB/s
I/O and Transfer Rate | DDR4 1600MT/s | DDR5 3200MT/s | DDR5 6400MT/s

## Slide 11: Content
What is SSM and what we (think we) know
How is it different from SXP
How does it benchmark with other RRAM
Bipolar decoder and architecture

## Slide 12: Classes of “Ducks”
2-T NVM (focus on memory element)
PCM (Samsung, Micron, IBM/Macronix)
SSM (Intel/Micron)
VMCO/CMOx (IMEC, Unity)
  4DS: PCMO (CMOSx) with HGST/WD partnership?
  WD/Toshiba: Binary conductive oxide instead of PCMO
  IMEC: VMCO
  CMOx: Unity (Rambus)
VORAM/CBRAM (Redox)
  Weebit: Porous SiO, TaO
  Panasonic/Fujitsu/HP: TaO
  TSMC/ITRI: HfO
  Macronix: WO
  Adesto: Te in AlO
  Micron/Sony: Cu in GdO
  NEC: Cu in oxide(?) – targeting FPGA
  Crossbar: Ag/Cu in α-Si (with Si/SiO diode)
STT (too many)
FTJ
  Toshiba: HfO + interface layer
  AIST consortium: UoTokyo and etc
Other NVM (not benchmarked)
SXP-like
  Intel/Micron
  Macronix/IBM: Si-STAG + N doped 225
  Hynix: As doped SiO + ReRAM(?)
  IMEC: N doped GeSe (selector only)
  LETI: GeSe + HfO
FECAP as in 1T1C
  IMEC, NAMLAB (GF), MFC, Hynix/LAM : HfO
  TI: PZT in production/ research HfO
  Panasonic: PZT in production
  Sony: SBT in production
FEFET
NRAM (Nantero)
Charge trap
See also: https://en.wikipedia.org/wiki/Resistive_random-access_memory
https://semiengineering.com/what-happened-to-reram/
https://semiengineering.com/a-new-memory-contender/ (FECAP/FEFET)

## Slide 13: “Hysteresis” of Transfer characteristics
Hysteresis: Output traces subject to input and prior history in a cyclic loop SRAM PCM
Transfer characteristics:
  Input (WRITE) metrology actuates the switching mechanism
  Output (READ) metrology manifests the switched physics
Comparing RRAMs with the similar transfer characteristics to construct physical hypothesis
i/p
o/p
i/p [v]
o/p [v]
Pulse [μA]
VT [v]

## Slide 14: PCM
Write: Polarity symmetry
  Current pulse from 5 to 40 MA/cm2 (20~160uA of 20nm cell)
  Pulse width from 10ns to 200nsc
  Typical Imelt ~15MA/cm2
  Typical Isat ~ 25 MA/cm2
Read: Polarity symmetry
  Vt detect, either by SCU 30ns pulse or QS I-V scan for 1uA or snapback detect, in both polarity.
  Typical Set Vt is ~0.1V
  Typical Reset Vt is ~1V
Pulse width effect
  Insignificant impact from low to high Vt
  Strong influence from high to low Vt
Polarity Symmetry: Axial symmetry both in read and write
Pulse [μA]
VT [v]
Pulse [μA]
❷
❶
❸
❹
10ns
200ns

## Slide 15: PCM
Pulse [μA]
Log(I@0.4V]
Pulse [μA]
❷
❶
❸
❹
10ns
200ns
Pulse [μA]
VT [v]
Pulse [μA]
❷
❶
❸
❹
10ns
200ns

## Slide 16: SSM
Write:
  Current pulse from 7.5 to 25 MA/cm2 (30~100uA of 20nm cell)
  Pulse width from 20ns to 500nsc
Read
  FVMI or Vt detect, either by SCU 30ns pulse or QS I-V scan for snapback detect, in both polarity.
  Typical Set Vt is ~4.8@22nm
  Typical Reset Vt is ~5.7V@22nm
Insignificant pulse width effect on the range explored (20ns to 500ns)
Polarity Symmetry: Point Refection at origin
Pulse [μA]
VT [v]
Pulse [μA]
Log(I@3.5V)
≈
≈
❷
❶
❸
❹
Slope 1~5KΩ

## Slide 17: Transfer Charx Summary
Pulse [μA]
Log(I@0.4V]
❷
❶
❸
❹
Pulse [μA]
Log(I@3.5V)
Pulse [V]
Log(I@0.5V)
❷
❶
❸
❹
Pulse [V]
I@0.1V
Pulse [V]
Log(I@3V)
❷
❶
❸
❹
PCM
SSM
VMCO/CMOx
VORAM/CBRAM
STT
FTJ
❷
❶
❸
❹
❷
❶
❸
❹
Pulse [V]
Log(I@3V)
❷
❶
❸
❹

## Slide 18: Content
What is SSM and what we (think we) know
How is it different from SXP
How does it benchmark with other RRAM
Bipolar decoder and architecture

## Slide 19: Unipolar vs. Bipolar
Unipolar
Bipolar

## Slide 20: Challenge in Decoder Size & Energy
Invention | Architecture & Key Features | Problem addressed | Embodiments
Current Art of Unipolar Architecture | One MOSFET to select or inhibit in each of global decoder | Best Known Architecture for most compact decoder (die size) and lowest operation energy | S26A POR
Current Art of Bipolar Architecture | Inverters for global select and inhibit bias for bipolar operation, one inverter for each polarity | To address bipolar bias for wordline and bitline potential but double transistor count for global decoder & higher operating energy required | SR71 POR S24S POR
Idea #1 | Global bipolar select bias and one MOSFET for global inhibit bias | To reduce global decoder footprint and reduce energy from current art of bipolar architecture | Embodiment #1 Embodiment #2
Idea #2 | Global bipolar select bias and one MOSFET for global inhibit bias with additional high voltage MOSFET | To further reduce operating energy of idea #1 And reduce address transition sequencing | Embodiment #3 Embodiment #4 Embodiment #5 Embodiment #6

## Slide 21: Embodiments of Bipolar Decoder
“TO”  HV Transistor
Embodiment1
Embodiment2
Embodiment3
Embodiment4
Embodiment5
Embodiment6
S24S POR
SR71 POR
S26A POR

## Slide 22: S24S decoder
Uses separate paths to support positive and negative polarity biases.

## Slide 23: Voltage Stress
Oxide Stress MAX (purple)
  VPP or |VNN|
Jn Stress MAX (green)
  VPP-VNN
POSITIVE POLARITY
POSITIVE POLARITY
VSS
VPP
“Uses S26S CMOS”
NEGATIVE POLARITY
NEGATIVE POLARITY
VPP
VSS
Selected decoder
Deselected decoder
Selected decoder
Deselected decoder

## Slide 24: Why S24S decoder has higher energy?
Deselects gates need to toggle from VPP  VNN
or VNN  VPP when switching polarity.
This node has high fanout causing a large CV^2 component of energy when compared with the POR S26A. ~50% higher.