## Slide 2
 | 27nm CB RAM | 20nm SSM | 40nm Panasonic | ¼𝛍m Adesto | 40nm VMCO | Cross Bar | Hynix
Cell size (effective) | 6 (13.4) λ2 | 4 (1.68)λ2 | (Prashant) |  | 4λ2 | 4λ2 | 4λ2
Density | 16Gb` | 128~256Gb | 8Mb | 2Mb |  |  | 
Read Energy |  | 52pJ/b |  |  |  |  | 
Write Energy |  | 180pJ/b  120pJ/b |  |  |  |  | 
Technology ? | 1T1R | Self select | 1T1R | 1T1R | Self select |  | 
Circuit/product | 5V | 8V | 5V | 3V | 7V |  | 
Scalability | Transistor limited | Litho limited | Transistor limited | Transistor limited | (40nm)2 ,no array Sigma limited |  | 
Cross Point | In planning with Sony’s OTS (BCx) | SD | No visibility | No visibility | VMCO, nonlinearity |  | 
3D NAND like | Cu is limiter | SAG/Carbon | n/a | n/a | n/a |  | 

## Slide 3: Key issues on S24S and Solution Guesstimate
 | S26A | S24S | alpha@ 20nm | BGM
Density @200mm2 | 256Gb 4D | 32Gb 2D | 256Gb 4D | 
Read Energy [pJ/b] | 52 | > 52 (reset to read) |  | 
Write Energy [pJ/b] | 118 | 180 |  | 
Reset Read Disturb | 3K/300mV GB |  |  | 
Write inhibit Disturb |  |  |  |