## Slide 1: TL170627003
S26A SSM (SD-only) In-Doped SD with 2x AlOx lamina TEM Analysis -- post 51 WL seal (AUTOSTEM prep)
Prepared by : Ning Lu

## Slide 2: Job Description
SD only SSM flow on S26A WL etch development with In doped SD stack; PROD SWR # 8412604 group 8E: wf#25 SSM SD 22nm 2% In; 5A AlOx lamina top and bot dual airbreak; 23s SD etch no SO2; 18/25s W etch Need EDS composition estimates, maps, and line scan across TE,BE and SD. Including Si/O/N/Al maps in addition to chalc. composition elements.
Item# | Lot# | Wafer# | Part Type | Location | Direction | Remarks
010 | 9971352.0M3 | 25 | S26A | Center | X-Direction | 
020 | 9971352.0M3 | 25 | S26A | Edge | X-Direction | 
030 | 9971352.0M3 | 25 | S26A | mid-radius | X-Direction | 

## Slide 3: Sample ID :
Item# | Lot# | Wafer# | Part Type | Location | Direction | Remarks
010 | 9971352.0M3 | 25 | S26A | Center | X-Direction | 

## Slide 4
TEM Image

## Slide 5
TEM Image

## Slide 6
TEM Image

## Slide 7
TEM Image

## Slide 8
STEM Images

## Slide 9
STEM Images

## Slide 10
STEM Images

## Slide 11
STEM Images

## Slide 12
EDS Elemental Maps

## Slide 13
EDS Elemental Maps

## Slide 14
EDS Line Scanning Profile

## Slide 22: Sample ID :
Item# | Lot# | Wafer# | Part Type | Location | Direction | Remarks
020 | 9971352.0M3 | 25 | S26A | Edge | X-Direction | 

## Slide 23
TEM Image

## Slide 24
TEM Image

## Slide 25
TEM Image

## Slide 26
TEM Image

## Slide 27
STEM Images

## Slide 28
STEM Images

## Slide 29
STEM Images

## Slide 30
STEM Images

## Slide 31
EDS Elemental Maps

## Slide 32
EDS Elemental Maps

## Slide 33
EDS Line Scanning Profile

## Slide 41: Sample ID :
Item# | Lot# | Wafer# | Part Type | Location | Direction | Remarks
030 | 9971352.0M3 | 25 | S26A | mid-radius | X-Direction | 

## Slide 42
TEM Image

## Slide 43
TEM Image

## Slide 44
TEM Image

## Slide 45
TEM Image

## Slide 46
STEM Images

## Slide 47
STEM Images

## Slide 48
STEM Images

## Slide 49
STEM Images

## Slide 50
EDS Elemental Maps

## Slide 51
EDS Elemental Maps

## Slide 52
EDS Line Scanning Profile

## Slide 60
Job ID | Sample ID | Lot ID | Wafer ID | Part Type | Location | Cut Dir | Bit | SD Ge | SD As | SD Se | SD In
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 1 | 13.38 | 25.76 | 55.08 | 5.78
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 2 | 13.66 | 25.37 | 55.33 | 5.64
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 3 | 13.6 | 25.73 | 55.06 | 5.61
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 4 | 13.54 | 24.67 | 55.89 | 5.9
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 5 | 13.28 | 25.25 | 55.99 | 5.49
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 6 | 13.55 | 25.61 | 55.6 | 5.24
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 7 | 12.74 | 26.1 | 55.14 | 6.01
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 8 | 13.07 | 25.97 | 55.89 | 5.07
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 9 | 13.57 | 25.6 | 55.6 | 5.23
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 10 | 12.97 | 25.63 | 56.09 | 5.31
EDS Element Composition Estimate: at.%

## Slide 61
Job ID | Sample ID | Lot ID | Wafer ID | Part Type | Location | Cut Dir | Bit | SD Ge | SD As | SD Se | SD In
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 1 | 13.21 | 25.34 | 55.23 | 6.22
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 2 | 13.61 | 25.37 | 55.2 | 5.82
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 3 | 13.61 | 25.37 | 55.27 | 5.74
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 4 | 12.74 | 26.16 | 55.23 | 5.86
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 5 | 13.3 | 25.67 | 54.9 | 6.14
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 6 | 13.42 | 25.45 | 54.98 | 6.14
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 7 | 13.05 | 25.08 | 55.77 | 6.1
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 8 | 13.29 | 25.35 | 54.84 | 6.53
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 9 | 13.12 | 26.23 | 54.62 | 6.03
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 10 | 13.17 | 25.51 | 54.48 | 6.85
EDS Element Composition Estimate: at.%

## Slide 62
Job ID | Sample ID | Lot ID | Wafer ID | Part Type | Location | Cut Dir | Bit | SD Ge | SD As | SD Se | SD In
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 1 | 13.04 | 25.21 | 56.19 | 5.56
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 2 | 13.54 | 25.27 | 55.3 | 5.89
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 3 | 12.85 | 24.64 | 56.32 | 6.19
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 4 | 13.36 | 24.72 | 56.17 | 5.75
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 5 | 12.88 | 25.2 | 56.37 | 5.54
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 6 | 13.02 | 25.92 | 55.22 | 5.84
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 7 | 13.41 | 24.8 | 56.07 | 5.72
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 8 | 13.83 | 24.61 | 55.75 | 5.81
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 9 | 13.51 | 25.75 | 55.2 | 5.55
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Mid-radius | D0; X | 10 | 13.31 | 25.35 | 55.37 | 5.97
EDS Element Composition Estimate: at.%

## Slide 63
Calibrated SD composition estimate: at.% (calibrated based on ICP composition in TL170621002)
Center of wafer, Si concentration is assumed to be 7 at% in SD
Job | Sample | Lot | Wafer | Part Type | Location | Cut | Bit | SD | SD | SD | SD | SD
ID | ID | ID | ID |  |  | Dir |  | Ge | As | Se | In | Si
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 1 | 13.00 | 23.92 | 52.96 | 3.12 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 2 | 13.29 | 23.47 | 53.05 | 3.19 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 3 | 12.97 | 23.75 | 53.35 | 2.93 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 4 | 12.93 | 23.25 | 53.80 | 3.02 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 5 | 12.83 | 23.73 | 53.65 | 2.78 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 6 | 13.03 | 23.44 | 53.95 | 2.59 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 7 | 12.68 | 24.30 | 53.32 | 2.70 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 8 | 13.03 | 23.82 | 53.53 | 2.62 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 9 | 13.01 | 24.20 | 53.15 | 2.64 | 7
TL170627003 | 010 | 9971352.0M3 | 25 | S26A | Center | D0; X | 10 | 12.90 | 23.86 | 53.54 | 2.70 | 7

## Slide 64
Calibrated SD composition estimate: at.% (calibrated based on ICP composition in TL170621002)
Edge of wafer, Si concentration is assumed to be 7 at% in SD
Job | Sample | Lot | Wafer | Part Type | Location | Cut | Bit | SD | SD | SD | SD | SD
ID | ID | ID | ID |  |  | Dir |  | Ge | As | Se | In | Si
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 1 | 12.85 | 23.12 | 53.94 | 3.09 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 2 | 13.23 | 23.28 | 53.36 | 3.12 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 3 | 13.62 | 23.03 | 53.33 | 3.03 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 4 | 13.04 | 23.34 | 53.55 | 3.07 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 5 | 13.02 | 23.97 | 52.99 | 3.01 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 6 | 13.17 | 23.55 | 53.22 | 3.06 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 7 | 12.87 | 23.15 | 53.75 | 3.23 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 8 | 13.00 | 23.69 | 53.02 | 3.28 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 9 | 13.05 | 23.62 | 53.09 | 3.25 | 7
TL170627003 | 020 | 9971352.0M3 | 25 | S26A | Edge | D0; X | 10 | 13.02 | 23.27 | 53.34 | 3.37 | 7

## Slide 65
Calibrated SD composition estimate: at.% (calibrated based on ICP composition in TL170621002)
Middle of wafer, Si concentration is assumed to be 7 at% in SD
Job | Sample | Lot | Wafer | Part Type | Location | Cut | Bit | SD | SD | SD | SD | SD
ID | ID | ID | ID |  |  | Dir |  | Ge | As | Se | In | Si
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 1 | 12.77 | 23.29 | 54.03 | 2.91 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 2 | 13.06 | 23.07 | 53.78 | 3.09 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 3 | 12.72 | 22.94 | 54.43 | 2.90 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 4 | 13.21 | 23.06 | 53.81 | 2.92 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 5 | 13.21 | 23.06 | 53.81 | 2.92 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 6 | 12.96 | 23.19 | 53.74 | 3.11 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 7 | 12.79 | 23.54 | 53.68 | 2.99 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 8 | 12.75 | 23.39 | 53.87 | 2.99 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 9 | 13.22 | 22.94 | 53.89 | 2.95 | 7
TL170627003 | 030 | 9971352.0M3 | 25 | S26A | Middle | D0; X | 10 | 12.99 | 23.22 | 53.81 | 2.98 | 7