## Slide 1: TL170718004
SD only SSM flow on S26A WL etch development with In doped SD stack; PROD SWR # 8527404 group 3E,4E:
Prepared by : Hongqi Li/John Jin

## Slide 2
Job Description
wf#25 group 3E: SSM SD 22nm 2% In; 21s SD etch no SO2; 15/22s W etch wf#23 group 4E: SSM SD 22nm 5% In; 21s SD etch no SO2; 15/22s W etch Need EDS composition estimates, maps, and line scan across TE,BE and SD. Including Si/O/N/Al maps in addition to chalc. composition elements.

## Slide 3
Sample ID

## Slide 4
Item #: 010
Lot #: 0024682.0J3
Wafer #: 25
Part type: S26A
Location: Center; X-Dir

## Slide 5
TEM Image

## Slide 6
TEM Image

## Slide 7
TEM Image

## Slide 8
TEM Image

## Slide 9
STEM Image

## Slide 10
STEM Image

## Slide 11
STEM Image

## Slide 12
STEM Image

## Slide 13
STEM Image

## Slide 14
STEM Image

## Slide 15
EDS Element Mapping
In map
Sb map
Te map
Se map
As map
Ge map

## Slide 16
EDS Element Mapping
C map
O map
Si map
N map
W map
Ar map

## Slide 17
EDS Element Line Scan

## Slide 18
EDS Element Line Scan

## Slide 19
EDS Element Line Scan

## Slide 20
EDS Element Line Scan

## Slide 21
EDS Element Line Scan

## Slide 22
EDS Element Line Scan

## Slide 23
EDS Element Line Scan

## Slide 24
EDS Element Line Scan

## Slide 25
Item #: 020
Lot #: 0024682.0J3
Wafer #: 25
Part type: S26A
Location: Edge; X-Dir

## Slide 26
TEM Image

## Slide 27
TEM Image

## Slide 28
TEM Image

## Slide 29
TEM Image

## Slide 30
STEM Image

## Slide 31
STEM Image

## Slide 32
STEM Image

## Slide 33
STEM Image

## Slide 34
STEM Image

## Slide 35
STEM Image

## Slide 36
EDS Element Mapping
In map
Sb map
Te map
Se map
As map
Ge map

## Slide 37
EDS Element Mapping
C map
O map
Si map
N map
W map
Ar map

## Slide 38
EDS Element Line Scan

## Slide 39
EDS Element Line Scan

## Slide 40
EDS Element Line Scan

## Slide 41
EDS Element Line Scan

## Slide 42
EDS Element Line Scan

## Slide 43
EDS Element Line Scan

## Slide 44
EDS Element Line Scan

## Slide 45
EDS Element Line Scan

## Slide 46
Item #: 030
Lot #: 0024682.0J3
Wafer #: 23
Part type: S26A
Location: Center; X-Dir

## Slide 47
TEM Image

## Slide 48
TEM Image

## Slide 49
TEM Image

## Slide 50
TEM Image

## Slide 51
STEM Image

## Slide 52
STEM Image

## Slide 53
STEM Image

## Slide 54
STEM Image

## Slide 55
STEM Image

## Slide 56
STEM Image

## Slide 57
EDS Element Mapping
In map
Sb map
Te map
Se map
As map
Ge map

## Slide 58
EDS Element Mapping
C map
O map
Si map
N map
W map
Ar map

## Slide 59
EDS Element Line Scan

## Slide 60
EDS Element Line Scan

## Slide 61
EDS Element Line Scan

## Slide 62
EDS Element Line Scan

## Slide 63
EDS Element Line Scan

## Slide 64
EDS Element Line Scan

## Slide 65
EDS Element Line Scan

## Slide 66
EDS Element Line Scan

## Slide 67
Item #: 040
Lot #: 0024682.0J3
Wafer #: 23
Part type: S26A
Location: Edge; X-Dir

## Slide 68
TEM Image

## Slide 69
TEM Image

## Slide 70
TEM Image

## Slide 71
TEM Image

## Slide 72
STEM Image

## Slide 73
STEM Image

## Slide 74
STEM Image

## Slide 75
STEM Image

## Slide 76
STEM Image

## Slide 77
STEM Image

## Slide 78
EDS Element Mapping
In map
Sb map
Te map
Se map
As map
Ge map

## Slide 79
EDS Element Mapping
C map
O map
Si map
N map
W map
Ar map

## Slide 80
EDS Element Line Scan

## Slide 81
EDS Element Line Scan

## Slide 82
EDS Element Line Scan

## Slide 83
EDS Element Line Scan

## Slide 84
EDS Element Line Scan

## Slide 85
EDS Element Line Scan

## Slide 86
EDS Element Line Scan

## Slide 87
EDS Element Line Scan

## Slide 88
Job ID | Sample ID | Lot ID | Wafer ID | Die XY | Cut Dir | Bit | PM Ge | PM As | PM Se | PM In | PM Sb | PM Te | SD Ge | SD As | SD Se | SD In | SD Sb | SD Te
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 1 |  |  |  |  |  |  | 14.29 | 27.10 | 53.06 | 5.55 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 2 |  |  |  |  |  |  | 13.84 | 27.58 | 53.48 | 5.10 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 3 |  |  |  |  |  |  | 13.82 | 27.35 | 53.44 | 5.39 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 4 |  |  |  |  |  |  | 14.45 | 27.38 | 54.02 | 4.15 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 5 |  |  |  |  |  |  | 13.78 | 28.24 | 52.83 | 5.15 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 6 |  |  |  |  |  |  | 14.05 | 26.92 | 54.03 | 5.00 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 7 |  |  |  |  |  |  | 14.76 | 26.83 | 53.99 | 4.42 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 8 |  |  |  |  |  |  | 14.05 | 27.67 | 53.70 | 4.58 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 9 |  |  |  |  |  |  | 14.29 | 27.04 | 54.02 | 4.65 |  | 
TL170718004 | 010 | 0024682.0J3 | 25 | Center | X | 10 |  |  |  |  |  |  | 14.17 | 27.68 | 53.16 | 4.99 |  | 
EDS Element Composition Estimate: at.%

## Slide 89
Job ID | Sample ID | Lot ID | Wafer ID | Die XY | Cut Dir | Bit | PM Ge | PM As | PM Se | PM In | PM Sb | PM Te | SD Ge | SD As | SD Se | SD In | SD Sb | SD Te
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 1 |  |  |  |  |  |  | 14.15 | 26.98 | 54.36 | 4.51 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 2 |  |  |  |  |  |  | 13.99 | 26.70 | 54.75 | 4.56 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 3 |  |  |  |  |  |  | 14.01 | 26.52 | 54.58 | 4.89 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 4 |  |  |  |  |  |  | 13.99 | 27.59 | 54.42 | 4.00 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 5 |  |  |  |  |  |  | 14.04 | 26.94 | 54.84 | 4.18 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 6 |  |  |  |  |  |  | 14.33 | 27.30 | 54.07 | 4.30 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 7 |  |  |  |  |  |  | 13.68 | 27.09 | 54.58 | 4.65 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 8 |  |  |  |  |  |  | 14.20 | 26.48 | 54.72 | 4.60 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 9 |  |  |  |  |  |  | 14.05 | 26.83 | 54.27 | 4.85 |  | 
TL170718004 | 020 | 0024682.0J3 | 25 | Edge | X | 10 |  |  |  |  |  |  | 14.53 | 26.26 | 54.63 | 4.58 |  | 
EDS Element Composition Estimate: at.%

## Slide 90
Job ID | Sample ID | Lot ID | Wafer ID | Die XY | Cut Dir | Bit | PM Ge | PM As | PM Se | PM In | PM Sb | PM Te | SD Ge | SD As | SD Se | SD In | SD Sb | SD Te
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 1 |  |  |  |  |  |  | 13.32 | 26.39 | 52.08 | 8.21 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 2 |  |  |  |  |  |  | 14.29 | 26.59 | 51.86 | 7.26 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 3 |  |  |  |  |  |  | 13.53 | 26.98 | 52.38 | 7.11 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 4 |  |  |  |  |  |  | 13.77 | 26.28 | 51.87 | 8.08 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 5 |  |  |  |  |  |  | 13.31 | 26.14 | 53.05 | 7.50 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 6 |  |  |  |  |  |  | 13.50 | 26.83 | 51.98 | 7.69 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 7 |  |  |  |  |  |  | 13.21 | 27.19 | 51.99 | 7.61 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 8 |  |  |  |  |  |  | 13.47 | 26.35 | 51.99 | 8.19 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 9 |  |  |  |  |  |  | 13.68 | 26.35 | 52.18 | 7.79 |  | 
TL170718004 | 030 | 0024682.0J3 | 23 | Center | X | 10 |  |  |  |  |  |  | 13.51 | 26.68 | 52.18 | 7.63 |  | 
EDS Element Composition Estimate: at.%

## Slide 91
Job ID | Sample ID | Lot ID | Wafer ID | Die XY | Cut Dir | Bit | PM Ge | PM As | PM Se | PM In | PM Sb | PM Te | SD Ge | SD As | SD Se | SD In | SD Sb | SD Te
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 1 |  |  |  |  |  |  | 13.97 | 25.37 | 52.70 | 7.96 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 2 |  |  |  |  |  |  | 13.88 | 25.68 | 53.00 | 7.44 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 3 |  |  |  |  |  |  | 13.93 | 26.13 | 52.26 | 7.68 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 4 |  |  |  |  |  |  | 13.58 | 26.06 | 52.79 | 7.57 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 5 |  |  |  |  |  |  | 13.91 | 25.63 | 52.48 | 7.98 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 6 |  |  |  |  |  |  | 13.56 | 26.55 | 52.35 | 7.54 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 7 |  |  |  |  |  |  | 13.77 | 26.48 | 51.52 | 8.23 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 8 |  |  |  |  |  |  | 13.91 | 26.02 | 52.60 | 7.47 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 9 |  |  |  |  |  |  | 13.86 | 26.17 | 52.29 | 7.68 |  | 
TL170718004 | 040 | 0024682.0J3 | 23 | Edge | X | 10 |  |  |  |  |  |  | 13.56 | 26.41 | 51.92 | 8.11 |  | 
EDS Element Composition Estimate: at.%