## Slide 1: TL170718005
SD only SSM flow on S26A WL etch development with In doped SD stack; PROD SWR # 8527404 group 5E,6E:
Prepared by : (Tim Conroy)

## Slide 2: Job Description
wf#24 SWR # 8527404 group 5E: SSM SDv12 22nm 4% In; 21s SD etch no SO2; 2-step etch CD-; 20/20s W etch
wf#19 SWR # 8527404 group 6E: SSM SDv12 22nm 4% In; 21s SD etch no SO2; 2-step etch CD--; 20/18s W etch
Need EDS composition estimates, maps, and line scan across TE,BE and SD. Including Si/O/N/Al maps in addition to chalc. composition elements.

## Slide 3: 010 0024682.0J3-24 Center X-Direction

## Slide 11
80kV EDS Mapping

## Slide 12
80kV EDS Mapping

## Slide 13
EDS Line Scan

## Slide 14
EDS Line Scan

## Slide 15
EDS Line Scan

## Slide 16
EDS Line Scan

## Slide 17
EDS Line Scan

## Slide 18
EDS Line Scan

## Slide 19
EDS Line Scan

## Slide 20
EDS Line Scan

## Slide 21
80kV EDS Mapping

## Slide 22
80kV EDS Mapping

## Slide 23
EDS Line Scan

## Slide 24
EDS Line Scan

## Slide 25
EDS Line Scan

## Slide 26
EDS Line Scan

## Slide 27
EDS Line Scan

## Slide 28
EDS Line Scan

## Slide 29
EDS Line Scan

## Slide 30
EDS Line Scan

## Slide 31
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 1 | 14.67 | 27.3 | 50.01 | 8.02 | --- | ---
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 2 | 14.17 | 27.08 | 49.99 | 8.77 | --- | ---
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 3 | 13.86 | 27.31 | 50.3 | 8.17 | 0.24 | 0.12
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 4 | 14.33 | 27.91 | 48.79 | 8.97 | --- | ---
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 5 | 15.2 | 26.1 | 50.06 | 8.58 | --- | 0.07

## Slide 32
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 6 | 14.09 | 26.8 | 50.94 | 8.04 | 0.06 | 0.07
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 7 | 14.11 | 26.38 | 50.72 | 8.58 | 0.14 | 0.07
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 8 | 13.71 | 27.32 | 51.08 | 7.89 | --- | ---
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 9 | 13.7 | 28.4 | 49.87 | 7.96 | --- | 0.08
010 | 0024682.0J3 | 24 | S26A | Center | X-Dir | bit 10 | 14.18 | 26.65 | 51.16 | 8.01 | --- | ---

## Slide 33: 020 0024682.0J3-24 Edge X-Direction

## Slide 41
80kV EDS Mapping

## Slide 42
80kV EDS Mapping

## Slide 43
EDS Line Scan

## Slide 44
EDS Line Scan

## Slide 45
EDS Line Scan

## Slide 46
EDS Line Scan

## Slide 47
EDS Line Scan

## Slide 48
EDS Line Scan

## Slide 49
EDS Line Scan

## Slide 50
EDS Line Scan

## Slide 51
80kV EDS Mapping

## Slide 52
80kV EDS Mapping

## Slide 53
EDS Line Scan

## Slide 54
EDS Line Scan

## Slide 55
EDS Line Scan

## Slide 56
EDS Line Scan

## Slide 57
EDS Line Scan

## Slide 58
EDS Line Scan

## Slide 59
EDS Line Scan

## Slide 60
EDS Line Scan

## Slide 61
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 1 | 14.2 | 27.13 | 49.9 | 8.74 | --- | 0.03
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 2 | 13.56 | 27.56 | 50.64 | 8.25 | --- | ---
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 3 | 14.41 | 27.08 | 50.24 | 8.11 | 0.08 | 0.08
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 4 | 13.84 | 26.5 | 51.38 | 8.28 | --- | ---
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 5 | 13.58 | 27.56 | 50.86 | 7.86 | 0.11 | 0.04

## Slide 62
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 6 | 14.59 | 26.4 | 49.38 | 9.23 | 0.39 | ---
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 7 | 14.74 | 26.98 | 49.33 | 8.8 | 0.05 | 0.09
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 8 | 15.49 | 25.99 | 49.55 | 8.97 | --- | ---
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 9 | 14.36 | 26.12 | 50.42 | 9.04 | 0.06 | ---
020 | 0024682.0J3 | 24 | S26A | Edge | X-Dir | bit 10 | 13.83 | 27.9 | 48.95 | 9.32 | --- | ---

## Slide 63: 030 0024682.0J3-19 Center X-Direction

## Slide 71
80kV EDS Mapping

## Slide 72
80kV EDS Mapping

## Slide 73
EDS Line Scan

## Slide 74
EDS Line Scan

## Slide 75
EDS Line Scan

## Slide 76
EDS Line Scan

## Slide 77
EDS Line Scan

## Slide 78
EDS Line Scan

## Slide 79
EDS Line Scan

## Slide 80
EDS Line Scan

## Slide 81
80kV EDS Mapping

## Slide 82
80kV EDS Mapping

## Slide 83
EDS Line Scan

## Slide 84
EDS Line Scan

## Slide 85
EDS Line Scan

## Slide 86
EDS Line Scan

## Slide 87
EDS Line Scan

## Slide 88
EDS Line Scan

## Slide 89
EDS Line Scan

## Slide 90
EDS Line Scan

## Slide 91
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 1 | 13.03 | 27.53 | 50.57 | 8.88 | --- | ---
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 2 | 14 | 26.25 | 51.57 | 8.18 | --- | ---
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 3 | 13.76 | 27 | 51.35 | 7.88 | --- | ---
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 4 | 14.37 | 25.98 | 51.07 | 8.23 | 0.21 | 0.12
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 5 | 13.47 | 26.89 | 51.33 | 8.29 | 0.02 | ---

## Slide 92
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 6 | 13.79 | 26.22 | 51.64 | 8.24 | 0.08 | 0.03
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 7 | 13.99 | 25.99 | 50.53 | 9.42 | 0.01 | 0.06
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 8 | 13.88 | 26.05 | 51.52 | 8.55 | --- | ---
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 9 | 14.15 | 27.27 | 49.99 | 8.59 | --- | ---
030 | 0024682.0J3 | 19 | S26A | Center | X-Dir | bit 10 | 13.91 | 25.88 | 51.71 | 8.51 | --- | ---

## Slide 93: 040 0024682.0J3-19 Edge X-Direction

## Slide 101
80kV EDS Mapping

## Slide 102
80kV EDS Mapping

## Slide 103
EDS Line Scan

## Slide 104
EDS Line Scan

## Slide 105
EDS Line Scan

## Slide 106
EDS Line Scan

## Slide 107
EDS Line Scan

## Slide 108
EDS Line Scan

## Slide 109
EDS Line Scan

## Slide 110
EDS Line Scan

## Slide 111
80kV EDS Mapping

## Slide 112
80kV EDS Mapping

## Slide 113
EDS Line Scan

## Slide 114
EDS Line Scan

## Slide 115
EDS Line Scan

## Slide 116
EDS Line Scan

## Slide 117
EDS Line Scan

## Slide 118
EDS Line Scan

## Slide 119
EDS Line Scan

## Slide 120
EDS Line Scan

## Slide 121
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 1 | 14.95 | 27.14 | 50.4 | 7.35 | 0.16 | ---
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 2 | 13.01 | 27.85 | 51.06 | 7.81 | 0.23 | 0.04
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 3 | 14.43 | 26.44 | 51.32 | 7.72 | --- | 0.09
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 4 | 13.89 | 27.88 | 51.19 | 7.05 | --- | ---
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 5 | 14.8 | 25.22 | 52.07 | 7.91 | --- | ---

## Slide 122
EDS Atomic Percent Estimate
Sample | lot | wafer | design | location | direction | Deck Bit | SD Ge-K | SD As-K | SD Se-K | SD In-L | SD Sb-L | SD Te-L
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 6 | 15.08 | 26.96 | 50.15 | 7.81 | --- | ---
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 7 | 13.96 | 26.25 | 51.09 | 8.43 | 0.26 | ---
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 8 | 13 | 28.1 | 51.12 | 7.77 | --- | ---
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 9 | 13.97 | 26.39 | 50.99 | 8.31 | 0.13 | 0.2
040 | 0024682.0J3 | 19 | S26A | Edge | X-Dir | bit 10 | 14.29 | 26.9 | 50.12 | 8.46 | --- | 0.23