## Slide 1: ISO JDP on Chal electrodes
Q3, 2015 experiment results from D2 and RH

## Slide 2: OTS Plug process flow
D2 deposited 1040 Prime,
OTS SL9
SLD TiSiN plug OTS flow
CMP’d TiSiN Bot electrode
500A OTS
750A TiAlN
~ 110 nm
Lot OTS_SL9, Wafer 302
Die B, X2y3, CPAD Area

## Slide 3: Cycling Evolution
D2 deposited 1040 Prime,
OTS SL9
SLD TiSiN plug OTS flow
CMP’d TiSiN Bot electrode
500A OTS
750A TiAlN
IV 1 1st_RI b31
IV 2 2nd_RI b31
IV 3 RI1Cyc_1E+0 b31
IV 4 RI1Cyc_1E+1 b31
IV 5 RI1Cyc_1E+2 b31
IV 6 RI1Cyc_1E+3 b31
IV 7 RI1Cyc_1E+4 b31
IV 8 RI1Cyc_1E+5 b31
IV 9 RI1Cyc_1E+6 b31
IV 10 RIFCyc_1E+6 b31

## Slide 4: Fountain of Youth?
1st 10 IV scans at 25C. Notice Vff of ~4.1V.
Following 175C anneal for ~1hr, Vth returns to near-Vff value(?) What would happen with higher temperatures and/or longer times?

## Slide 5: Plug vs. Elevated Pore (EP), DOT
5
Plug
EP
DOT

## Slide 6
D2 deposited 1040 Prime OTS
wfr 55BR:
TP2 elevated pore
TiAlN Bottom electrode: 60A Spt etch
500A OTS
750A TiAlN / 1000A Ti
EP OTS process flow
D2 deposited 1040 Prime OTS
wfr 235 (SL4):
DOT planar OTS flow
TiAlN Bottom electrode: 250A TiAlN
500A OTS
750A TiAlN
Plug TiSiN: Vt ~ 5 (at 100 cycles) Voffset ~ 1.9 >95% yield
EP TiAlN: Vt ~ 4.1v Voffset ~ 0.9-1.2 >95% yield
DOT TiAlN: Vt ~ 1.3-2.1 Voffset ~0.5 5-40% yield
DOT OTS process flow
OTS Plug process flow
D2 deposited 1040 Prime OTS
SL9
SLD TiSiN plug OTS flow
CMP’d TiSiN Bot electrode
500A OTS
750A TiAlN

## Slide 7: Plug Process: BE – TiSiN
Vth migrates down with cycling. Relatively stable from 2nd to 1E3 cycles.
Both 300ns and 1us pulse width shows similar Vth migration down with cycling.

## Slide 8: SubVth Cycling Evolution
The subthreshold characteristics shown in the plot below are not normalized to the pulsed VT data.
The absolute leakage is observed to increase during cycling.
1st Cycle
1x105 Cycles
100 Cycles

## Slide 9: SAG Lot S095147KTT

## Slide 10
TP2
LE = TiAlN
TE = 500A TiAlN

TP2
LE = TiAlN
OTS = 250A SAG
TE = 400A Carbon
(Control)

TP2
LE = TiAlN
TE = Ti / TiAlN 70 / 500A

TP2
LE = TiAlN
TE = Ti / TiAlN 20 / 500A

Lot S095147KTT Electrical Test Results
Initial I-V

## Slide 11
TP2
LE = TiAlN
TE = 500A TiAlN

Rload = 2.5kΩ
TP2
LE = TiAlN
OTS = 250A SAG
TE = 400A Carbon
(Control)

TP2
LE = TiAlN
TE = Ti / TiAlN 70 / 500A

TP2
LE = TiAlN
TE = Ti / TiAlN 20 / 500A


## Slide 12: Scratch Pad

## Slide 13
10
IV 1 1st_RI b31
IV 2 2nd_RI b31
IV 3 RI1Cyc_1E+0 b31
IV 4 RI1Cyc_1E+1 b31
IV 5 RI1Cyc_1E+2 b31
IV 6 RI1Cyc_1E+3 b31
IV 7 RI1Cyc_1E+4 b31
IV 8 RI1Cyc_1E+5 b31
IV 9 RI1Cyc_1E+6 b31
IV 10 RIFCyc_1E+6 b31
IV 1 1st_RI b31
IV 2 2nd_RI b31
IV 3 RI1Cyc_1E+0 b31
IV 4 RI1Cyc_1E+1 b31
IV 5 RI1Cyc_1E+2 b31
IV 6 RI1Cyc_1E+3 b31
IV 7 RI1Cyc_1E+4 b31
IV 8 RI1Cyc_1E+5 b31
IV 9 RI1Cyc_1E+6 b31
IV 10 RIFCyc_1E+6 b31
IV 1 1st_RI
IV 2 2nd_RI
IV 3 RI1Cyc_1E+0
IV 4 RI1Cyc_1E+1
IV 5 RI1Cyc_1E+2
IV 6 RI1Cyc_1E+3
IV 7 RI1Cyc_1E+4
IV 8 RI1Cyc_1E+5
IV 9 RI1Cyc_1E+6
IV 10 RIFCyc_1E+6