## Slide 1: BiSM re-start for low risk a-product definition
Team BiSM
a-product definition
Critical paths to restart BiSM at F11x
BiSM vs. Full Stack (Baseline – P1240.1/ALF32)
  Technology, RWB, Reliability, Algorithm, Array Architecture, die size, performance, energy
Perspective – Higher density, higher speed, lower BER
WIP

## Slide 2: a-product definition
Definition placeholder & Process/Design dependency
  Low Risk BiSM Demo: Product level validation by matching HVM full stack (S26)
  Technology Demo: Product level demonstration of BiSM stack with main TD collateral (ATF32) (See backup Material on S26 and ATF32 definition)
  G+1 scaling: P1242 candidate; pitch scaling, new collateral may be required
Definitions | Goal (ref. to ATF32) |  |  | Process and Design Dependency |  |  | 
 | BiSM Demo | Tech Demo | G+1 Scaling | Design Collateral & CMOS | Pitch Decision & Integration | DTS/MTS | Algorithm
Wafer Cost | 90% | 90% | 90% | X | X | X | 
Capacity | match | match | match | X | X |  | 
Die size | 1.4X | match | 85% | X | X |  | 
Tile Capacity | match | match | match | X | X | X | 
Read BW | 1.5X | 1X | 1.5X | X |  | X | X
Read Energy | 1.2X | match | match | X | X | X | X
Write BW | 1.5X | 1.5X | 1.5X | X |  | X | X
Write Energy | 1.2X | Match | Match | X | X | X | X
Power | 1.8X | 1.5X | 1.5X | X | X | X | X

## Slide 3: Logistics for BiSM Si based learning
 | TC03/04 | S26/SR71 | ALF32/Bantu | ATF16X/SR71 | S24SX | ATF32 (double scribe)
Design Collateral & CMOS | X |  | X |  |  | 
Pitch Decision & Integration |  |  |  | X | X | X
DTS/MTS |  |  |  | X | X | X
Algorithm |  | some | X | some | X | X
Vehicle | Coverage
TC03 | Only needed if CMOS and collateral require significant change to P1241.0
S26 | No need. Training for new array/cell engineer.
ALF32 | Only useful with Bantu. Good for algorithm exploration and development @ 41P
ATF16X | SR71 for scaling learning, smaller density, low thru put testing (5 array / wafer), low visibility to RWB and reliability tail, some but limited learning on algo development
S24SX 3T Decoder | New design required. 3T decode design with live die; enables algo development (for latency, energy assessment) and float deselect development (~3% die size opportunity.)
ATF32 3T Bantu | New Bantu with 3T decode design for cell/array/algo development; enable algo, float deselect, single cell chax, smaller density (low visibility to RWB and reliability, tail)
True DTS/MTS learning pending on PVD, 1st cut last partial and 2nd cut tool isolation.

## Slide 4: Value Proposition
BiSM vs. Full Stack 3DXP

## Slide 5: BiSM vs. Full Stack and Scalability
Process: Integration and Module
SLC: RWB, Set, Reset
Algorithm: Set, Reset, Read
Reliability: endurance, disturb, retention
Array: density and energy and performance
Si Policy: Compatible with full stack; no additional scaling challenge is expected

## Slide 6: BiSM Silicon Empiricals
Last silicon Rev 6.6, In doped SAG and DOE, in June/2018.
Yield learning curves with 100s of wafers (one lot every 2 weeks)
Rev 6.6 SD.k2 BKM process demonstrated PG1 structure yield (S26 live die): >75% 1D & >40% 2D (on par with full stack at the same time frame)
1st & 2nd cut profile meets MTS; SWA @ 87.5° & 88.5° correspondingly.
Parametric and reliability sampling – 8 lots, 40 wafers, 5 die per wafer.
PG4 capable RWB (SR71 based, limited by array size 3.3s)
PG1 capable of endurance; good/upper quartile die passing 2M cycles FW
No ULR performed

## Slide 7: Process Technology
Metric | Full Stack |  |  |  |  |  |  |  |  | BiSM |  |  |  |  | Scaling Challenge
Periphery | LVT, HVT + 5~6 interconnect |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Cell Stack | BE | SD | ME1 | ME2 |  | PM |  | TE |  |  | BE | SD | TE |  | 
Array Metals | W, 30nm First Cut, 30/40 nm 2nd Cut |  |  |  |  |  |  |  |  | ½ or more metal thickness reduction possible (>50% Ipgm/Ilkg reduction) |  |  |  |  | 
Patterning | Partial etch and Liner are required |  |  |  |  |  |  |  |  | Single etch, no liner required; lower AR, lower scope for hard-mask |  |  |  |  | 
Seal | Nitride seal required |  |  |  |  |  |  |  |  | Required, lower AR, more options |  |  |  |  | 
Gap fill | No air gap, 1st/2nd Rq tuning for TD |  |  |  |  |  |  |  |  | No air gap, no visible TD issue |  |  |  |  | 
CMP | Similar challenges as nodes scale, socket size scaling limitations may impact |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Ambient | Required |  |  |  |  |  |  |  |  |  |  |  |  |  | 
On Pitch Via | Scaling challenges expected at 28 pitch and below for via resistance |  |  |  |  |  |  |  |  |  |  |  |  |  | 

## Slide 8: SLC RWB @ 41nm Pitch
Full Stack op. (unipolar)
Metric | Unit | Full Stack^ | BiSM^
DVT @ 1ms ( = RST-SET ) | mV | 1140 | 1380
E2 Consumers |  |  | 
sVt | mV | 95 | 100
Drift: 1ms-10s (3s-48h) | mV | 260 (320) | 330 (220)
GB (WE,RD,BD) | mV | - | -
E3 Consumers |  |  | 
sVt | mV | 100 | 105
Drift: 1ms-10s (3s-48h) | mV | 630 (>1100) | 590 (1050)
GB (WE,RD,BD) | mV | 100 | 100
Array Op. |  |  | 
x-tile | mV | 30 | 30
Leakage: SET (RST) | mV | 5nA (2nA) | 5nA (0.2nA)
E1 | mV | 4030 | 4040
E4 | mV | 7600 | 7500
^ 10s Qual SORT for full-stack, while non-opt. TBD for BiSM
BiSM op. (bipolar)
E2
10s
E3
10k FW
RBER goal
RWB
Vinh
1ms
time
time
Pulse Amplitude
RST
SET
RST
SET

## Slide 9: Set State
Metric | 41nm Pitch Full Stack | 41nm Pitch BiSM | Scaling Challenge
VT | Tunable by SD MTS (thickness, alloy, transfer function) |  | 
MLC feasibility | Lower tuneability by waveform | More flexibility (without PM) | 
sVt | SD MTS + cross contaminations | SD MTS | 
Drift | SD structure relaxation |  | 
EvolutionVt | SD + PM WE, higher VT turn-around | SD WE at lower power | 
Leakage | SD MTS + cross contaminations | SD MTS | 
E1 | SD WE + cross contamination | SD WE | 
E2 | SD WE + PM set-ability + RD | SD WE | 

## Slide 10: Reset State
Metric | Full Stack | BiSM | Scaling Challenge
VT | Tunable by PM material & thickness | Tunable by SD material | 
MLC feasibility | Tunable by waveform | Tunable by waveform | 
sVt | (SD + PM) MTS + cross contamination | SD MTS | 
Drift | SD + PM structure relaxation | SD structure relaxation | 
EvolutionVt | SD + PM WE | SD WE at lower power | 
Leakage | SD intrinsic (low a-PM contribution) | SD intrinsic subVt shift right | 
E3 | SD + PM WE + TD | SD WE + RD | 
E4 | SD + PM WE + PM drift + Leakage | SD WE | 

## Slide 11: Set Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Crystallization: Nucleation/Growth | Mass transport @ TG (Segregation) | 
IProgram | 25uA + 60uA (ambipolar) | 50uA (polarity dependent) | 
tpulse | 130ns+70ns | 50ns | 
VSelection | E4 | E4 | 
Spike Miti. | Needed for PM endurance | No | 

## Slide 12: Reset Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Vitrification (Glass) | Mass Transport @ TG (Segregation) | 
IProgram | 110uA (ambipolar) | 50uA (polarity dependent) | 
tpulse | 5ns | 50ns | 
VSelection | E2 | ”E4” | 
Spike Miti. | Needed for PM endurance | No | 

## Slide 13: Read Operation
Metric | Full Stack | BiSM | Scaling Challenge
Mechanism | Demarcation Read/Set Back/Termination | Demarcation Read(/termination?) | 
Iread | 25uA/60uA/25uA | 25uA or higher (/25uA) | 
tpulse | 35ns/35ns/30ns | 35ns(/35ns) | 
VSelection | E2 | E2 | 
Spike Miti. | Needed to PM RD | No | 

## Slide 14: Reliability
Metric | Full Stack | BiSM | Scaling Challenge
WE (Write End.) | Limiter: E2 (PM turn-around) Tuning: (SD + PM) MTS, waveform | Limiter: Extrinsic E1/E4 Tuning: SD MTS (SD ‘health’) | 
Array init. (Seasoning) | SD stabilization (low PM contribution) Tuning: SD MTS (SD ‘health’) | SD stabilization Tuning: SD MTS (SD ‘health’) | 
WD (Write dist.) | PM proximity disturb + (SD+PM) BD Tuning: Stack MTS, waveform | SD BD (‘reverse’ dominating) Tuning: SD MTS | 
RE (Read End.) | SD WE + (PM+SD) disturb Tuning: (PM + SD) MTS, waveform | SD WE Tuning: SD MTS | 
RD (Read Dist.) | PM disturb (low SD contribution) Tuning: PM MTS, and waveform | SD WE + SD BD (‘reverse’) Tuning: SD MTS and waveform | 
Retention | SD + PM structure relaxation Tuning: (SD+PM) MTS, and waveform | SD structure relaxation Tuning: (SD) MTS, and waveform | 

## Slide 15: 3T Bipolar Decoder
-3.7
0
-3.7
0
0
0
-3.7
3.7
1.2
0
-3.7
3.7
0
0
-3.7
3.7
-3.7
3.7
1.2
1.2
IDLE
0
3.7
3.7
0
0
0
-3.7
3.7
1.2
0
POS
NEG
3T Solves the energy problem present in 2T POR
  No Deselect Toggle
  At Cost of adding on transistor. (Small N Xtr.)
Decoder footprint is expected on par with 2T POR
  [Med P + Med N + Small N] vs. [Big N (or P) + small P (or N)]
  Need decoder layout to drive assessment.
 | ALF32 | S24S | 3T
Status | POR | POR | Pre POR
Cell Arch | Unipolar | Bipolar | Bipolar
Decode Type | 2T | 2T | 3T
Deselect Togl. | No | Yes | No
Float Deselects | No | No | No
Energy | 104 | 154 | ~104
Die size | 198 | 221 | 227
 | 3T |  |  |  | 
 | POS |  | NEG |  | IDLE
 | SEL | DESEL | SEL | DESEL | 
gp | 3.7 | 3.7 | 0 | 0 | 0
lselp | 0 | 3.7 | 0 | 3.7 | 3.7
lbwl | 3.7 | 0 | -3.7 | 0 | 0
lseln | 0 | -3.7 | 0 | -3.7 | -3.7
gn | 0 | 0 | -3.7 | -3.7 | 0
lselg | 0 | 1.2 | -3.7 | 1.2 | 1.2
vss | 0 | 0 | 0 | 0 | 0
#/patch | 32 | 992 | 32 | 992 | 1024

## Slide 16: Read
3DXP Full Stack
BiSM Read
Read Pulse incl. Ramp
(37.5ns)
Sense Amp Latch
(12.5ns)
BL 1st Termination (20ns)
Start
Read Pulse incl. Ramp
(37.5ns)
Sense Amp &
Latch
(12.5ns)
SET Pulse 3 (25ns)
BL 1st Termination (20ns)
Set? (5ns)
Yes
No
Start

## Slide 17: Set a reset cell
3DXP Full Stack
BiSM
WL/BL Ramp
(211ns)
Incl.
Spike Miti (71ns)
Snap Detect (45ns)
C-cell (95ns)
Ilow (P1)
(30ns)
Ihigh (P3)
(103ns)
P4
(30ns)
Start
BL1st
(20ns)
WL/BL Ramp
(140ns)
Incl.
Snap Detect (45ns)
C-cell (95ns)
Ihigh (P3)
(50ns)
Start
BL1st
(20ns)

## Slide 18: Reset a set cell
3DXP full Stack
BiSM
WL/BL Ramp
(37.5ns)
Sense
(12.5ns)
Reset Pulse (15ns)
Set? (5ns)
Yes
No
Start
WL/BL Ramp
(140ns)
Incl.
Snap Detect (45ns)
C-cell (95ns)
Ihigh (P3)
(50ns)
Start
BL1st
(20ns)

## Slide 19: Memory Hierarchy expansion
Perspective in Memory Displacement Strategy of Von Neumann Architecture

## Slide 20: Multi Level Cell capable for high density/high speed Storage
+VDM2
1
0
Y
SLC
Write PA
Read VTH
+VDM1
+VDM2
-VDM1’
+PA1
+PA2
-PA1’
-PA2’
Write PA
1
0
Write PW
+PA1
-PA1’
+VDM1
1
+VDM2
.5
0
Y
Y
1.5 b/c
Write PA
1
0
.5
Write PW
+PA1
-PA1’
+PA2
+VDM1
11
01
+VDM2
10
-VDM1’
00
Y
Y
Y
MLC
Write PA
11
01
10
00
Write PW
+PA1
-PA1’
+PA2
-PA2’

## Slide 21: Multi Level Cell (II)
+VDM2
1
0
Y
SLC
Write PW
Read VTH
+VDM1
+VDM2
-VDM1’
+PW1
+PW2
-PW1’
-PW2’
Write PA
1
0
Write PW
+PW1
-PW1’
+VDM1
1
+VDM2
.5
0
Y
Y
1.5 b/c
Write PA
1
0
.5
Write PW
+PW1
-PW1’
+PW2
+VDM1
11
01
+VDM2
10
-VDM1’
00
Y
Y
Y
MLC
Write PA
11
01
10
00
Write PW
+PW1
-PW1’
+PW2
-PW2’

## Slide 22: Multi Level Cell (III) – TLC or more
Write PA
Read VTH
+VDM1
+VDM2
-VDM1’
+PA1
+PA2
-PA1’
-PA2’
+PW1
+PW2
-PW2
+VDM3
+VDM4
-PW1
-VDM2’
-VDM3’
Write PA
111
110
Write PW
+PW1
+PW2
+PW2
101
100
+PW1
+PA1
+PA2
Write PA
011
010
Write PW
-PW1’
-PW2’
-PW2’
001
000
-PW1’
-PA1’
-PA2’

## Slide 23: High speed / lower RBER for Random Word Access Application DRAM RBER is < 1E-9 or 5.998s
Bianca Schroeder et.al, 'DRAM Errors in the Wild - A large scale field study’ https://doi.org/10.1145/1897816.1897844
  Studied in Google server farm for 2½ years
  25,000 to 70,000 FIT of 'ECC correctable error’ of 64-bit-word per Megabit
  one single-bit-error every 14 to 40 hours per Gigabit
Disclaimer: This statistical analysis of RBER can not be used universally for all applications
Extrapolation based on
Rev 6.6,
In doped SAG SD.k2
SR71 (3.3s)
Post 1µses
After seasoning
Sigma of bit
Distribution focus include
Noise (traps), snapback (charge multiplication process) stability as manifest in threshold bounce
Glass metastability related to drift and seasoning
Cycle endurance

## Slide 24: BackUp Materials

## Slide 25: Optane Media Roadmap (Pre-POR)
Key Spec | S26A | Atlantic Falls 32
Technology node | 2nd | 3rd
Density | 32GB | 32GB
Die Size | 199mm2 | 136mm2
Cost $/GB vs. S26A (TCS) | 1X | 0.75X
Alpha Fab Memory PRQ | EOY 2019 | Q1-Q2’ 2022
Read BW | 1600 MB/s | 3200 MB/s
Write BW | 800 MB/s | 1100-1600 MB/s
Read Energy | 49 pJ/b | 47 pJ/b*
Write Energy | 112 pJ/b | 95 pJ/b*
IO Interface | 1600 MT/s/pin DDR4 | Combo Phy (DDR4+ LPDDR4x w/o DFE)
Package | 256b | 392b 2-ch
Server Memory/Platform | CrowPass/SPR | DonahuePass/GNR
Server Memory PRQ | Q2’21 | Q2-Q3’22
Server Memory perf. GnG 2R:1W 256GB | 1X | 1.5X (w/ Media), 3X (w/ controller)
Datacenter Storage | Alderstream (G4) | Alderstream Refresh (G4)
Storage PRQ | Q4’20 | Q2’22
Storage Perf 70/30 BW 0.8TB | 1X | 1X