## Slide 3: VT response Vs. near threshold @ PFA
II
[Np]
I
[Pp]
A
B
C
A
B
C
STS ~ const
IT ↓
STS ~ const
IT ↑ (~1.3x ITA)
EA ~ const (or↑) w/ Iprog
EA ~ 0 (and ~ ↑ w/ Iprog)
TE BE
TE BE
TE BE
?
TE BE
?
WIP
Iprog
Iprog
Attributing the contained VT shift w/in quadrant to local barrier modulation. Switching ascribed to MT w/ polarity as main driver [WIP].

## Slide 4: Electrical Equivalent Circuit and Possible Underline Physics
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. The best known ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Near parallel shift on SubVt I-V on polarity effects
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
From empirical to physical
  Pursuing the validation of heterogeneous junction model
  Programmable battery is formed by the band offset
  Write –Band offset switching subject to mass transport.
  Read – Space Charge modulation results in voltage shift
SD Resistor
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Post
Neg
Write
0V
(−)
Read Polarity

## Slide 5: Basic Band Diagram of SAG and Model assumptions Electronic Structure of Amorphous Semiconductors, D. Adler and E. J. Yoffa, Phys. Rev. Lett. 36, 1197-1200 (1976)
Assumptions:
  EG:2eV
  Effective intrasite electronic correlation energy is negative therefore P-type is exhibited (pinned)
3 Electronic models on with SAG mass transport by polarity
  Ge/As moves toward cathode
  Homojunction – Correlation energy changed to positive therefore n-type (similar to tetrahedrally coordinated amorphous semiconductor)
  Heterojunction-I – Band offset due to coordination changes (Michaelson’s Electronegativity Scales & The work Function, IBM JRD 1978), higher Work Function
  Heterojunction-II – Band offset, but lower Work Function
  0.8eV Change is used to illustrate all 3 models
Vacuum
Ec
Ev
Ef
ϕe
Vacuum
(I)
(II)
(III)
∆Ef=+0.8eV
∆χ=−0.8eV
∆χ=+0.8eV
SAG/Se+
C
C
As+/Ge+

## Slide 6: 1D Space Charge and Built-in Field
Trap Density [cc-1]
ε[MV/cm]
εmax
Space Charge Width
Trap Density [cc-1]
εmax [MV/cm]
Space Charge Width [nm]
Vbi=1V
Vbi=.1V
ϵSD = 10
EBD : Si ~0.3MV/cm SiO2 10~15MV/cm, GST ~0.3MV/cm, TAG ~1MV/cm, SAG ~3MV/cm

## Slide 7: Physical model – working principles & assumptions
SSM device is a string of domains serially concatenated. Node is an abstract point junction between domains.
  Simplified with 1D model
Per Kirchhoff law
  The nodal current is zero
  Assumption – Qausi-static SubVt I-V represents device I-V at nano-second regime
  The “domain” voltage drop for a current level will determine the shape of the I-V curve;
  Shift right is higher threshold voltage and Voltage contribution of shifting is the memory effects
4 carrier transport mechanisms –
  Conduction in delocalized state such as Diffusion and Drift
  Conduction between localized and delocalized states such Poole-Frankel
  Direct tunneling such as band to band and defect to defect between metallurgical junctions
Drift is linear function of electrical field – contribution is very low due to low free carrier and low mean-free path
  Likewise, Diffusion contribution is also low (Einstein relation)
Electronic trap density is in the order of 1% of atomic density (inactive or pinned) ~1021/cc
  10% structural vacancies in typical crystalline GST225, If electronically active, Debye length is < lattice constant; CV measurement exhibits Debye length in the order of μm or longer
  Space charge region @ junction established by direct tunneling with build-in potential

## Slide 8: 1D Space Charge and Built-in Field in SAG
Trap Density [cc-1]
Space Charge Width
ε[MV/cm]
εBD
EBD : SAG ~3MV/cm
Vbi [volt]

## Slide 9: Model Comparison
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
Model (I) – Homojunction
Model (II) – Heterojunction, higher 𝛘
Model (III) – Heterojunction, lower 𝛘
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
0V
(−)
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 10: Model (I) – Homojunction
(–) Bias Read, same polarity of write
  Bias initially contributed to barrier reduction, very low current, shift I-V to right.
(+) Bias Read, opposite polarity of Write
  Space charge region maintained or no change. Potential drop evenly cross Chal glass.
Homogeneous junction model does not support the observed polarity effect
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 11: Model (II) – Heterojunction, higher 𝛘
(–) Bias Read, same polarity of write
  Space charge region maintained or little change. Potential drop evenly cross Chal glass.
(+) Bias Read, opposite polarity of Write
  Bias initially contributed in compensating built-in potential, shift I-V to right.
Higher 𝛘 heterogeneous junction model supports the observed polarity effect
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias
0V
(−)

## Slide 12: Model (III) – Heterojunction, lower 𝛘
(–) Bias Read, same polarity of write
  Bias initially contributed in compensating built-in potential, shift I-V to right.
(+) Bias Read, opposite polarity of Write
  Space charge region maintained or very low. Potential drop evenly cross Chal glass.
Lower 𝛘 heterogeneous junction model does not support the observed polarity effect
Vacuum
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Bias

## Slide 13: Electrical Equivalent Circuit and Possible Underline Physics
A VT window (∆VT) has been observed by applying programming pulses with opposite polarity. The best known ∆VT physics is an electrochemical potential modulation effect subject to mass transport by polarity.
  Near parallel shift on SubVt I-V on polarity effects
  The equivalent circuit – a programmable battery connected to a Chal Glass Resistor serially
From empirical to physical
  Pursuing the validation of heterogeneous junction model
  Programmable battery is formed by the band offset
  Write –Band offset switching subject to mass transport.
  Read – Space Charge modulation results in voltage shift
SD Resistor
SAG
C
C
As+/Ge+
0V
(−)
(+)
⊕
⊖
ϕ
⊕
⊖
ϕ
⊕
⊖
ϕ
Post
Neg
Write
0V
(−)
Read Polarity