## Slide 1: ADM Scaling Roadmap
2019
2020
2021
2022
2023
2024
2025
2026
2027
Production
Dev on Prod
Gen1 eDRAM (1st ADM)
Dev on Test Chip
Prod A-0 TI
Prod PRQ
Production
Dev on Prod
Gen2 eDRAM (Stacked ADM)
Dev on Test Chip
Prod A-0 TI
Prod PRQ
Production
Dev on Prod
Gen3 eDRAM (In Development)
Dev on Test Chip
Prod A-0 TI
Prod PRQ
Gen4 eDRAM (12-18m cadence)
Enabler for Scaling
Def. + SL TC
Stacking 2 ADM layers
Lateral Scaling
Lateral Scaling /
New ADM topology?
PDK0.1
PDK0.1
PDK0.1
Definition for each generation will be re-evaluated / closed for PDK0.1
FL option masks for X22S taped in
RECL test chip taped in
Production
Dev on Prod
Dev on Test Chip
Prod A-0 TI
Prod PRQ
Use Hacked X22G Process
PDK0.1
Decide on Topology
Note this is extended for new topology
Need to have Si validation of right topology for Gen4
Courtesy: PTD/Travis L.
Value in Memory PF team to evaluate & validate Gen4 topology
Decision on Gen4 topology in 2022 is KEY to deliver cadence

## Slide 2
Chart: 
| 2022.5 | 2024 | 2025.5 | 2027 | 2028.5
 | 0.005 | 0.01 | 0.014 | 0.03 | 0.05
Capacity (GB/mm 2)
ADM Gen 1
108x135 (1H)
ADM Gen 2
108X135nm (2H)
ADM Gen 3
120x90nm (2H)
Production Year
ADM
‘Simplest’ FinFET 107 X 75 nm (2H)
ADM Cell Scaling Options:
High Bandwidth/capacity 1TB/sec/GB; <20 ns
ADM Gen4
Topology?
ADM FinFET (2H)
Stars are projections, not official TD roadmap
ADM 6F2: 95 x 85nm (2H)
ADM FinFET (2H)

## Slide 3
Memory PF team to validate Gen4 topology : 6F2 BG or Top gate FinFET?
Gen
6F2 Backgate (95x85nm2)
Assumptions: (OGD = 110 nm)
Lcon=26.5 nm
Lg= 30 nm
Ls= 6 nm
Li = 15 nm
Wfin=10 nm
Simple FinFET Layout (107x75nm2)
Need to validate 6F2 (120x90nm) with shared contacts.
Use: Gen3 X22GR RECL w/ADG mask
FinFET- validate scalability of Lcon, Lg with BEOL stability; reliability.
Use: 1X35SA mask
No shared contacts, no angling required

## Slide 4
Backup slides

## Slide 5
6F2 cell @ 95 (PGD) X 85 (OGD) nm2: (assumptions)
Lg1=Lg2=30 nm (shrink Lg from 40 (Gen1,2) to 30 nm)
act=act2=d=26.5 nm
COB (80x70xZ nm3)-assume Double wall capacitor
Iso= 50 nm (EPE= 10-15 nm, COB overhang=25 nm, 10 nm space)
act patterned separately from act2 (extra mask)
190 nm/2 = 95 nm
Iso gap considerations: EPE, COB overhang, COB profile
PGD: (parallel gate direction)
Risk items:
Shared drain- Ioff leakage issues? Need to simulate
Rext due to underlap contact to back gate (region d)
Need to see if enough drive current if we scale down to Z= 70 nm (15 nm space, total 85 nm= OGD)
Need to calculate if COB dimensions are good for acceptable sense margin
Smaller Lg- is Ion/Ioff on target still?
VBG2
COB
COB
Lg1
Lg2
d
VBG2
COB
COB
Lg1
Lg2
d
Iso
act2
act2
6F2 Backgate Cell Topology
Assume 95x85nm2
d
d

## Slide 6
Notes:
6F2 is a back-gate topology with shared drain to enable further back-gate scaling but needs to be validated
Initial design parameters in table are based on integration but need device simulations to understand the performance tradeoffs
Sensitivity of design parameters Lg and Lcon tradeoff (impacts Ioff and Ion), and iso values impact density/yield, d-parameter is going to be set by litho (will need 2 litho passes)
6F2 is introducing at least 3 more masks (2x cut gate; and 1x act2)
Scaling 6F2 cell to 80x70 nm2 is high performance risk
Transistor ‘Design Rules’ (≤ 90x90 nm2 cell)
Parameters | 8F2 | 8F2 | 6F2 | 6F2
Cell Sizes (nm2) | 135X108 | 120x90 | 95x85 | 80X70
Lg (nm) | 40 | 35 | 30 | 22.5
Act (nm) | 27.5 | 25 | 26.5 | 22.5
Act2 (nm) | 0 | 0 | 26.5 | 22.5
Iso (nm) | 40 | 35 | 50 | 45
d (nm) | 0 | 0 | 26.5 | 22.5
Act (nm) | 27.5 | 25 | 26.5 | 22.5
PGD direction (nm) | 135 | 120 | 93 | 78.75
OGD (nm) | 108 | 90 | 85 | 70
Z (nm) | 73 | 73 | 70 | 55
COB (top dim)-nm | 89x65x500 | 75x65x500 | 80x70xZ | 65x58xZ
scaling factor | 1 | 1.35 | 1.805572755 | 2.603571429

## Slide 7
Backgate (no sharing) 8F2 at 95x85 nm2 is at risk for electrostatics and Ion not meeting target-would like to see calibrated simulations based on R96 (on TD’s line)
Sharing contacts at 95x85 nm2 (6F2) enables 50% longer Lg; 33% longer Lcon compared to 8F2 @ 95x85 nm2 but WL pitch is tighter!
Need to evaluate angling with shared contacts to see ROI of 6F2 cell. Currently 80x70 nm2 @6F2 manhattan is risky for not meeting total drive current
Parameters | 8F2 (Gen1) | 8F2 | 8F2 | 8F2 | 6F2 | 6F2
Cell Sizes | 135X108 | 120x90 | 95x85 | 95x85 | 95x85 | 80X70
Lg | 40 | 35 | 26 | 20 | 30 | 24
act | 27.5 | 25 | 22 | 20 | 26.5 | 22.5
act2 | 0 | 0 | 0 | 0 | 26.5 | 22.5
iso | 40 | 35 | 25 (EPE risk) | 35 (at EPE margin) | 50 | 45
d | 0 | 0 | 0 | 0 | 26.5 | 22.5
act | 27.5 | 25 | 22 | 20 | 26.5 | 22.5
PGD direction | 135 | 120 | 95 | 95 | 94.75 | 80.25
OGD | 108 | 90 | 85 | 85 | 85 | 70
Z | 73 | 73 | 70 | 70 | 70 | 55
COB (top dim) | 89x65x500 | 75x65x500 | 75x65x500 | 75x65x500 | 75x65x500 | 65x55x680
scaling factor | 1 | 1.35 | 1.3374613 | 1.3374613 | 1.3374613 | 1.441964286
scaling wrt to Gen1 | NA | 1.35 | 1.805572755 | 1.805572755 | 1.805572755 | 2.603571429

## Slide 8
WL
COB
BLD
8F2 Top Down View: (95x85 nm2)
OGD
BL
BL
Unit cell
WL
COB
BLD
WL
COB
BLD
WL
COB
BLD
BL
COB
BLD
COB
BLD
COB
BLD
COB
BLD
BL
PGD
BL pitch=85 nm
WL pitch=95 nm

## Slide 9
WL
WL
WL
WL
COB
COB
COB
COB
COB
COB
COB
COB
BLD
BLD
BLD
6F2 Top Down View: 95x85 nm2)
PGD: (parallel gate direction)
OGD
BL
BL
BL
BL
Unit cell
BL pitch = 85 nm
WL pitch =26.5 nm + 30 nm=56.5 nm
Dummy WL

## Slide 10
Simplest FinFET-1st Gen FinFET
2) Top gate
Gate oxide
Metal gate (ALD)
3) S/D engineering
Metals
doping
stability
ADM
1) ALD spacer fin profile
Simplest FinFET focus on topology ONLY
No shared contacts, no angling and no backside contacts FinFET
@ 107x75 nm2 (meets Gen4 scaling target)

## Slide 11
Simplest FinFET Layout
Simplest FinFET focus on topology ONLY. No shared contacts, no angling and no backside contacts
Cell Design considers BL, VCB, WL placement +EPE
Fin
Isolation
S
D
Lcon
Lg
Lcon
Ls
Ls
Fin
Isolation
S
D
Fin
Isolation
S
D
Fin
Isolation
S
D
Li
WL
BL
VCB
VCB
Wi
Wfin
WA
WA
VCB
VCB
Cell length = 2*Lcon + 2*Ls + Lg + Li
Cell width = Wi + 2*WA + Wfin
OGD= cell length direction
PGD = cell width direction
Assumptions: (PGD = 75 nm)
Wi= 15 nm
2*WA= 20 nm
Wfin= 10 nm
+ 30 nm BL/VCB shorting margin (due to all topside routing)
Assumptions: (OGD = 107 nm)
Lcon=25 nm
Lg= 30 nm
Ls= 6 nm
Li = 15 nm
Risk Items:
Top gate reliability unknown
TOP-DOWN VIEW