## Slide 1: 1222.6 Stack
CE! 1222.2 Front end
Metal 1 (90 nm)
Metal 2 (90 nm)
Metal 3 (90 nm)
Metal 4 (90 nm)
Metal 5 (90 nm)
Metal 6 (90 nm)
Metal 7 (360 nm)
Metal 8 (360 nm)
GM0 (1080 nm)
GM1 (4000 nm)
ADM section
PGD cut
OGD cut
C4B (110.3 um)
C4T needed, too

## Slide 2
Ta
CDO
ES
Logic
Memory Array
M5
M5
V4
V4
Si sub
P1222 M5/VA4 POR processing
Notes: 2

## Slide 3
5)130nm PR
4)26nm SiARC
3)170nm CHM
Logic
ADM Array
1)1.3nm HALO
No TiN
2)+42nm Copulean VBG ES
CVD (SiC) double dep 10 and 32nm
VBG patt
Ta
ES
M5
V4
Si sub
halo

## Slide 4
VBG dry etch (TAO)
Logic
ADM Array
TAO does TriLayer and Cop
Stops on halo (strong ES)
1.3nm HALO
170nm CHM
+42nm Copulean

## Slide 5
VBG ash/cleans
RCL ASH removes CHM
CAT BLU wet cleans removes HALO
Logic
ADM Array
1.3nm HALO
+42nm Copulean

## Slide 6
+ 35nm Ta (top)
CSB VBG metal fill and overburden
Logic
ADM Array
35nm TaN
1.3nm HALO
+42nm Copulean

## Slide 7
VBG polish (CE! NVM VJB polish)
1)Optically endpointed on TaN/Copulean reflectivity difference outside array
Logic
ADM Array
~20nm Cop/TaN
20nm TaN
1.3nm HALO
+42nm Copulean

## Slide 8
Bottom electrode dep/polish
35nm TiN dep “Bottom Electrode”
Hanging polish; timed. 20-25nm TiN left
Logic
ADM Array
20-25nm TiN gate electrode
20nm TaN
1.3nm HALO
+42nm Copulean

## Slide 9
137.5nm PR
26nm SiARC
160nm CHM
**Frame only**
ADB spin/expose/develop; align to MT5
ADB trilayer litho stack/SED
Frame-only topographical alignment feature
Aligns to MT5 (VBG)
Logic
20-25nm TiN gate electrode
1.3nm HALO
+42nm Copulean
20nm TaN
MT5
MT4

## Slide 10
**Frame only** -> need to have keep away distance from MT5
Logic
ADB dry etch (TAO/GTA)
Etch touched down into V4 etchstop
Etch down to V4 ES/halo
CHM
20-25nm TiN gate electrode
1.3nm HALO
+42nm Copulean
20nm TaN

## Slide 11
**Frame only**
ADB ash/cleans
Ash RCL H2/He removes CHM; DHF cleans preserves BE
Logic
20-25nm TiN gate electrode
1.3nm HALO
+42nm Copulean
20nm TaN

## Slide 12
**Frame only**
ADM stack dep
Too thick for downstream optical alignment
6nm HfOx
7nm ADM
Top seal 1nm AlOx
N implant
Logic
Needed for ADO/ADP litho to align
Full adm stack (ignore color)
20-25nm TiN gate electrode
1.3nm HALO
20nm Copulean
20nm TaN
Array

## Slide 13
ADO vert
ADP horiz

## Slide 14
Ta
CDO
ES
Logic
Memory Array
M5
M5
V4
V4
ES
ADM/HiK/TiOx Film Stack
Si sub
160nm-180nm
TiN 25 nm
HfOx 6nm
ADM 20nm
AlOx 3nm
  PVD SiN 50nm
Si 40nm
HM 30nm
Fox NSA-PSA,
TiN 25nm bot gate
HfO gate ox
ADM 10nm channel
AlO 3nm protection
PVD SiN – ILD for contact
Spu a-Si BB (BE material, sacr)
CVD SiN HM (sacr)
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 15
Ta
CDO
ES
Logic
Memory Array /PGD
M5
M5
V4
V4
ES
Litho ADO: Define OGD pat
Si sub
SiN
CHM
Si ARC
Resist
resist
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
ILD/SiN 50nm
Si 40nm
HM 30nm
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 16
Ta
CDO
ES
Logic
Memory Array PGD
M5
M5
V4
V4
ES
Spacer : low temp FOX
Si sub
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
ICE patt Siarc/CHM
Dep 32nm(?) fox to make narrower
FOX on CHM to get right etch bias
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 17
Ta
CDO
ES
Logic
Memory Array -PGD
M5
M5
V4
V4
ES
Spacer ETCH and Si etch to form Lg+S-D
Si sub
Si
Si
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
ICE patt Siarc/CHM
Dep 32nm(?) fox to make narrower
ICE etches CVD SiN and Si BB
20nm TaN
25nm TiN
6nm HfO
7nm ADM
1nm AlO
50nm SiN

## Slide 18
Ta
CDO
ES
Logic
Memory Array -PGD
M5
M5
V4
V4
ES
Si sub
Si
Si
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
ILD/SiN 50nm
Si 50nm
SiN 30nm
CHM and FOX SPCR removal with
insitu ICE + RCL for CHM
DHF clean for FOX
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 19
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array/ OGD
Resist
Si
resist
resist
resist
ADP patterning: Define transistor isolation in OGD
Memory array/ PGD
CHM
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 20
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Resist
resist
resist
resist
ADP patterning: fox spacer dep on resist
ADO/ADP same trilayer?
ADP is thicker to fill ADO topo
Memory arreay/ PGD
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 21
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory arreay OGD
Resist
resist
resist
resist
ADP patterning: ICE: Spacer etch, Si
Memory arreay PGD
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 22
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Resist
Memory array PGD
PR consumed but fox remains
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm

## Slide 23
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Resist
Memory array PGD
ADP spacer removal DHF
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
ILD/SiN 50nm
Si 40nm
SiN 30nm

## Slide 24
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
ICE etches CVD SiN and SI BB
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
hm 30nm
25nm in 2X cell
30nm in 2X cell
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 25
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
PVD SiN
50nm
Si 40nm
CVD SiN
50nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
CHM ashed with RCL O2/N2
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
25nm
30nm

## Slide 26
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory arreay OGD
Memory arreay PGD
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
ILD/Oxide 50nm
Si 40nm
HM 30nm
ANT etch dual step all the way thru TiN
20nm TaN
25nm TiN
6nm HfO
7nm ADM
3nm AlO
50nm SiN
25nm
30nm

## Slide 27
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
TiN 25nm
HfOx 6nm
ADM 20nm
3nm AlOx
PVD SiN 50nm
Si 40nm
HM 30nm
Side sealing layer of HfOx (3nm)
For wet etch selectivity
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
25nm
30nm

## Slide 28
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
TiN 25nm
HfOx 6nm
ADM 20nm
AlOx 3nm
ILD/Oxide 50nm
Si 40nm
HM 30nm
30nm AlO dep’d fills in gap between transistors
With little divots
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm

## Slide 29
Logic-Transition Vs. Array X section
AlO removed by DHF
HfO implanted by TIM
Implanted HfO rem’d by DHF
Ta
CDO
ES
M5
M5
V4
V4
ES
Logic PGD
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 30
Logic-Transition Vs. Array X section
300nm CDO film depostition
Ta
CDO
ES
M5
M5
V4
V4
ES
Logic PGD
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 31
Logic-Transition Vs. Array X section
PLM – polish down to 140nm
DROC (TAO) – remove ~20nm
120nm
20nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Logic PGD
TiN 25nm
HfOx 5nm
ADM 20nm
AlOx 3nm
PVD SiN 50nm
Si 40nm
HM 30nm
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN

## Slide 32
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
ACG+ACP patterning to define SD
CDO
TiN HM
CVD Oxide
resist
resist

## Slide 33
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
CDO
TiN HM
CVD Oxide
CAT THF to de-cap FOX
TAO removes CHM
BB
CM

## Slide 34
CVD OX HM etch, consumes FOX, Siarc
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
CDO
TiN HM
CVD Oxide

## Slide 35
resist
resist
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
CDO
TiN HM
CVD Oxide
ACP patterning
resist
resist

## Slide 36
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
CDO
TiN HM
CVD Oxide
ADP etch (ICE)
And CHM clean (TGR)

## Slide 37
10nm
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
AlOx
HfOx
20nm TaN
25nm TiN
6nm HfO
20nm ADM
3nm AlO
50nm SiN
30nm
25nm
CDO
TiN HM
ACP HM etch to transfer pattern to TiN HM (ICE)
ACP HM clean to remove remaing oxide (TGR)

## Slide 38
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
25nm TiN
20nm ADM
25nm
30nm
50nm
SiN
AlOx
20nm TaN
6nm HfO
10nm CDO
HfOx
ACT etch (ICE, etch TiN and CDO/SiN, stop on ADM)
BLU clean off remaining TiN
AA to reset ADM interface

## Slide 39
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
25nm TiN
20nm ADM
25nm
30nm
50nm
SiN
AlOx
20nm TaN
6nm HfO
3nm AlO
10nm CDO
HfOx
CON hole W:40nm/H:70nm
1nm HfOx (MIS)
CSB Cu seed
Cu EPN
1nm HfOx
CuBS+EPN

## Slide 40
Ta
CDO
ES
M5
M5
V4
V4
ES
Memory array OGD
Memory array PGD
Memory array OGD
Memory array PGD
25nm TiN
20nm ADM
25nm
30nm
50nm
SiN
AlOx
20nm TaN
6nm HfO
3nm AlO
10nm CDO
HfOx
CON hole W:40nm/H:70nm
CON Cu polish
Removes Cu/HfOx/some CDO on top

## Slide 41
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
ES Film Dep
AD1
750 nm
End of Transition
1 micron from array
2nm HALO (WE)
3.5nm Si3N4 (DE)
ES

## Slide 42
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
AD1 litho
2nm HALO (WE)
3.5nm Si3N4 (DE)
BARC
Resist
ES
AD1
750 nm
End of Transition
1 micron from array

## Slide 43
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
AD1 Etch
2nm HALO (WE)
3.5nm Si3N4 (DE)
BARC
Resist
ES
AD1
750 nm
End of Transition
1 micron from array
ICE

## Slide 44
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
AD1 ASH and Clean
2nm HALO (WE)
10nm Si3N4 (DE)
ES
AD1
750 nm
End of Transition
1 micron from array
RCL O2/N2
and BLU 120s (doesn’t blow CD)

## Slide 45
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
HM DEP
180nm
100nm
35nm TiN HM
5nm of Ti
30nm of TiN
ES

## Slide 46
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
CHM/SiARC DEP
180nm
100nm
35nm TiN HM
Currently 2000 A, but can make thinner
CHM
SiARC
ES

## Slide 47
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
BLD SED
180nm
100nm
35nm TiN HM
CHM
SiARC
Currently 2000 A, but can make thinner
PR
ES

## Slide 48
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
BLD SED
180nm
100nm
35nm TiN HM
CHM
SiARC
PR
ES

## Slide 49
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
BLD HM ETCH
180nm
100nm
35nm TiN HM
CHM
ICE
ES

## Slide 50
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
BLD in situ ASH ICE
Clean XM
180nm
100nm
35nm TiN HM
ES

## Slide 51
CHM
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
MT6 CHM/SiARC/SED
180nm
100nm
35nm TiN HM
Currently 1600 A, but can make thinner
SiARC
PR
ES

## Slide 52
CHM
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
MT6 HM ETCH
180nm
100nm
35nm TiN HM
HME
ES

## Slide 53
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
MT6 In Situ ASH
180nm
100nm
35nm TiN HM
HME ASH
XM clean
ES

## Slide 54
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
VA5 CHM/SiARC/SED
180nm
100nm
35nm TiN HM
CHM
SiARC
PR
ES

## Slide 55
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
VA5 Etch
180nm
100nm
35nm TiN HM
CHM
TAO
ES

## Slide 56
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
VA5 ASH+Clean
180nm
100nm
35nm TiN HM
*This is the ASH step that we are skewing for
V5 ASH O2N2 v H2He
RCL ASH O2N2 v H2He
CLN XM
ES

## Slide 57
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
M6+BLD BT
180nm
100nm
35nm TiN HM
HME (may change back to CAR or ICE)
ES

## Slide 58
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
M6 HMR
180nm
100nm
CAT BLU 120s
ES

## Slide 59
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
M6 CSB+EPN
180nm
100nm
ES

## Slide 60
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
M6 Polish
BLD PGD Cut landing on ACT

## Slide 61
Post M6 HM Etch
Post BT Etch
Post Polish
M6 on top, BLD on bottom (of image)

## Slide 62: COB Differences
ADM COB is in one large SiOx dielectric layer
Capacitance comes from COB only (no need to etch out bottom interconnect)
COB Size is about 170x89 in 1271.3 and it is 62x89 for X22MA
1271 REF
ADM COB
Edram | Size | Scaled area
1271.3 | 170 x 89 | 1
ADM 1.5x | 134 x 89 | 0.78
ADM 2x | 89 x 64 | 0.37

## Slide 63: Goal is to match TZT Dielectric as close as possible
1271 REF
ADM COB

## Slide 64
CHM
SIARC
Resist
V6 ES 35nm CDN
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
Etch this one first. So we do not expose Cu to CHM on the bridge via. If we etch the other one first then we have risk on wafer for corrosion and risk in FAB for Cu contamination
V5 ILD
CAP VIA (VCB) dielectric and litho stack dep and SED
V5
M6
M6
M6
VCB ILD
Array
35nm CDN ES
20nm SiOx
60nm
P3T
End of Transition
1 micron from array
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD

## Slide 65
CHM
SIARC
Resist
V6 ES 35nm CDN
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
VCB Etch - TAO
V5
M6
M6
M6
VCB ILD
Array
35nm CDN
20nm SiOx
60nm
P3T
End of Transition
1 micron from array
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD

## Slide 66
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
CAP VIA RCL H2/H2 ASH and BLUE 120s clean
V5
M6
M6
M6
VCB ILD
60nm
P3T
35nm CDN
20nm SiOx
Array
End of Transition
1 micron from array
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD

## Slide 67
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
CAP VIA fill
V5
M6
M6
M6
VCB ES
60nm
P3T
35nm CDN
Array
End of Transition
1 micron from array
CSB BS
EPN
20nm SiOx
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 68
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
CAP VIA polish
V5
M6
M6
M6
VCB ES
40nm
P3T
10nm HALO
35nm CDN
Array
End of Transition
1 micron from array
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
VCB
VCB
VCB
BLD

## Slide 69
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
V6 ES dep – AVD AlOx and CVD CDN
V5
M6
M6
M6
VCB ES
40nm
P3T
10nm HALO
35nm CDN
Array
2nm HALO
35nm CDN
End of Transition
1 micron from array
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 70
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Matching 1271.3 will use TiN HM and HALO.
Current COB height is set at 520nm for BLD height of 60
Deposit V6ES and COB ILD and TiN HM+HALO
V5
VCB ES
M6
M6
M6
Array
35nm CDN
520nm SiOx CVD
35nm TiN
6nm HALO for etch
COB ES/HM
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 71
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
M6
M6
COB/V6 ILD
CHM
Resist
SiARC
Deposit COB litho stack and SED (CBG+CBP)
CHM needs to be thick to withstand the etch. Patterning will be grating/plug matching 1271.3
M6
V5
Array
35nm CDN
520nm SiOx
35nm TiN
6nm HALO
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 72
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
COB Etch and Wet clean
V5
COB
VCB ES
BLD ES
M6
M6
M6
Array
35nm CDN
520nm SiOx
2nm HALO
35nm CDN
ICE trilayer
OXT ILD
RCL ASH
CAT DHF/SRO3B clean
CAR BT (ES)
BLU HM 270s
Halo still there
6nm HALO
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 73
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Dep Ta/TaN bottom electrode
V5
COB
M6
M6
M6
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 74
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
AMBER is the conducting TiN film. SAB is TiO2
Dep AMBER+SAB Film
V5
COB
VCB ES
M6
M6
M6
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4nm AMBER
1.5nm SAB
2nm HALO
35nm CDN
2 AVD steps
TiN (AMBER) bottom electrode
TiO (SAB) first layer of hiK
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 75
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
SLAM Dep
V5
COB
M6
M6
M6
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4 nm AMBER
1.5 nm SAB
375nm SLAM
2nm HALO
35nm CDN
Double SLM dep
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 76
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Polish for Metal recess etch
V5
COB
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4 nm AMBER
1.5 nm SAB
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB

## Slide 77
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
HME Metal Recess Etch
V5
COB
VCB ES
M6
M6
M6
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4nm AMBER
1.5nm SAB
2nm HALO
35nm CDN
HME etch
SLM
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 78
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
SLAM Clean
SR03B Cleans. Two cleans 360s each
V5
COB
VCB ES
M6
M6
M6
Array
35nm CDN
2nm HALO
520nm SiOx
30nm Ta/TaN
4.4nm AMBER
1.5nm SAB
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 79
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Deposit HiK Dielectric
Will want to tune ZrOx THX for CAP. May need to decrease.
V5
COB
VCB ES
M6
M6
M6
BLD
BLD
BLD
BLD
VCB
VCB
VCB
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4nm AMBER
1.5nm SAB
5.4nm SID
2nm HALO
35nm CDN
PGD Cut
OGD Cut
1.5nm SAB
Deposit top HiK film. ZrOx and TiOx

## Slide 80
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
M6
COB/V6 ILD
Deposit Top electrode
Dep AMBER (conductive TiN), ESM (protective film for AMBER) and TaN (copy from 1271.3)
Top will be close to pinching off. Okay if pinches off with thick dep.
V5
COB
VCB ES
M6
M6
BLD
BLD
BLD
BLD
VCB
VCB
VCB
Array
35nm CDN
520nm SiOx
30nm Ta/TaN
4.4nm AMBER
1.5nm SAB
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
2 steps
AMBER+ESM (TaAl)
1 CSB Ta
PGD Cut
OGD Cut

## Slide 81
CHM+BARC
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Deposit CTP HM and CTP litho patterning
Resist
V5
COB
VCB ES
M6
M6
M6
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
15nm TiN
2nm HALO
35nm CDN
Actually using CHM+Barc+PR
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 82
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
CTP HME Etch, ASH, and Clean
Etch away blanket TE, leaving MIM like structure floating in V6 ILD
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
ICE instead of HME, etches all stack
RCL O2N2
CLEAN DHF
BLU (TiN)
DIW
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 83
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
V6 ILD Dep
Dep rest of V6 ILD. 430nm
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 84
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
V6 ILD Polish
Do oxide polish for rest of V6 ILD and continue V6 pattern as if there were MIM (but this will be Top COB Electrode). Total oxide heght is now 800nm above top ES
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
~280+nm SiOx
2nm HALO
35nm CDN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 85
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
V6 will land on M6 and go through the TE like MIM and land on Dummy M6 (or connected). V6 OXS etch will end on HALO and the subsequent clean will take care of HALO. CAR BT will happen as normal. V6 will have to have new etch to clear metals for some V6 but not on others. HALO+COPULEAN will help stop etch for naked Via6.
Finish V6 processing and connection
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
Resist
V6
V6
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 86
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Finish V6 processing and connection
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
V6
V6
OXS
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 87
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Second Car BT Etch will land on MT6
Finish V6 processing and connection
V5
COB
VCB ES
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
V6
V6
CAR
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 88
V6 ES
CDO
WL
V4 ILD
WL
M5
M5
M5
WL
WL
M5
Logic
eDRAM Array
V5 ILD
COB/V6 ILD
Complete Connection. V6 connecting through CTP may only hang partway through the ILD, but that is okay for connection for CTP To MT7
Finish V6 processing and connection
V6
V5
COB
VCB ES
V6
M6
M6
M6
VCB
Array
35nm CDN
520nm SiOx
5.4nm SID
1.5nm SAB
2.2nm AMBER
7.2nm ESM
10nm Ta
2nm HALO
35nm CDN
CSB
EPN
PGD Cut
OGD Cut
ES
BLD
BLD
BLD
BLD
VCB
VCB
VCB

## Slide 90
TiN 20 nm
20-25nm TiN gate electrode
1.3nm HALO
+42nm Copulean
20nm TaN
HZO-6 nm
Cu
Cu
oxide
TiN-4 nm (stack #1, remove TiN if stack #2)
Silicon Oxide on Si Substrate (HiRES)-P823-3030-38
Incoming stack: 2 types
TiN/HZO/TiN
TiN/HZO only
**note that HZO/TiN thicknesses may be modulated +/- 50%
Request to strip 5 nm of TiN
Request to clean TiN electrode before HZO deposition

## Slide 91
**Frame only**
Incoming to ZDE X22S wafer:
Program- Agni
Purpose- qualify X22S for Agni Ferroelectric work
Request-
N2 plasma nitridation on TiN electrode
Constraints-
Need to not etch TiN, cause issues in frame (exposed Copulean and SiO2 ILD; 1.3 nm HALO)
Logic region
20-25nm TiN gate electrode
1.3nm HALO
+42nm Copulean
20nm TaN
Memory region
Cu (M4)
Via 4
M5