## Slide 1: 14nm JDP pathfinding – Definition Closure
DerChang, Shafqat, Sandeep, Matt, Andrea & team
DDR5 expectation, S37 Intercept and Scaling continuity
Energy Scaling in Current, Voltage and Capacitance (i∙V∙t and ½C∙V2∙n)
Die size and density chop scaling: Pitch cell, circuit under tile
Read Latency @ 80ns
Spike Mitigation
R/W Polarity

## Slide 2: 3DXP Interface vs. DDR5 Expectation
DDR4 was released to the market in 2014 after JEDEC finalized its specifications in 2012.
JEDEC is expected to release DDR5 Spec in 2018.
DDR5 is expected to be twice as fast as DDR4, far more efficient in power and twice the density.
S37 expectation: DRAM latency, BW, Power at NAND cost and capacity
  Constant Power Envelope (700mW) and constant Bandwidth/Capacity Ratio
  Double Density (512Gb)
  Double Bandwidth 3200 MT/s (initially) to 6400MT/s
Some analysts predicted that DDR lineage would end at DDR4 with alternatives to DDR DRAM such as
  Optane memory (Ironic)
  HBM
  GDDR5X

## Slide 3: S37 Intercept and Scaling Continuity

## Slide 4: High Level Scaling Strategy
Process Technology
  Cell/Array: 50% current scaling, 500mV reduction on E2 drift and Vt evolution.
  Parasitics: Array Via resistance reduction, BL/WL R∙C
  CMOS/Interconnect: low K BEOL (30% reduction) and thinner metal (20% reduction)
Design Technology
  Level Shifter improvement
  Extra supply

## Slide 5: Summary and Follow up
Scaling Goal (with respect to S26)
  ¾ Read Energy reduction for 6400MB/s
  ⅔ Write Energy reduction for 2100MB/s
Create idea list, id owners for weekly tracking in Arch PF meeting (W/7-8 PST) and TD-DE meeting (Th/11-12 PST).
Targeted definition closure by the end of Q4/2017

## Slide 6: Back Up Materials

## Slide 7: Current Scaling
Halved program current
  S26 POR is 115uA
  Using Hemant’s S15 CD learning: med Isat is 98uA and 4ua/nm @ 17nm
  14nm technology cell dimension is ~11nm
  The scaled reset current is 57.5uA.
    Med Isat is 50uA (= 98 uA – 4uA/nm * 12nm)
    IRESET TDB is 57.5uA = 13 X 1.15 over-reset

## Slide 8: Voltage Scaling
Selection:
  Reset drift reduction? Need 1V
Program
  Reduce Array Via resistance Move WSiN from 2nd cut to 1st cut  7KΩ to 0.5KΩ  sub 0.5V reduction