## Slide 1: 14nm BL/WL Resistivity using S26A Pitch Quad Mask
Kolya, Tony, Shafqat and DerChang, WW41/2017
S26A Pitch Quad L1D current Status
Proposal on resistance evaluation with single damascene copper layer
Critical path and help needed

## Slide 2: W only L1D Status, WW41
2nd cut like:
  55nm W;
  after WMMP etch:
  HM has to be adjusted (down);
  Over-etch increased.
1st cut like:
  37nm W + 25A WSiN;
  after 20s W1 etch only:
  CDs are too low; HM might need to be adjusted (down)
  Need to balance the over-etch vs undercut
  Some local blocked W etch.

## Slide 3: W only L1D Expectation
1st Cut: 37nm W / CD: 12 to 16nm
2st Cut: 55nm W / CD: 10 to 14nm
Nitride

## Slide 4: Single Damascene Copper Layer
Probe Pad -1
Probe Pad -2
Number of fingers
Length of fingers

## Slide 5: Structure Design –I: Lengths of Fingers
L1
L2
L3
L
R
Rterminal

## Slide 6: Structure Design–II: Number of Fingers
N1
N1
N3
N
R
Rterminal

## Slide 7: Critical Path and Help needed
Goal: to intercept S26A Pitch Quad W only L1D capability at best forecast capability @ WW43
Layout – 3 man∙day, need resources
Tapeout – x day, need to be prioritized
Process Development – 1 man∙week, need module allocation
Resistivity Eval – 1 man∙week, need etest bench support