## Slide 1: Pathfinding on material stack / cell architecture (DerChang’s feedback)
Maintain AR by reducing ~ 40nm in height
  Electrode thermal/electrode resistivity therefore thickness reduction
  Upto 100% PM ETH increment with higher EG (~1.5eV) material
  Some opportunity in SD3 threshold field improvement with CD scaling
  SD electrode/interface to increase ITH therefore VTH
Thermal profile management  Improve electro-thermal efficiency and Thermal disturb immunity
  Electrode resistance gradient
  Hot spot management – ME or PM
  Liner/Seal/gapfill thermal boundary resistance improvement
  Upper deck WL tungsten heat removal
SET Strategy –
  Homogenous nucleation or heterogeneous nuclearation?
  If HomoG nuke Thermal profile decision – symmetry (center hot spot) vs. asymmetry thermal profile (grow from edge)
  Ig HeteroG nuke -- where is the seed layer therefore hot spot management?

## Slide 2: SXP Project 30s SxP: on the cell architecture September 21st, 2015
30s Team

## Slide 3: From 10s to 30s: Scaling options
37 nm
PM
SD
BE
ME
TE
20 nm
16 nm
10 nm
15 nm
5 nm
30s must double the density:
10s SxP
30s SxP hypothesis:

## Slide 4: From 10s to 30s: Scaling options (1/2)
37 nm
PM
SD
BE
ME
TE
20 nm
16 nm
10 nm
15 nm
5 nm
10s SxP
30s SxP
Isotropic scaling
Considering a perfect isotropic scaling by 70% of each quantity (apart laminas)
26 nm
PM
SD
BE
ME
TE
12 nm
7 nm
10 nm
5 nm
7 nm

## Slide 5: From 10s to 30s: Scaling options (2/2)
30 nm
PM
SD
BE
ME
TE
12 nm
7 nm
7 nm
5 nm
26 nm
PM
SD
BE
ME
12 nm
7 nm
14 nm
7 nm
30s SxP
More reasonable scaling
30s SxP
Isotropic scaling
TE
10 nm
5 nm
Saving A/R from electrodes and giving more room to PM

## Slide 6: Chances for a more thermally symmetric structure
30 nm
PM
SD
BE
ME
TE
12 nm
7 nm
7 nm
5 nm
7 nm
30s SxP
Plausible scaling
30 nm
PM
SD
BE
ME
TE
12 nm
7 nm
5 nm
5 nm
7 nm
5 nm
30s SxP
Symmetrizing the nr of interfaces below and above PM
Note:
We could think to thinner flash lamina recovering 2 nm allowing a PM height = 32 nm

## Slide 7: VTH scaling
CLV
PTX @ 30 nm
S15
30s
We could hypothesis to re-gain the ~150 mV in VT due to the lower PM thickness as a consequence of the VT increase with cell area scaling
Very rough-preliminary data extrapolation – just to have a first idea