## Slide 1: Ihold vs Electrical Distance
S15C QTT
asebasti
See the notes on the left margin of many of these slides for instructions on their use.

## Slide 2: Ihold vs. ED: preliminary data
S15C QTT
Lot 9922922 wf #1
Cell rev. 7.45; CMOS rev. C17
Flow:
  FF
  ON-IV
Ihold decreases with higher electrical distance
Data only from D0; test @ 25C Scope traces (not reported here) are ok.

## Slide 3
Slope : -0.1uA / Kohm
Tot WL+BL length in number of equivalent cells
(WL length * ~12Ohm/sq + BL length * ~4.5Ohm/sq)

## Slide 4: First fire
No trend of First fire with ED