## Slide 1: VT sigma: scaling projections
For the DTS of 30S
Paolo

## Slide 2: VT sigma: scaling rules
VT distribution includes both the b2b variability and Bounce:
In fact, being:
The most evident scaling rule of the sigma VT is with the SD thickness (tSD):
related with elemental composition fluctuation
related with SD thickness fluctuation
where:
The ETH fluctuation term is related with the EG variability and in this model does not scale with area. In the past we obtained reasonable modeling with 1% stoichiometry fluctuation for each element of the SD (link at JET meeting)

## Slide 3: VT sigma: PTX – 10S comparison and 30S projection
S15 data
PTX
S15 data reports today the sigma VT ~120 mV in reasonable agreement with PTX data (array PTX data are also a bit worse as a consequence of the not optimized process control)
Coherently with model (previous slide) we can conclude that we do not expect a worsening scaling of the sigma VT with cell area scaling
Key point: for 30S we propose to assume 120 mV as target value for sigma VT of DTS

## Slide 4: Back-up

## Slide 5: Sigma EG:
Then we can computed the sigma of EG due to the statistical fluctuation of the elemental concentration ai:
From the experimental trend (obtained also on S15):
This local fluctuation (die level) of the elemental composition cannot be experimentally measured. We can suppose it in the range of 1%.
It is a % fluctuation, so it does not scale with volume/area.

## Slide 6: Possible influence of discreetness nature
If we suppose a Poissonian distribution of the number of traps (NT) inside the SD
NT fluctuation will be correlated with a variation of the activation energy for conduction EA inside the SD
Dividing member-by-member:
;
Only with a value of NT inside the SD < 25 the Poissonian spread of NT is expected to play a role. Reasonable values for NT are in the range of thousands (on 105 atoms).