## Slide 1: Ihold vs Electrical Distance
S15C QTT
asebasti
See the notes on the left margin of many of these slides for instructions on their use.

## Slide 2: Summary
Lot 9993272 wf 9 cell rev 7.64
Ihold vs. ED (Electrical Distance) vs Deck vs. Cycles
  Ihold increases with lower access resistance (lower ED)
  Ihold on Deck 1 lower than Deck 0
  Ihold increases with cycles
Ihold vs. buffer capacitance
  With same ED, cells with WL buffer connected to LWL have Ihold higher than cells with buffer connected at HNREG (+1.2uA on virgin cells, +2.3uA after 10Kcycles)
Ihold vs. LWL voltage
  Small trend of decreasing Ihold with lower LWL (from 13.5uA to 12.4uA, when LWL goes from 3.6V to 1.7V)
Ihold vs ON-IV slope (ramp down)
  Lower ramp down time  lower Ihold (from 20us to 500ns (POR is 2us)  Ihold from 14.4uA to 12.3uA (with very fast ramp rates, there could be detection problems)
Next: I hold vs Temperature

## Slide 3: 9993272 wf 9 cell rev. 7.64 : Deck 0
Values of R used for Rtot calculation: WL : R ~10; BL : R ~ 4.5
Ihold increases with lower access resistance
Ihold increases with cycling
Virgin
1Kcycles
10Kcycles
ED4-D0, ED4-DO_DIAG1, ED4-DO_DIAG2, ED4-DO_DIAG3 are ED4 cells in different positions in the QTT, trying to imbalance WL and BL length

## Slide 4: 9993272 wf 9 cell rev. 7.64 : Deck 1
Values of R used for Rtot calculation: WL : R ~10; BL : R ~ 4.5
Ihold increases with lower access resistance
Ihold increases with cycling
Ihold of D1 lower than D0

## Slide 5: Ihold on D0: data

## Slide 6: Ihold on D1: data

## Slide 7: ON-IV characterization
Local buffers
Global buffers
AXN/HNREG buffers
Array path
Scheme of WL buffer connections:

## Slide 8: Effect of WL buffer capacitance
ED2-ONIV cells: WL buffer connected at LWL (higher capacitance)  higher Ihold
ED2 cells: WL buffer connected at HNREG ( lower capacitance seen by the cell)
Ihold vs. access resistance  same ED !!

## Slide 9: Effect of WL buffer capacitance (deck 1)
ED2-ONIV cells: WL buffer connected at LWL (higher capacitance)  higher Ihold
ED2 cells: WL buffer connected at HNREG ( lower capacitance seen by the cell)
Ihold vs. access resistance  same ED !!

## Slide 10: Imax and LWL segmentation (ED2-ONIV cells after 10kcycles)
Same median value
std
Imax =60

## Slide 11
LWL=3.6V
LWL=1.7V
ON-IV full curve
Imax=60uA
LWL is low for all the ON-IV measure
LWL: from 3.6V to 1.7V
Ihold shows a small decrease (from 13.5uA to 12.4uA, when LWL goes from 3.6V to 1.7V)

## Slide 12: ED2-CELLS after 10Kcycles
Repeat same experiment of previous slides (LWL segmentation) on std cells (WL buffer connected at HNREG)
std
Imax =60

## Slide 13
Detection issue on these cells, when LWL is low
LWL=3.6
LWL=3.5
Detection problem
ON-IV
Decreasing LWL, higher series resistance and voltage drop at HNREG

## Slide 14: Ihold vs ramp down (ON-IV slope)
Lower ramp down time  lower Ihold (from 20us to 500ns; POR is 2us)
No effect on ON-IV curve
With 500ns time, there is an impact of scope resolution of time axis ( small increase of Ihold with 1us/div instead of 2us/div, +0.12uA)
VPXS trace: 2 mV/div (POR conditions). With 1 us, Ihold is higher (+2.3uA)
ED2-D0_ONIV cells, 10Kcycles
VPXS trace: 2mV/div
ON-IV: all curves
(red: ramp up
Blue: ramp down)

## Slide 15
Std condition (ramp down = 2us)
ramp down = 20us
ramp down = 500ns
ramp down = 500ns

## Slide 16: Ihold vs ramp down (ON-IV slope)
Lower ramp down time  lower Ihold (from 20us to 500ns; POR is 2us)
No effect on ON-IV curve
With 500ns time, there is an impact of scope resolution of time axis (Ihold increases with 1us/div instead of 2us/div, + 0.37uA)
Median values
ON-IV: all curves
(red: ramp up
Blue: ramp down)
ED2-D0_ONIV cells, 10Kcycles
VPXS trace: 1mV/div

## Slide 17: Ihold vs ramp down : waveform and traces
2us
20us
1us

## Slide 18: Ihold vs ramp down : waveform and traces
500ns
500ns
Scope 1us/div

## Slide 20
LWL = 1.6V

## Slide 21
LWL = 1.4V

## Slide 22
LWL = 1.2V

## Slide 23
LWL = 1V

## Slide 24
LWL = 0.8

## Slide 25
LWL = 0.6V

## Slide 26
LWL = 0.4V

## Slide 27
LWL = 0V

## Slide 28: Next
Misure su ED2-ONIV e ED2-std
Misure dopo 1Kcycles
Valutare dipendenza da capacita’
LWL dependence ?  1
Deck 1 ?
Aumentare statistica ?
Cell rev piu’ recente ? (7.64?)
Misurare a pari BL resistance e varie WL che coprono I vari ED
Slope della ON IV !!!!!!!! (up, down, up/down)  2
Cell rev. trend chart

## Slide 29: Ihold vs. ED: preliminary data
S15C QTT
Lot 9922922 wf #1
Cell rev. 7.45; CMOS rev. C17
Flow:
  FF
  ON-IV
Ihold decreases with higher electrical distance
Data only from D0; test @ 25C Scope traces (not reported here) are ok.

## Slide 30: 9993272 wf 9 cell rev. 7.64
Trend of First Fire with access resistance

## Slide 32
WL : R ~10
BL : R ~ 4.5

## Slide 34
Vt detection (Second Fire routine)
Ilim=12uA (all cells have oscillations)