## Slide 1: 30s MTS change proposal
Beyond 10s architecture pathfinding team

## Slide 2: MTS Rev0
Anisotropic scaling approach adopted to guarantee the constant V prog and RWB scaling
Constant thickness scaling (also for W interconnect)
WSiN scaled to 4 nm (from 10s 5 nm) to reduce impact on AV1 R
CN electrode adopted at ME and TE, actually not POR in 10s/20s cell
AV1 (AV3/5/7) has WSiN on top (not reported here)
BL W 55 nm
WSiN 4 nm
HUCN 8nm + HUC 2 nm
TopL 2 nm
PM 40 nm
BottomL 2 nm
HUCN 5nm + HUC 7 nm
+ HBC 5 nm
SD 17 nm
HUC 3 nm + HUCN 7 nm
WSiN 2.5 nm
WL W 35 nm

## Slide 3: MTS Rev1
PM thickness reduction mandatory for WD management and quad pitch development; small reduction of TE, ME and BE thickness to further help WD.
No thickness scaling of WL/BL W until we get rho values from W-only (possibly it can go in MTS Rev2)
No change in SD thickness to guarantee absolute set Vt and leakage
No change in WSiN 2nd cut thickness wrt 10s/20s (+1 nm wrt 30s Rev0)
PM moves from 40 nm  30 nm
BE moves from 3 nm HUC+ 7 nm HUCN  3 nm HUC + 5 nm HUCN
TE moves from 10 nm HUC (post CMP)  8 nm HUC (post CMP)
ME moves from 5 nm HUCN/ 7 nm HUC/ 5nm HBC to 10 nm HUC + 5nm HBC
Via has no WSiN on top, assuming we will adopt a no-WSiN via approach
BL W 55 nm
WSiN 5 nm
HUC 8 nm
TopL 2 nm
PM 30 nm
BottomL 2 nm
HUC 10 nm + HBC 5 nm
SD 17 nm
HUC 3 nm + HUCN 5 nm
WSiN 2.5 nm
WL W 35 nm

## Slide 4: MTS Rev0/Rev1 comparison
 | Rev0 | Rev1
1st cut AR | 10 | 8.9
2nd cut AR | 11.2 | 10.14
WD projected | 0.4X wrt 10s | 1X wrt 10s
IRST projected | 69 uA | 71 uA
AV1 R | 1.6X 10s | 0.2X 10s*
ΔVt (@1e-6s, 85C) | 1.18V | ~1.0V
AR calculated assuming +5nm TE @ 1st cut due to 65CMP consumption
Drawing in scale
Rev0
Rev1
*Silicon validation on going
Main drawback of PM scaling is the intrinsic window decrease

## Slide 5: Possible execution plan to get to MTS rev1
Move L1D QP on t_x and mat_x
Y-GST on S15/S26
L1D ok & t_x<30 nm?
Start L3 with t_x and mat_x
Yes
No
increase thickness
t_x=t_x+5nm
L3 show better set-Vt trade-off?
Yes
No
mat_x=Y-GST
mat_x =In-GST skew
t_x= 15 nm* mat_x=In-GST
t_x= PM thickness
mat_x= PM material
*initial thickness to be adjusted based on DE feedback
is t_x=30 nm?
No
Stop L1D
Yes

## Slide 6: Milestone by quarter for S37 DBR
 | Q1 | Q2 | Q3 | Q4
S37 |  |  |  | DBR
CMOS/BEOL | 4800MT/s | Low-K dielectric |  | Should we do 2-phases? If so, firs step is 3200MT/s 4800MT/s need to be in-sync with 60pJ/b for write and 35pJ/b for read (1600/4800 MB/s of W/R BW)
Array/DTS/RWB | WL/BL R/C Array Via resistance | PM thickness requirement to meet ∆VT RWB Gap assessed | DTS/Reliability gap assessed Rev 1 Roadmap for PG4 developed | Reset current (delivery vs. I3) aligned Energy reduction roadmap developded
Integration/MTS |  | Structure yield One S36X single deck die functional | S37A0 Start Up flow and roadmap | 
PM material | Y-GST go-nogo (S15 based) |  |  | 
SD material | In-SAG go-nogo (based on S15) |  |  | 
S36X |  |  |  |