## Slide 1: On the superposition of time, temperature and cycling effects on the VTH stability
Building a strategy the VT control
Paolo and DerChang

## Slide 2: VTH trend vs the device life time: a holistic figure
FF
SF
Cycling
T
Stress
time
Recovery time
Segr + Drift + E/I forming
Drift
Permanent loss in 10 yrs @85C
Contaminants +…
induced Cyc degradation
The overall figure of the VTH evolution returs a wide VT range (>3 Volts!) spanned over the entire device life time
To scale down the SxP technology we need to learn how to control better and better the VT evolution
This aim can be reached only with a well addressed 360 MAP strategy

## Slide 3: Key-points of the strategy to control the VTH
Develop a physics-based switching model allowing to indicate the physical quantities modulating the switching [link]
How does the process manipulate or is neutral with respect to SD material? In S15 a huge impact of the process is captured, however the microscopic understanding is still incomplete [link]
More stable SD materials (In-SiSAG is a candidate – see last meeting)
Algo: the role of readout Algo (tsense); better understanding of Seasoning and cycling effects [VT evolution huddle]
to Goal

## Slide 4: Switching model understanding
+
-
Holes energy
Highest II probability for holes
SD thickness
back
The relationship between VTH and the SD film optical band-gap has been highlighted and verified on variuos vehicles/cell rev
The gap dependence of VTH has been also physically explained in terms of avalanche phenomena at switching
However, a complete physics-based model of switching is still under scrutiny
We are addressing this also thru the collaboration with Politecnico of Milano (update scheduled for next month)

## Slide 5: The key role of the process on drift performances
The pronounced impact of the cell rev. is captured, neglecting the same SDv12 film that Swapnil deposited!
The role of SD film is observable, but the process impact is huge
We need to enhance our ability to invetigate microscopically how process alterates the SD cell
At the next meeting Hefei will give the picture of the State of the Art about the TEM characterization of chalcogenides-based cells
SDv12 – old cell rev
SDv12 – new cell rev
back
85C
40C

## Slide 6: VT evolution: 30S goal
Today the key-points of the learnt lesson from S15 to mitigate drift thru the process are reported (Jenny, Dany, Darren, DerChang)
The goal of 30S is to strongly tighten the VT evolution
Stress
time
Recovery time
Forming limited:
  Al2O3 laminas
  Bi-layered SD
Cycling degradation limited:
  H-k seal Cell iso
Drift limited:
  In-SiSAG film
  Process optimization
Some seminal ideas:

## Slide 7: Integrated 30s Pathfinding Strategy
Expanding scorecard with probe-able single chal L1D.
  L1E: Electrical testable L1D  this is what we called L2 in the past
  Physical (L1D) and Electrical (L1E) scorecard to be developed to rank the integrity of stack and material sensitivity to the architecture.
Effectively building pathing finding collateral using other JDP projects
  5 JDP projects – S15 PG4, S15 PG1, S26, SSM, S37
  Cell architecture learning comes from S15 and S26 – what to test and how to score
  Fully exploit SSM to build pathfinding collateral of scaled cell (L1E)