## Slide 1: State of art about the TEM characterization of chalcogenides-based cells
Hefei Hu, Rohini Sankaran, Mary Alexander, Dan Baumbach, John Nugent
Intel Folsom TEM lab

## Slide 2: Outline
Structural analysis by (scanning) electron diffraction
  Detection of nucleation site (small nano-crystal)
  Amorphous transition on dual deck
  Analysis of amorphous diffraction ring
Determination of amorphous thickness by combing NBD and DF-STEM
EDX analysis of PM
  Bit-level correlation (segregation and contamination)
  Electrical distance (ED) dependent segregation
Challenge of EDX analysis of SD
  FIB prep induced segregation in SD
  Si% quantification in SD delta – planar view sample prep
Electron energy loss spectroscopy (EELS)

## Slide 3: Structural analysis by electron diffraction - Phase identification

## Slide 4: Detection of nucleation site
5nm probe size, scanning capability
Provides a definitive answer on crystallinity (compared to HRTEM)

## Slide 5: Amorphous transition
5
Element
-
+
-
+
Thermal profile
Hotter
Cooler
2D0
2D1
2D0 and 2D1 has opposite element segregation direction because of polarity.
However, the thermal profile in the PM are matched between decks because stack is matched.
2D0
2D1
TEC
SD
MED
PM
TEC
W
-
+
-
+
Te rich
Sb/Ge rich
Te rich
Sb/Ge rich
Low Melting temperature
High Melting temperature
Low Melting temperature
High Melting temperature
Hongmei/Yao-Feng

## Slide 6: Amorphous transition
6
Element
-
+
-
+
Thermal profile
Hotter
Cooler
2D0
2D1
Amorphousizing
2D0
2D1
-
+
-
+
2D0 and 2D1 has opposite element segregation direction because of polarity.
However, the thermal profile in the PM are matched between decks because stack is matched.
Amorphous start from Sb rich area for both decks.
2D0
2D1
TEC
SD
MED
PM
TEC
W
-
+
-
+
Te rich
Sb/Ge rich
Te rich
Sb/Ge rich
Low Melting temperature
High Melting temperature
Low Melting temperature
High Melting temperature
2D1
2D0
Hongmei/Yao-Feng

## Slide 7: Phase identification
PFA-347 Group 3 FCC [3 -1 2]
d1*
d2*
Simulation
Measured d1= 1/d1* = 1.38 Å (1 -3 -3)
Calculated d1 = 1.38 Å, 0.0 % difference
Measured d2 = 1/d2* = 3.45 Å (-1 -1 1)
Calculated d2 = 3.48 Å, 0.9 % difference
PFA-302 sample 3 66 HCP [3 4 -2]
d1*
d2*
Measured d1 = 1/d1* = 3.354 Å (0 -1 -2)
Calculated d1 = 3.368Å, 0.4% difference
Measured d2 = 1/d2* = 2.087 Å (2 -1 1)
Calculated d2 = 2.097Å, 0.5% difference

## Slide 8
Quantitative analysis of amorphous rings
SD1
Electron diffraction
SD v10
Electron diffraction
 | PFA number | Ge% | As% | Se% | Si% |  | 
SD1 | PFA-560 | 26.1 | 29.3 | 44.4 | 0 |  | 
SD2 ver10 | PFA-591 | 15.4 | 29.9 | 48.3 | 6.5 |  | 

## Slide 9
Quantitative analysis of amorphous rings
SD1
Electron diffraction
SD v10
Electron diffraction
 | PFA number | Ge% | As% | Se% | Si% | Peak 1 (1/Å) | Peak2 (1/Å)
SD1 | PFA-560 | 26.1 | 29.3 | 44.4 | 0 | 3.43 | 5.81
SD2 ver10 | PFA-591 | 15.4 | 29.9 | 48.3 | 6.5 | 3.43 | 5.78
SD1
SD v10
1/Å
Peak 1
Peak 2
Curve fitting:
background: exponential decay
Peak 1: Lorentzian function
Peak 2: Gaussian function
No obvious difference between SD1 and SD v10

## Slide 10: Determination of amorphous thickness by combing NBD and DF-STEM

## Slide 11
Optimization of camera length (tested on 4 partially crystalline/amorphous bits)
cl=150mm
cl=200mm
cl=300mm
cl=490mm
cl=680mm
cl=970mm
cl=1850mm
cl=3000mm
cl=4000mm
cl=4500mm
HAADF STEM – Z contrast
DF STEM – diffraction contrast
BF STEM – diffraction+thickness contrast
90 uA/0/(31)
90 uA/1e6/(30)
HAADF STEM provides difference in contrast only for bit 30 on 2D1 (cl 150mm), but not for the other 3 bits.
BF STEM provides some contrast difference between crystalline and amorphous phase, but thickness contrast washes it out a little bit.
DF STEM leads to better diffraction contrast, providing contrast difference for all the other 3 bits (cl 680mm)
cl 680mm was used to take DF STEM images for this sample.
crystalline
amorphous
crystalline
amorphous
crystalline
amorphous

## Slide 12
Orientation-dependent contrast of DF STEM images (cl 680mm)
crystalline
amorphous
crystalline
amorphous
No tilt
90 uA/0/(31)
90 uA/1e6/(30)
5° beta tilt
crystalline
amorphous
With cl 680mm at 5° beta tilt, the bit that doesn’t show contrast at zero tilt shows good contrast between amorphous and crystalline areas.
Tilt of 5°/10°/15° in beta direction and tilt of 10° in alpha direction were used to image all the bits

## Slide 13
All the partially amorphous bits show clear contrast difference between amorphous and crystalline phases at different tilt angles.
Caution: either amorphous or crystalline phase could show brighter contrast than the other phase due to the nature of diffraction contrast (bit 07 vs bit 06 on the left image). Hence, scanning NBD is needed to provide determinate phase information (whether it’s crystalline or amorphous, and phase identification). NBD study of this sample can be found here: https://intelweb.micron.com/sites/sxp/10s/SXP%20Cell%20Sync%20Meeting/Intel%20TEM%20Folder/pfa-942/PFA-942%20FM%20TEM%20Report.pptx
Once phase information is determined by NBD, contrast of DF STEM can be correctly interpreted (whether it’s amorphous or crystalline). Amorphous thickness or fraction can be measured using DF STEM images.
124108
124104
90uA
0
90uA
1e6
124107
124106
5° tilt
10° tilt
c
c
a
a

## Slide 14: EDX analysis of PM - Bit-level correlation (segregation and contamination)

## Slide 15: Set probability PFA (LQ 54)
Wafer | Die | Partition | Slice | Tile | X_Addr | Y_Addr | Phys WL | Phys BL | Phys Slice | Phys Quat. Tile | set prob | Final State | npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 |  |  | 207329 | 260577 | 50 | 250 |  | virgin | 
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 67 | 207329 | 260578 | 50 | 250 | 0.65 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 99 | 207329 | 260579 | 50 | 250 | 0.45 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 68 | 207329 | 260580 | 50 | 250 | 0.65 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 100 | 207329 | 260581 | 50 | 250 | 0.65 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 69 | 207329 | 260582 | 50 | 250 | 0.85 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 101 | 207329 | 260583 | 50 | 250 | 0.35 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 70 | 207329 | 260584 | 50 | 250 | 0.25 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 102 | 207329 | 260585 | 50 | 250 | 0.3 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 71 | 207329 | 260586 | 50 | 250 | 0.5 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 103 | 207329 | 260587 | 50 | 250 | 0.5 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 72 | 207329 | 260588 | 50 | 250 | 0.15 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 104 | 207329 | 260589 | 50 | 250 | 0.35 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 73 | 207329 | 260590 | 50 | 250 | 0.25 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 105 | 207329 | 260591 | 50 | 250 | 0.25 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 74 | 207329 | 260592 | 50 | 250 | 0.2 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 106 | 207329 | 260593 | 50 | 250 | 0.9 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 75 | 207329 | 260594 | 50 | 250 | 0.35 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 107 | 207329 | 260595 | 50 | 250 | 0.6 | set | LQ47FA_odd.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 76 | 207329 | 260596 | 50 | 250 | 0.55 | rst | LQ47FA_even.npt
9423612.0D3 w23 | 1,10 | 12 | 2 | 3 | 89 | 108 | 207329 | 260597 | 50 | 250 | 0.55 | set | LQ47FA_odd.npt
 |  |  |  |  |  |  | 207329 | 260598 | 50 | 250 |  | virgin | 
The shortest pulse was used
Each bit was tested for 20 times

## Slide 16: Set probability PFA (Set prob vs composition (LQ 54) )
Se contamination in PM shows correlation to SET probability.

## Slide 17: Set probability PFA (set vs rst (LQ 54))
Te/Sb occurs similar for set and rst.

## Slide 18: Tgrowth PFA
Crystallization 1-> 7
E-test Result:
tgrow vs cycle from virgin
Virgin + placement
0: Virgin + test (reset + set + RO)
PFA Result:
“Gradual” element segregation builds up for both decks from virgin to a few cycles. No significant difference between decks up to probe condition.
From probe to 1million cycle, D1 has larger segregation increase than D0
Test Result:
Growth time shows significant deck-to-deck difference in 1-2 cycles after virgin.
At probe condition, usually 30ns tgrow deck to deck difference
A
B
B
A
PFA 1029 Yao-Feng Rohini Hefei Lu Hongmei

## Slide 19: EDX analysis of PM - Electrical distance (ED) dependent segregation

## Slide 20: PM segregation at NN/MM/FF on 2D0 and 2D1
Top vs bottom EDX analysis doesn’t show much difference at different ED.
Vt window seems to be anti-correlated to PM segregation index
FF has the smallest window, which is probably not seasoned properly. Trim by ED has been implemented.

## Slide 21: PFA-942 sample 3 raw EDX linescan (2D0)
8nm
Sb saturated
7nm
Sb saturated
No flattop
12 bits of each location (NN/MM/FF) on 2D0 are averaged to improve statistics.
On 2D0,
  At NN/MM, Sb is found to be saturated in the area of 8nm/7nm from bottom W lamella.
  At FF, Sb is not saturated at PM bottom, which can be explained by its larger electrical distance from the driver.
Sb saturation is consistent with Vt window. FF has the smallest window, which is probably not seasoned properly. Trim by ED has been implemented.
Ge
In
Sb
Te

## Slide 22: PFA-942 sample 3 raw EDX linescan (2D1)
Ge
In
Sb
Te
Te saturated
4nm
12 bits of each location (NN/MM/FF) on 2D1 are averaged to improve statistics.
On 2D1,
  At NN/NN, Te is found to be saturated in the area of 7nm/4nm from bottom W lamella.
  At FF is not saturated at PM bottom, which can be explained by its larger electrical distance from the driver.
Te saturation is consistent with Vt window. FF has the smallest window, which is probably not seasoned properly. Trim by ED has been implemented.
Te saturated
7nm
No flattop

## Slide 23: Challenge of EDX analysis of SD - FIB prep induced segregation in SD

## Slide 24: Sample prep challenge for SD delta
Sample prep induced Se/As segregation in SD delta was a long-standing problem, making it impossible to see the true signal of Se/As segregation from electrical programming.
This Se/As segregation was shown experimentally to be cut-direction dependent, as demonstrated in the figure below:
  on x-cut, Se moves towards SD bottom and As moves towards SD top.
  on y-cut, Se and As move in an opposite direction.
Wafer information: Rev 6.7 WL BGM, WLWSiN, 65NCMP PL6118, virgin die
Ga+
+
+
+
+
+
+
+
+
+
+
+
+
E-field
E-field
E-field
E-field
X-cut: floating WL
Y-cut: floating BL
Ga+
Se-
As+
Se-
As+
Se-
As+
Se-
As+

## Slide 25: Grounding method (single deck)
Pt cap
e-
e-
e-
e-
e-
e-
e-
e-
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
WL is connected to BL through Pt cap, making WL and BL equal potential.

## Slide 26: Segregation vs cycling/final state (LQ67)
PM
*Note: 1. cycling of “-1” means virgin bits
2. The sample is properly grounded, but it is noted that virgin SD showed Se/As index of 1.1. It’s possible that chemical gradient existed in virgin bits.
SD
1. Segregation in PM remains more or less the same with cycling. No obvious difference between SET/RST states except for 1e7 cycling which showed strong segregation for RST bits
2. Segregation in SD clearly increases with cycling. RST bits showed stronger segregation than SET bits.
SD
PM

## Slide 27: Grounding method (dual deck)
Pfa-956 ycut
Pfa-956 xcut
Properly
grounded
Not properly
grounded
No grounding

## Slide 28: Segregation in SD delta on dual deck (submitted by Fuga)
SD top is Se rich and As poor on 2D1, which is opposite to our previous observation in SD1.
Overall, in terms of final state, segregation in SD shows the same trend as seen in PM: Untouched < SET < Seas_SET < RST
SD delta
SD1

## Slide 29: Challenge of EDX analysis of SD - Si% quantification in SD delta

## Slide 30: Planar-view sample prep – quantification of Si in SD delta

## Slide 31: EDX analysis of SD delta - linescan
Lateral EDX scan
vertical EDX scan
Lateral EDX scan
vertical EDX scan
There is a flat area of Si in SD which is from SD.

## Slide 32
SD v10 – composition as a function of acquisition time
Si map
Quantification without Si
Quantification with Si
Quantification box
EDX quantification was done every 1 minute to monitor composition change.
Se% was found to be gradually decreasing and Si% was increasing during EDX mapping. There was also a small increase in Ge%

## Slide 33
1min
2min
4min
6min
8min
10min
SD v12 – EDX mapping over acquisition time
Se was gradually moving out of the cell during EDX mapping, while Ge and As maps showed no obvious change.

## Slide 34: Comparison of EDX collection efficiency
 | Tecnai (200kV) | Osiris (200kV) | Themis (200kV) | Themis (80kV)
Beam current (nA) | 1.0 | 0.31 | 1.0 | 1.0
Se peak count rate (cps/eV) | 1.2 | 0.8 | 5.4 | 9.0
Efficiency (cps/eV/nA) | 1.2 | 2.6 | 5.4 | 9.0
Tecnai 200kV
~ 1.2 cps/eV at Se peak
Themis 200kV
~ 5.4 cps/eV at Se peak
Comparison method:
Spectra from the same size of area on SD are extracted from different TEMs/settings for efficiency comparison.
Se peak counts are taken as a reference
Conclusion: Compared to Tecnai 200kV in Folsom, Themis 200kV provides ~4.5 times more efficiency and Themis 80kv provides 7.5 times more efficiency.
~ 9 cps/eV at Se peak
Themis 80kV
Osiris 200kV
~ 0.8 cps/eV at Se peak

## Slide 35: Electron Energy Loss Spectroscopy (EELS)

## Slide 36: Electron energy loss spectroscopy in ADF-STEM
Specimen
ADF detector
Electron probe
DE
EELS spectrometer
R. Egerton, Electron Energy-loss Spectroscopy in the Electron Microscope, 3rd Edition, Springer, 2011

## Slide 37: Fine structures of different carbon materials
R. Kuzuo et al., Phys. Rev. B, 49 (1994)
Low-loss EELS
Core-loss EELS

## Slide 38: SD core loss
Ge/As/Se all have broad peaks with no fine structures
Hongqi Li, Micron

## Slide 39: SD low loss
SD1
SD v10
SD1
SD v10
Plasmon peak
1
2
3
3
2
1
Plasmon energy is the same for SD1 and SD delta v10
Three transitions (peak 1, 2 and 3) were observed in low-loss region. No much difference between SD1 and SD delta v10 was observed.

## Slide 40
EELS mapping of SD
Spectrum from
Carbon electrode
ϖ plasmon
ϖ+σ
plasmon
SD plasmon
Spectrum from SD
SD
C
liner
As-M4,5
Ge-M4,5
Spectrum from
liner
Carbon ϖ and σ bonding are observed in carbon electrode, reflected by two plasmon peaks (~5eV and ~23.6eV).
Plasmon energy of SD (~18 eV) is lower than that of carbon electrode (~23.6 eV).
Ge-M4,5 and As-M4,5 edges are observed in SD low-loss spectrum.
Edge A and B are observed in seal, but not identified yet.
liner
plasmon
A
B

## Slide 41
EELS mapping of SD - continued
SD
C
seal
Carbon ϖ plasmon (4-6 eV)
Liner edge A (10-11 eV)
SD (17-19 eV)
Overlay

## Slide 42: Conclusion
Electron diffraction can be used to identify phase information of crystalline PM and study amorphous PM and SD.
Contrast between amorphous and crystalline areas can be distinguished by DF-STEM imaging with optimized CL. Diffraction may be needed to determine whether it’s contrast of amorphous phase or crystalline phase.
Bit-level correlation between composition and electrical signals is generally not clear. So far, the only clear trend is that Se contamination in PM decreases PM set probability.
EDX analysis of SD delta is very challenging. Grounding method has been developed to get rid of FIB induced segregation. However, SD segregation direction is not polarity dependent, which needs to be further verified. Planar-view sample prep is developed to quantify Si%, but beam damage causes composition change during data collection.
EELS may be useful for future experiments.