## Slide 1: Atomistic simulation results of Zr/Hf-doped GST
Through the collaboration with Prof. Marco Bernasconi
Paolo Fantini
To create this effect:
  From Selection Pane, hide Tinted Rectangle.
  Use Change Picture command to place photo. Or replace it with a Clipboard paste or a drag and drop from a folder.
  Unhide Tinted Rectangle and set it to desired level of transparency. (25% usually works well.)
  From the Title Slide layout, copy and paste the circuit line and the logo onto this slide.
See the notes on the left margin of many of these slides for instructions on their use.
©2015 Micron Technology, Inc. All rights reserved. Information, products, and/or specifications are subject to change without notice. All information is provided on an “AS IS” basis without warranties of any kind. Statements regarding products, including regarding their features, availability, functionality, or compatibility, are provided for informational purposes only and do not modify the warranty, if any, applicable to any product. Drawings may not be to scale. Micron, the Micron logo, and all other Micron trademarks are the property of Micron Technology, Inc. All other trademarks are the property of their respective owners.

## Slide 2: Simulation framework
A 297-atom cubic cell of molten Ge2Sb2Te5 (GST)
2 doping levels have been considered:
  7 atoms of Ge atoms substituted with Zr or Hf corresponding to a doping of ~ 2.4 %
  14 atoms of Ge atoms substituted with Zr or Hf corresponding to a doping of ~ 4.8 %
  I will report the lower doping results (more similar to the doping we can achieve experimentally with Zr). In any case, conclusions for the higher doping are the same.
Models have been quenched from ~1000 K to 300 K in ~ 100 ps
Structural and electronic properties have been analyzed separately for Zr and Hf-doped GST

## Slide 3: Zr doped GST: structural properties
Distribution of the coordination numbers for the different species have been computed
Zr atoms are mostly coordinated with Te.
  Also wrong Ge-Ge, Ge-Sb and Sb-Sb bonds, as in pure GST, are detected
  CN of Zr is 7-8 resembling the local bonding geometry in crystalline ZrTe3 and ZrTe

## Slide 4: Zr doped GST: structural properties
Structure of crystalline ZrTe3, whereas each Zr atom is coordinated by six Te atoms
Zr atoms in the GST matrix resemble the bonding geometry of ZrTe3 with coordination 7-8 and similar bonding angles
ZrTe3 crystalline structure

## Slide 5: Zr doped GST: electronic properties
The electronic DoS of the Zr-doped GST and the pure GST are almost overlapped
Although the local bonding configuration of the metal atoms are different, no pronounced effect in the electronic properties, defects,…
Inverse participation ratio (IPR) captures the localization of electronic states
  Edge sharing tetrahedra around Ge atoms
  Empty d-orbitals of Zr atoms

## Slide 6: Zr doped GST: electronic properties
Projected Electronic Dos on the different species and orbitals types

## Slide 7: Zr doped GST: electronic properties
Tauc plot for optical band gap
Little effect by the Zr presence on the optical Band gap. Differences are within the fluctuations we expect among different models (due to size effects) and incomplete relaxation of the amorphous phase.

## Slide 8: Same analysis for Hf-doped GST

## Slide 9: Hf doped GST: structural properties
Distribution of the coordination numbers for the different species have been computed
Hf atoms are mostly coordinated with Te.
  Also wrong Ge-Ge, Ge-Sb and Sb-Sb bonds, as in pure GST, are detected
  CN of Hf is 6-7-8 resembling the local bonding geometry in crystalline HfTex (see also slide #3)

## Slide 10: Hf doped GST: electronic properties
The electronic DoS of the Hf-doped GST and the pure GST are almost overlapped
Although the local bonding configuration of the metal atoms are different, no pronounced effect in the electronic properties, defects,… as for Zr-GST
In gap states with high IPR are due to wrong bonds (Sb-Sb and Sb-Ge)

## Slide 11: Hf doped GST: electronic properties
Projected Electronic Dos on the different species and orbitals types

## Slide 12: Hf doped GST: electronic properties
Tauc plot for optical band gap
Tauc plot of Hf-doped GST essentially equal to that of pure GST

## Slide 13: Zr/Hf doping effects on the ring length statistics
distributions of closed loops
The idea:
Many four- and six-fold rings in a-GST act as nuclei for crystallization. The large fraction of crystalline nuclei in a-GST (>40% of `embryo nucleation') is the origin of the `nucleation-driven' crystallization in GST. In a-GST, dominant small-sized rings with chemical alternation (`ABAB squares', A, Sb or Ge; B, Te) act as nuclei for crystallization.
Nat. Mat., 10, p. 129 (2011)

## Slide 14: Conclusions
Both Zr and Hf bond essentially with Te atoms
They give rise to bonding geometry with coordination number 6-7-8, resembling the local bonding of the crystalline ZrTex and HfTex
No strong effects in the electronic properties:
  Band gap remains almost unaltered
  These metals do not introduce filled defect states in the gap
The presence of Zr/Hf dopants slightly decreases the 4-fold rings statistics
No strong effect benefit of Zr/Hf-doped GST can be extrapolated from these results proposition, but neither strong drawbacks
It could happen to get improved integrability  Thus, it’s worth to try