## Slide 1: XPS Core levels and valence band analysis of SD
Deeper insights on moisture and annealing effects in SD
Kent Zhuang, Swapnil and Paolo

## Slide 2: Experimental
Element | 1 | 2 | 3
As | 35.9 | 31.4 | 28.5
Se | 57.4 | 53.1 | 46.6
Ge | 0.0 | 9.0 | 19.0
Si | 6.6 | 6.5 | 5.9
3 SiSAG films have been analyzed thru XPS:
  One w/o Ge, the other two with ~9% (similar to our POR) and 19% Ge
35 nm SiSAG films were deposited on bare Si wafer and capped with 3 nm Carbon
Compositions 2 and 3 have been analyzed both after dep and after annealing at 280C for 30 min in vacuum
High resolution of C1s, O1s, Si2p, Ge3d/Ge2p3, As3d/As2p3 and Se3d core levels and the valence band spectra were acquired with two different at 45 and 85o take-off angles (TOAs)
45o TOA is more surface sensitive, while 85o TOA is more bulk sensitive

## Slide 3: Key results summary:
Carbon capped SiSAG SD film incorporates moisture
Annealing (280C for 30 min in vacuum) effects:
  likely converts As(OH)3 to As2O3 (evidenced from reduced Oxygen post anneal in the As 2p3/2 peak) and oxides Ge (Ge3d shift at higher BE)
  Moisture is partially released after annealing (evidenced from reduced O 1s peak intensity post anneal)
  Annealing shifts the valence band maximum toward higher binding energy, thereby widening the band gap which is consistent with independent optical measurements (see next slide)
As 2p3/2 core level
Sample | Film | Anneal
07 | ~As2Se3 | No
08 | 9% Ge, SiSAG | No
09 | 9% Ge, SiSAG | Yes
10 | 18% Ge, SiSAG | No
11 | 18% Ge, SiSAG | Yes
Shift at higher BE with annealing indicates more GeOx
O 1s core level
Ge 3d core level
As 2p3/2 core level allows identifying the presence of As2O3 or As(OH)3 in the film. Spurious peak at higher BE.
As 2p3/2 core level
Decrease of Ox peak w/ ann supports moisture loss
The retire of the VB is coherent w/ optical BG widening
Top of the VB
Doc link

## Slide 4: Link w/ independent optical characterizations
Eu decreases w/ ann temperature
Lot X985963.003
EG and Eu have a linear relationship for each material. Fit line gives the bandgap energy of the “perfect”/clean material (Eu = 0).
The highest energy state (A1) of the Electronic DoS of SAG is ascribed to Se LP
EG increases w/ ann temperature
By J. Hauck
A1
We could speculate that H+ ions bond with Se LP shifting up their energy and then narrowing the BG
As a consequence of annealing moisture release will lead to the retire of the top of the VB previously stretched by H+ ions accumulation
Top of the VB
Ab-initio simulations need to check this proposed model
Doc link

## Slide 5: Study of annealing effects
As2p3 core level
The chemical shift of the As2p3 binding energy as a consequence of oxidation allowed monitoring the oxidation levels of the films
The As oxidized core level component appears depressed as a consequence of the annealing process  Annealing likely converts As(OH)3 to As2O3 (evidenced from reduced Oxygen post anneal)
0% Ge – No Ann
9% Ge – No Ann
9% Ge – With Ann
19% Ge – With Ann
19% Ge – No Ann

## Slide 6: XPS Valence band spectra
Wafer ID | Film | Anneal
7353-07 | ~As2Se3 | No
7353-08 | 9% Ge, SiSeAsGe | No
7353-09 | 9% Ge, SiSeAsGe | Yes
7353-10 | 18% Ge, SiSeAsGe | No
7353-11 | 18% Ge, SiSeAsGe | Yes
Features of the valence band spectra are in good agreement with literature for the SAG system [R. Golovchak, J. Non-Cryst. Solid 357, 3454 (2011)]
  The Ge 4p and As 4p electronic states of the atoms participating in Ge–Ge, Ge–As and As–As bonding should contribute to the peak around ~3-4 eV, but it could be partially overlapped also with stronger Se 4p band (5-6eV) shifted towards lower binding energy because of decreased number of Se–Se bonds as per specific composition.
A shift at lower BE of the top of the valence band is observed as a consequence of the annealing process

## Slide 7: 3d Core level spectra
Se3d
As3d
Ge3d
Wafer ID | Film | Anneal
7353-07 | ~As2Se3 | No
7353-08 | 9% Ge, SiSeAsGe | No
7353-09 | 9% Ge, SiSeAsGe | Yes
7353-10 | 18% Ge, SiSeAsGe | No
7353-11 | 18% Ge, SiSeAsGe | Yes
Shifts to lower BE with higher Ge likely due to homo-polar Ge-Ge or “wrong” bond Ge-As formation
Shift to lower BE for the higher Ge film due to “wrong” bond formation (As, Ge)-As-(Ge, As) *
Topology and chemical order in AsxGexSe1−2x glasses: A high-resolution X-ray
photoelectron spectroscopy study
R. Golovchak a,b, O. Shpotyuk c, M. Iovu d, A. Kovalskiy a, H. Jain a
*