## Slide 1: Hf-GST campaign
Check-point
30S Material Pathfinding Team

## Slide 2: Split table and score card
Main messages:
  Hf-GST tends to lower VT
  Hf-GST does not degrade the set-speed
  These messages are substantially coherent with theoretical prediction [link]

## Slide 3: VT and Optical band gap correlation
VT and optical band gap correlates:
  We need alloy with EG ~ 30 meV > EG of PM2.A3 to allow PM scalability coherently with link
30s goal
DEG
Hf 6-9%
Hf 3%
PM2.A3

## Slide 4: I-V curves for VT extraction
First Fire
1 Kcycles
POR
POR
POR
Fresh – used for VT extraction
PM2A.3 (POR) presents the higher VT
3%Hf-GST + N2 is also aligned with POR, but it appears a consequence of N2, since the same alloy w/o N2 presents very low VT (olive curve)

## Slide 5: Set to Reset/Set speed
Any particular speed issue, again accordingly with theoretical expectations [link]

## Slide 6: Programming curves after cycling