## Slide 1: Camp J* proposal
Swapnil Lengade, Dan Gealy
Fab 4

## Slide 2: Camp J* Proposal
Constraints
  High In leads to high leakage
    Cap In content at 11.2% (from Agrate’s SD kappa campaign)
  Co-ordination number
    Lower limit at 2.62 (assuming In as tri-valent co-ordination)
    Upper limit at 2.75 (for the As2Se3 based SAG systems, Vt drift dependency on Ge content makes splits with higher Ge content electrically not viable)

## Slide 3: Camp J* L0 proposal
CN<2.62
In>11.2%
CN>2.75
Recipe | In(at.%) | Ge (at.%) | As (at.%) | Se (at.%) | Si (at.%) | Ge+In
SDkappa.A005 | 11.1 | 13 | 21.8 | 53 | 1.1 | 24.1

## Slide 4: Campaign J* L0 proposal
Alloy | targets |  |  | Film |  |  |  |  |  |  |  | 
 | In2Se3 | Ge | As2Se3 | Ge | As | Se | Si | In | As+In | As+Se | CN | As/Se
1 | 0 | 18 | 82 | 18.0 | 32.8 | 49.2 | 0.0 | 0.0 | 32.8 | 82.0 | 2.69 | 0.67
2 | 5 | 18 | 77 | 18.0 | 30.8 | 49.2 | 0.0 | 2.0 | 32.8 | 80.0 | 2.69 | 0.63
3 | 10 | 18 | 72 | 18.0 | 28.8 | 49.2 | 0.0 | 4.0 | 32.8 | 78.0 | 2.69 | 0.59
4 | 15 | 18 | 67 | 18.0 | 26.8 | 49.2 | 0.0 | 6.0 | 32.8 | 76.0 | 2.69 | 0.54
5 | 20 | 18 | 62 | 18.0 | 24.8 | 49.2 | 0.0 | 8.0 | 32.8 | 74.0 | 2.69 | 0.50
6 | 25 | 18 | 57 | 18.0 | 22.8 | 49.2 | 0.0 | 10.0 | 32.8 | 72.0 | 2.69 | 0.46
7 | 20 | 16 | 64 | 16.0 | 25.6 | 50.4 | 0.0 | 8.0 | 33.6 | 76.0 | 2.66 | 0.51
8* | 28 | 14 | 58 | 14.0 | 23.2 | 51.6 | 0.0 | 11.2 | 34.4 | 74.8 | 2.62 | 0.45
9 | 15 | 14 | 71 | 14.0 | 28.4 | 51.6 | 0.0 | 6.0 | 34.4 | 80.0 | 2.62 | 0.55
10 | 10 | 20 | 70 | 20.0 | 28.0 | 48.0 | 0.0 | 4.0 | 32.0 | 76.0 | 2.72 | 0.58
11 | 15 | 20 | 65 | 20.0 | 26.0 | 48.0 | 0.0 | 6.0 | 32.0 | 74.0 | 2.72 | 0.54
12 | 15 | 16 | 69 | 16.0 | 27.6 | 50.4 | 0.0 | 6.0 | 33.6 | 78.0 | 2.66 | 0.55
13 | 15 | 22 | 63 | 22.0 | 25.2 | 46.8 | 0.0 | 6.0 | 31.2 | 72.0 | 2.75 | 0.54
* SD kappa A005-like
Recipe | In(at.%) | Ge (at.%) | As (at.%) | Se (at.%) | Si (at.%) | Ge+In
SDkappa.A005 | 11.1 | 13 | 21.8 | 53 | 1.1 | 24.1

## Slide 5
CN=2.61 safe for wrinkle 300C
EVARESI

## Slide 6
EVARESI

## Slide 7
B5
B2
B3
EVARESI

## Slide 8
EVARESI

## Slide 9: Campaign J* new proposal
Chart: 
| 0 | 57.735026918962497 | 115.47005383792499 | 0
 | 0 | 100 | 0 | 0
 | 0 | 91
 | 0 | 81
 | 0 | 71
 | 0 | 61
 | 0 | 51
 | 0 | 41
 | 0 | 31
 | 0 | 21
 | 0 | 11
 | 10 | 10
 | 20 | 20
CN<2.61
In>11.2%
CN>2.74
Incorporating Enrico and Paolo’s proposal

## Slide 10: Modified Campaign J* L0 proposal
Alloy | targets |  |  | Film |  |  |  |  |  |  |  | 
 | In2Se3 | Ge | As2Se3 | Ge | As | Se | Si | In | As+In | As+Se | CN | As/Se
1 | 0 | 18 | 82 | 18.0 | 32.8 | 49.2 | 0.0 | 0.0 | 32.8 | 82.0 | 2.69 | 0.67
2 | 7.5 | 18 | 74.5 | 18.0 | 29.8 | 49.2 | 0.0 | 3.0 | 32.8 | 79.0 | 2.69 | 0.61
3 | 15 | 18 | 67 | 18.0 | 26.8 | 49.2 | 0.0 | 6.0 | 32.8 | 76.0 | 2.69 | 0.54
4 | 22.5 | 18 | 59.5 | 18.0 | 23.8 | 49.2 | 0.0 | 9.0 | 32.8 | 73.0 | 2.69 | 0.48
5 | 28 | 18 | 54 | 18.0 | 21.6 | 49.2 | 0.0 | 11.2 | 32.8 | 70.8 | 2.69 | 0.44
6* | 28 | 13 | 59 | 13.0 | 23.6 | 52.2 | 0.0 | 11.2 | 34.8 | 75.8 | 2.61 | 0.45
7 | 22.5 | 15.5 | 62 | 15.5 | 24.8 | 50.7 | 0.0 | 9.0 | 33.8 | 75.5 | 2.65 | 0.49
8 | 15 | 15.5 | 69.5 | 15.5 | 27.8 | 50.7 | 0.0 | 6.0 | 33.8 | 78.5 | 2.65 | 0.55
9 | 15 | 21 | 64 | 21.0 | 25.6 | 47.4 | 0.0 | 6.0 | 31.6 | 73.0 | 2.74 | 0.54
10 | 22.5 | 13 | 64.5 | 13.0 | 25.8 | 52.2 | 0.0 | 9.0 | 34.8 | 78.0 | 2.61 | 0.49
11 | 15 | 13 | 72 | 13.0 | 28.8 | 52.2 | 0.0 | 6.0 | 34.8 | 81.0 | 2.61 | 0.55
12 | 7.5 | 13 | 79.5 | 13.0 | 31.8 | 52.2 | 0.0 | 3.0 | 34.8 | 84.0 | 2.61 | 0.61
* SD kappa A005-like
Recipe | In(at.%) | Ge (at.%) | As (at.%) | Se (at.%) | Si (at.%) | Ge+In
SDkappa.A005 | 11.1 | 13 | 21.8 | 53 | 1.1 | 24.1

## Slide 11: L0 data

## Slide 12: Camp J ICP composition data table

## Slide 13: Pseudo-ternary
Lowest In content in the film, achievable, was ~4.4%
Besides the low In splits, the other compositions were pretty close to the desired values

## Slide 14: Optical Bandgap, Eg
Eg shows dependance on Se, Ge content of the film and on the film CN.

## Slide 15: Optical Bandgap, Eg
Eg does not show any correlation to the In content
Effect of In on SAG – from the Kappa camp run in F14

## Slide 16: Raman spectra
Currently working on peak de-convolution and understanding the impact of In on the structural arrangement of the In-SAG

## Slide 17: SEM Wrinkle test
wafer | As | Ge | In | Se | Si | As/Se | As+Se | CN | Sepoor/rich | 270 | 280 | 290 | 300 | 310 | 320 | 330 | 340 | 350 | 360 | 370
1 | 32.4 | 17.7 | 0.0 | 50.0 |  | 0.648 | 82.3 | 2.68 | -33.9 |  |  |  |  |  |  |  |  |  |  | 
2 | 28.1 | 18.2 | 4.4 | 49.3 |  | 0.571 | 77.5 | 2.69 | -35.8 |  |  |  |  |  |  |  |  |  |  | 
3 | 27.0 | 17.8 | 5.7 | 49.4 |  | 0.547 | 76.4 | 2.68 | -35.4 |  |  |  |  |  |  |  |  |  |  | 
4 | 23.9 | 18.1 | 8.9 | 49.2 |  | 0.485 | 73.1 | 2.69 | -36.1 |  |  |  |  |  |  |  |  |  |  | 
5 | 22.2 | 17.7 | 10.6 | 49.5 |  | 0.450 | 71.7 | 2.68 | -35.2 |  |  |  |  |  |  |  |  |  |  | 
6 | 24.4 | 13.1 | 10.4 | 52.0 |  | 0.470 | 76.5 | 2.61 | -26.5 |  |  |  |  |  |  |  |  |  |  | 
7 | 25.6 | 13.0 | 9.3 | 52.1 |  | 0.491 | 77.7 | 2.61 | -26.1 |  |  |  |  |  |  |  |  |  |  | 
8 | 28.8 | 13.1 | 5.7 | 52.4 |  | 0.551 | 81.2 | 2.61 | -25.6 |  |  |  |  |  |  |  |  |  |  | 
9 | 30.0 | 13.1 | 4.4 | 52.5 |  | 0.571 | 82.5 | 2.61 | -25.2 |  |  |  |  |  |  |  |  |  |  | 
10 | 25.7 | 21.4 | 5.4 | 47.4 |  | 0.543 | 73.1 | 2.74 | -42.2 |  |  |  |  |  |  |  |  |  |  | 
11 | 28.2 | 15.4 | 5.4 | 51.0 |  | 0.553 | 79.2 | 2.64 | -30.3 |  |  |  |  |  |  |  |  |  |  | 
12 | 25.1 | 15.2 | 8.9 | 50.9 |  | 0.493 | 75.9 | 2.64 | -30.4 |  |  |  |  |  |  |  |  |  |  | 
All the 18 at% Ge splits did ok at 300C.
For the 13 at% Ge splits, the highest In split was marginal, all the other splits did not survive
The 15 at% Ge splits with ~6 and 9% In were marginal at 300C
Repeating the Group 7 wafer because of questionable sequence of annealing /SEM

## Slide 18
G1
G2
G3
G4
G5
G6
G7
SEM WRINKLE

## Slide 19: SEM Wrinkle
G8
G9
G10
G11
G12
SDv13

## Slide 20: Summary so far…
Eg shows a dependence on the Ge and Se content of the film but not on the In
  So In may not likely affect Vt /drift
Based on the SEM wrinkle data, 9 out of the original 12 splits survived the 300C anneal
All the surviving splits have Ge >15.0 at% except the one with Ge 13%, In 10.4%
  To get a better picture, we will collect L0 and L1 data on some splits in the (11% < In < 20%) region with (10% < Ge < 13%)
Deciphering the Raman data
Waiting on XRD at 300C to especially check if the higher In can induce some crystallinity

## Slide 21
Suitable area of further interest
Eg
Thermal stability
(300C)
No wrinkle
wrinkle
v13 level
Enrico/ Paolo