## Slide 1: Collaboration with Prof. Matthias Wuttig RWTH (Aachen University)
Competitive advantage in building a material roadmap
Aachen and Micron

## Slide 2: PM fundamentals
Fast crystallization (main factors):
  Cubic structure embryos present in amorphous
  High fragility (high diffusivity above Tg)
Amorphous low conductivity & switching threshold field
  Relatively strong localized bonds
  Dangling bonds/lone pairs
PM structure
Strong, localized
Floppy, resonant
bonding
Intrinsic speed-window trade-off
Looking for EOL composition (and doping) to optimize and tune the trade-off
SPEED
WINDOW

## Slide 3: Problem statement: The VT window vs. set-speed dilemma
DVT [mV]
Time for crystallization in sigma
The larger is the PM VT window, the slower is the SET process
Is this a fundamental physics barrier?
…let’s say: the stronger are the bonds and the higher is the glass rigidity and then the inertia to crystallize and higher is the EG, thus the VT?
Goal
The Goal for 30S scaling is finding a PM material offering high VT window without slowing down the crystallization speed necessary to have a high-throuput memory technology
The ability to handle this correlation is fundamental for SxP technology scaling: How can we tailor materials with high VT preserving a very good SET speed?

## Slide 4: Kick-off meeting summary
Map speed-Vth related parameters (on different alloys with corner properties)
  Speed (nucl.rate, crystal. rate, fragility, 4-ring structure, …)
  Vth (Eg, strong bonding, dangling bonds, long-pairs, avalance factor, …)
Evaluate structural/physical feature of mapped alloys to identify aspects which enable better trade-off (connections with ab-initio and structure (Raman-EXAFS) data)
Kick-off meeting for the collaboration has been held on June 1st Update phone-call meeting will be held every 6 wks
‘Italy flipped boot’ strategy
We will start plotting some fundamental quantities related to SET speed vs other related to the band-gap (and then the VT) for the strategies #2 (GST matrix) and #4 (GeTe-GeSe)

## Slide 5
Metrics
 | speed | Vth | 
measured | Crystall speed (DSC, fDSC) | Eg (optical) | 
 | Crystall speed (optical) | amorphous resistance | 
 | Nucl. rate (TEM) | Vth (CLV) | 
 | Growth rate (TEM) |  | 
 | Fragility (DSC, fDSC) |  | 
 | Tm, Tx (DSC) |  | 
Calculated/ extracted |  | Electronic localization | 
 |  | Born effective charge | 
 |  | ionicity | 
 |  | Peierls distorsion | 

## Slide 6: Strategy
Blending of two different PM: one slow with high VT with a second one fast with low VT
We should get a first glance on data for these systems at the next meeting (within July)
We should get also a ‘feeling’ about the promise of this system that Wutting is investigating for different purposes
Known high speed enabling:
  Ag, Ti, Sn, Bi, W
Known high resistance enabling:
  Se, Si, H, In

## Slide 9: Eg optical measurement