## Slide 1: Atomistic insights on the In-SAG system
Results from the collaboration with Prof. Marco Bernasconi – Milano Bicocca University – Report link
30S Material Pathfinding team

## Slide 2: Summary
Two 500-atom models of In10Ge13As29Se48 have been simulated:
  One with longer quenching time from melting, corresponding to the more stable material
  One with shorter quenching time from melting, corresponding to the unstable material that will tend to relax
Indium atoms are mostly in the stable tetrahedral configuration (4-fold coordinated) – as Si atoms in the Si-SAG system – more detailed comparison still running on
No localized states related to In are present at the band edges
Thus, the substitution of Ge by In leads to an overall decrease of Ge atoms in pyramidal and defective octahedral configurations responsible for drift
The substitution of Ge by In should be beneficial for the VT drift mitigation

## Slide 3: Distribution of the coordination numbers
FAST vs slow quench
FAST QUENCH
SLOW QUENCH
Indium atoms are in the stable 4-folded coordination still after the fast quench.
At variance Ge atoms are both in the unstable 3-fold configuration and in the stable 4-fold coordination.
Higher % of Ge in the unstable 3-fold coordination after fast quench is observed.
They partially relax in the more stable tetrahedral coordination with the slow quench, causing drift.

## Slide 4: Electronic Density of States (DoS)
FAST vs Slow quench
No localized states related to In, that might contribute to the drift, are present at the band edges nor in the gap.
What is responsible for the enhanced Poole-Frenkel conduction we observed in CLV?
- We are asking to Prof. Bernasconi an analytical comparison of the electronic features of In-SAG wrt similar compositions of Si-SAG and SAG systems.

## Slide 5: Relaxation of the Optical Bandgap
The optical bandgap widening of the relaxed amorphous network is still related to the Ge transition from 3-fold to 4-fold coordination
A more detailed comparison of the Tauc gap and slope with the similar Si-SAG and SAG system is needed to better understand the peculiarity of In-SAG
Tauc plot for the Relaxed (slow quench) and Un-Relaxed (fast quench) In-SAG