## Slide 1: In-doped SAG camp K*
See the notes on the left margin of many of these slides for instructions on their use.

## Slide 2: comments
Ge, Si, In are considered to form XSe4 tetrahedral clusters
X=Ge+Si+In=cost is an interesting metric to evaluate possible differences and to verify if they are equivalent to build the tetrahedral network component and to confirm Ge amount as the main driver for drift (Ge, among the three, is considered to form also other local structures (pyramids, defective octahedral, chain) whose instability is considered responsible for drift).

## Slide 3
 | A | B | C | note
Ge-Si skew (In=0) | Si=0,4,7 XSe4=19(SDv12) CN=2.70 |  |  | Si for Ge
Ge-Si skew (In=5%) | Si=0,4,7 XSe4=19 CN=2.67 | Si=0,3,5,7 XSe4=22 CN=2.72 | Si=0,3,5,7 XSe4=21 CN=2.71 | Si for Ge
In-Ge skew (no Si) | In=0,2,5 XSe4=24.6 CN=2.76-2.79(SD1) | In=0,2,5 Ge=17 CN=2.69-2.72 | In=0,2,5 XSe4=21 CN=2.74-2.71 | A,C: In for Ge B: In addition
Ge skew (no In,Si) | Si=0 Ge=19, 24.6(SD1) CN=2.70-2.79(SD1) | Si=0 Ge=17,21,25(SD1) CN=2.67-2.8(SD1) | Si=0 Ge=17,21,25(SD1) CN=2.67-2.8(SD1) | Ge addition
Ge skew (no In) | Si=5 Ge=14, 20 CN=2.67-2.76 |  |  | Ge addition
Skew directions:

## Slide 5
Ge-Si skew (In=0)
Ge-Si skew (In=5%)
In skew (no Si)
Ge skew
SD1
SDv12
SD1
SDv12
SD1
SDv12
A
B
C
Fixed Ge
Fixed XSe4

## Slide 6
SD1
SDv12
SD1
SDv12
SD1
SDv12
Ge-Si skew (In=0)
Ge-Si skew (In=5%)
In skew (no Si)
Ge skew (no In, no Si)