## Slide 1: SD Camp K* - InSiSeAsGe
Swapnil Lengade, Paolo Fantini, Enrico Varesi, Dan Gealy

## Slide 2: Camp K* - InSiSeAsGe (InSiSAG)
Motivation
  The primary motivation for adding In to the SAG (Camp J*) was CLV data on Camp Kappa from Agrate which showed almost “0” forming, “0” drift behavior
    The downside was ~10x higher leakage compared to SiSAG
  Camp K* is an extension of Camp J* where we want to investigate In addition into SiSAG. The idea is to mitigate the higher leakage seen on In-SAG with the addition of Si to the film
Goal
  Achieve low drift, low forming, acceptable leakage SD that meets the PG1 DTS spec

## Slide 3: Looking for 200 mV memory spec: WLR-like CLV data
Normalized IVs @ 1E3cyc
Indium addition
Se% | As% | Si% | Ge% | In%
53.0 | 21.8 | 1.1 | 13.0 | 11.1
> x10 higher leakage
Summary:
CLV and L3 data on A3* camp match
CLV data of lambda indicate the possibility to improve drift with F* (since we reduce Ge% in the ‘well tempered’ including Si)
The In-SAG composition shows the possibility to get the Memory spec
SD-k A005 ScoreCard
Strengths of SD-k: Forming ~0, lowest Drift, Low spread
Weakness of SD-k: Leakage
Courtesy: PFANTINI

## Slide 4: Camp K* - InSiSeAsGe
Methodology
  Experiment
    Grp IV skew from 13 to 18%
      Ge from 6.0 to 8.0%
      Si from 7.0 to 9.0%
    In skew from 6 to 13%
  L0 data collection
  L1 CLV assessment
  L1D based on CLV results
  L3 based on L1D results
Ge | As | Se | Si | In
6.0 | 34.7 | 52.1 | 7.2 | 0.0
6.0 | 27.2 | 53.6 | 7.2 | 6.0
6.0 | 24.8 | 53.1 | 7.1 | 9.0
6.0 | 23.1 | 52.8 | 7.1 | 11.0
6.0 | 21.6 | 52.4 | 7.0 | 13.0
7.0 | 26.5 | 52.3 | 8.2 | 6.0
7.0 | 24.1 | 51.8 | 8.1 | 9.0
7.0 | 22.5 | 51.4 | 8.1 | 11.0
7.0 | 20.8 | 51.2 | 8.0 | 13.0
8.0 | 25.7 | 50.9 | 9.4 | 6.0
7.9 | 23.4 | 50.5 | 9.2 | 9.0
8.0 | 21.7 | 50.1 | 9.2 | 11.0
7.9 | 20.1 | 50.0 | 9.0 | 13.0

## Slide 5: Camp K* deposition specifics
Camp K* runs on MMUM4C0300 F1 3C chamber (stage @75C)
Targets
  Gun1: As2Se3, Rf
  Gun2: SiGe, Rf
  Gun3: In2Se3, Rf
Ran a 5-pt DOE to define a process space (As2Se3 gun1 fixed at 150W)
SiGe / In2Se3 | 30W | 90W | 150W
75W | x |  | x
125W |  | x | 
175W | x |  | x

## Slide 6: Si0.5Ge0.5 composition not exactly 50-50
The Rf power matrix on SiGe only and the 5pt DOE composition data indicate that…

## Slide 7: Camp K* 13-way skew
 |  |  | Predicted based on 5pt DOE |  |  |  |  | Actual |  |  |  | 
As2Se3 Rf | SiGe Rf | In2Se3 Rf | Ge | As | Se | Si | In | Ge | As | Se | Si | In
150W | 115W | 0W | 6.0 | 34.7 | 52.1 | 7.2 | 0.0 | 7.1 | 32.4 | 52.4 | 8.2 | 0.0
150W | 108W | 34W | 6.0 | 27.2 | 53.6 | 7.2 | 6.0 | 5.9 | 27.9 | 53.2 | 7.1 | 5.9
150W | 127W | 68W | 6.0 | 24.8 | 53.1 | 7.1 | 9.0 | 6.1 | 24.6 | 52.3 | 7.4 | 9.5
150W | 133W | 90W | 6.0 | 23.1 | 52.8 | 7.1 | 11.0 | 6.0 | 24.1 | 52.3 | 7.0 | 10.5
150W | 140W | 110W | 6.0 | 21.6 | 52.4 | 7.0 | 13.0 | 6.2 | 22.6 | 52.3 | 7.0 | 11.9
150W | 124W | 35W | 7.0 | 26.5 | 52.3 | 8.2 | 6.0 | 6.9 | 26.8 | 51.5 | 8.3 | 6.5
150W | 147W | 69W | 7.0 | 24.1 | 51.8 | 8.1 | 9.0 | 7.2 | 24.2 | 51.1 | 8.3 | 9.3
150W | 153W | 92W | 7.0 | 22.5 | 51.4 | 8.1 | 11.0 | 7.2 | 23.4 | 50.8 | 8.1 | 10.6
150W | 160W | 110W | 7.0 | 20.8 | 51.2 | 8.0 | 13.0 | 7.2 | 22.2 | 50.6 | 8.2 | 11.7
150W | 145W | 33W | 8.0 | 25.7 | 50.9 | 9.4 | 6.0 | 8.4 | 26.0 | 50.0 | 9.5 | 6.0
150W | 167W | 70W | 7.9 | 23.4 | 50.5 | 9.2 | 9.0 | 8.4 | 23.3 | 49.6 | 9.7 | 9.1
150W | 175W | 92W | 8.0 | 21.7 | 50.1 | 9.2 | 11.0 | 8.4 | 22.5 | 49.3 | 9.4 | 10.4
150W | 180W | 110W | 7.9 | 20.1 | 50.0 | 9.0 | 13.0 | 8.4 | 21.5 | 49.4 | 9.4 | 11.3

## Slide 8: Camp K* split ternary – predicted vs. actual ICP data

## Slide 9: Camp K* proposed split table for L1
Split 1 will be changed to get a thermally stable alloy (~8% Ge)
Detailed split table on the next slide

## Slide 10: Camp K* proposed split table - detailed
The alloys agreed upon for L1 are highlighted in the last column
L0 data will be collected on these alloys in addition to some high In alloys

## Slide 11: Camp K L1 split table
3x2 matrix on Ge x In with an added alloy K015 (F on the ternary plot)
Disclaimer: these set of alloys are likely going to be thermally unstable based on Camp J*.

## Slide 12: SWR7713604 - SD CAMP K L1

## Slide 13: Extended L0
Collected L0 data on the above table of compositions
This has 3 more alloys (the last 3) in addition to the ones that ran on L1
  These alloys have higher (>12.5%) In in them
Split | As2Se3 Rf | SiGe Rf | In2Se3 Rf | Alloys
2 | 150W | 108W | 34W | K002
4 | 150W | 133W | 90W | K004
6 | 150W | 124W | 35W | K006
8 | 150W | 153W | 92W | K008
14 | 150W | 90W | 34W | K014
15 | 150W | 107W | 68W | K015
16 | 150W | 113W | 90W | K016
18 | 150W | 147W | 130W | K018
19 | 150W | 154W | 150W | K019
21 | 150W | 134W | 150W | K021

## Slide 14: ICP data
Split | Alloys | ICP Ge | ICP As | ICP Se | ICP Si | ICP In | As+In | Grp IV | As+Se | CN (In=3) | CN (In=4) | As/Se | delta Se
2 | K002 | 5.9 | 27.9 | 53.2 | 7.1 | 5.9 | 33.8 | 13.0 | 81.1 | 2.598 | 2.657 | 0.524 | -23.5
4 | K004 | 6.0 | 24.1 | 52.3 | 7.0 | 10.5 | 34.6 | 13.0 | 76.4 | 2.604 | 2.709 | 0.461 | -25.5
6 | K006 | 6.9 | 26.8 | 51.5 | 8.3 | 6.5 | 33.3 | 15.2 | 78.3 | 2.637 | 2.702 | 0.520 | -28.9
8 | K008 | 7.2 | 23.4 | 50.8 | 8.1 | 10.6 | 34.0 | 15.3 | 74.2 | 2.648 | 2.754 | 0.461 | -30.9
14 | K014 | 5.2 | 27.9 | 54.1 | 6.3 | 6.4 | 34.3 | 11.5 | 82.0 | 2.571 | 2.635 | 0.516 | -20.3
15 | K015 | 5.2 | 25.3 | 53.4 | 6.3 | 9.7 | 35.0 | 11.5 | 78.7 | 2.578 | 2.675 | 0.474 | -22.0
16 | K016 | 5.2 | 24.7 | 53.2 | 6.1 | 10.8 | 35.5 | 11.3 | 77.9 | 2.581 | 2.689 | 0.464 | -22.7
18 | K018 | 6.4 | 21.0 | 52.5 | 7.2 | 12.8 | 33.8 | 13.6 | 73.5 | 2.611 | 2.740 | 0.400 | -25.5
19 | K019 | 6.4 | 19.6 | 52.3 | 7.1 | 14.6 | 34.2 | 13.5 | 71.9 | 2.612 | 2.758 | 0.375 | -26.0
21 | K021 | 5.3 | 20.4 | 53.1 | 6.2 | 15.1 | 35.5 | 11.5 | 73.4 | 2.584 | 2.735 | 0.383 | -23.0

## Slide 15: XRR Density & Optical Eg
For the current composition space, In content controls the film density
Eg shows a unilateral decrease with In content for up to 10% In (jives with the historically high leakage seen in In-SAG). At higher In, the picture is not so clear
  Need to get a re-fit of the Eg data since some of the samples showed higher std. dev.

## Slide 16: Optical Eg data fit quality is questionable for some samples
Alloys | OPTICAL EG MEAN | OPTICAL EG %RSD
K002 | 1.835 | 0.11
K004 | 1.765 | 3.83
K006 | 1.822 | 2.22
K008 | 1.743 | 3.57
K014 | 1.832 | 0.24
K015 | 1.788 | 3.45
K016 | 1.761 | 3.13
K018 | 1.892 | 12.56
K019 | 1.824 | 7.99
K021 | 1.800 | 2.85

## Slide 17: SEM Wrinkle test
Samples at the lab for anneals

## Slide 18: Raman Spectra

## Slide 19: XRF setup for InSiSAG
Samples at the lab