## Slide 1: Campaign K preliminary results
3297243 lot
See the notes on the left margin of many of these slides for instructions on their use.

## Slide 2: Split table/thermal stability/scorecard
NOTES:
Lot healthy is good very poor wf to wf variability and spread;
Spread seems more alloy related;
From TH stability only K004/6/8 satisfy the criteria, unfortunately these alloys are the one with very high spread;
Leakage, that was the critical electrical parameter to be controlled is not diverging with In content.

## Slide 3: FF/SF/Vth cycled
Good lot;
variability seems to be alloy related more than wf to wf variability  not clear why: K004/6/8 have been retested to conform these data on a complementary map  Hp: Is variability ascribed to the too high Si?

## Slide 4: Leakage
Leakage is not increasing with In concentrations
9.7% In
No In

## Slide 5: Short time drift
Up to 1 sec at RT, all alloys are stable for drift and no particular differences among alloys are detectable.
We will address the WLR drift char for K016 and v12 to enhance our data with this kind characterization.

## Slide 6: Subthtreshold IV
Thermally stable alloys present a very high spread. While pretty good variability is found for K014-K015 and K016 alloys having Si<7%, but they did not pass the thermal stability test.

## Slide 7: Retest data
After retest the spread is confirmed on K004/6/8 alloys.

## Slide 8: Conclusions
Recommendation and follow-up
In order to meet the thermal stability criterion avoiding to Si > 7% we suggest to change the target configuration:
As2Se3
In2Se3
Si3.5Ge6.5
SiGe
Lot healthy is good very poor wf to wf variability and spread;
Variability, when rises-up, is ascribed to alloy goodness;
On the basis of the past experience we ascribe the bad shape of K002/4/6/8 to the presence of Si > 7%  see recommendations
Alloy K014/15/16 that present controlled spread did not pass the thermal stability test
As2Se3
In2Se3
Actual config
Proposed config
Indeed ~Si60Ge40 on wf

## Slide 9: Possible scheduling
L0/L1 check point to assess the possible L3 promotion of some compositions

## Slide 10: Comments on thermal stability limit
Alloys | As-dep | 270C | 280C | 290C | 300C | 310C | 320C
v12 |  |  |  |  |  |  | 
A36 |  |  |  |  |  |  | 
Ge10 Si6 |  |  |  |  |  |  | 
Ge9.5 Si6 |  |  |  |  |  |  | 
Ge9.0 Si6 |  |  |  |  |  |  | 
This is the thermal stability picture of the lot 9742432.003 with low Ge skew that is going to probe:
We are now considering as thermal stability limit for new alloys that we are exploring: 290C yellow  these alloys, in fact, demonstrated good probe yield w/o issues
If the new lot 9742432.003 with low Ge skew would demonstrate good probe yield also for the alloys with the limit at 280C we propose to shift down at that level the thermal stability limit
Today limit
For In-SiSAG  CN ~2.66-2.68