## Slide 1
Scalin

## Slide 2: Thermal-Electrical
Category | Attributes | Problem Statement | Risk | Strategy | Next Step
Thermal-Electric | Isat, IRESET | 10% higher than DTS | 2.5 | Optimization at CR4 | Q4 plan
Thermal-Electric | Imelt | xx% lower than DTS | 1.5 | (initial segmentation) | Get data
Set-ability | τnuc | Improper DTS assumption (constant vs. 2X in time due to 50% of nuclei reduction)  +65nsec CD skew Si projection T0: 200ns vs. 80ns 4M:600ns vs. 130ns | 1.5 | Set scheme analysis for timing redistribution for risk management | 

## Slide 3: Set-ability
Category | Attributes | Problem Statement | Risk | Strategy | Next Step
Set-ability | τnuc | Improper DTS assumption (constant vs. 2X in time due to 50% of nuclei reduction)  +65nsec CD skew Si projection T0: 200ns vs. 80ns 4M:600ns vs. 130ns | 1.5 | Set scheme analysis for timing redistribution for risk management | 
Set-ability | τgro | expected no rate reduction (nm/ns) D0 is okay, D1 poor predictability | 2 | Make clean process for char | 
Set-ability | Inuc | Low bound doesn’t scale Upper bound requires recharx at proper cycle/τnuc | 1.5 |  | 
Set-ability | Igro | seems matching to thermal I2 | 2 | Solving thermal I2 first | 

## Slide 4: I-V
Category | Attributes | Problem Statement | Risk | Strategy | Next Step
I-V | Subthreshold | No data |  |  | 
I-V | Threshold point | No data |  |  | 
I-V | NDR | Constant J-V (not a problem) | 3 |  | 
I-V | Ihold | No scaling (in sufficient data) | 2 1.5 |  | 

## Slide 5: VT and ∆VT
Category | Attributes | Problem Statement | Risk | Strategy | Next Step
VT and ∆VT | Amorphization |  |  |  | 
VT and ∆VT | Memory Effects |  |  |  | 
VT and ∆VT |  |  |  |  | 
VT and ∆VT |  |  |  |  | 

## Slide 6: Parasitics
Category | Attributes | Problem Statement | Risk | Strategy | Next Step
WL | Resistance |  |  |  | 
WL | Capacitance |  |  |  | 
BL | Resistance |  |  |  | 
BL | Capacitance |  |  |  | 
Via | WSiN |  |  |  |