## Slide 1: NVL PX/MX Intercept
CPG/GEMS/FTE presenting
DerChang Kau
By courtesy of Team Electric Pond, Dany Ly-Gagnon, Mike Goldsmith, Jason Zhang and Long Wang
March 31, 2023

## Slide 2: System in Package Mockup: Inspired by PX Processer
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate (UCIe-S)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
i16 Si Interposer/MiM* (UCIe-A)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
Si Interposer / MiM / i3FV SLC
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
SLC
DTC
SLC
MCP
Packaging cost baseline $8~$10
Passive interposer
(FOV, 2.5D)
Active interposer for eLLC / SLC
(Active FOV, 2.5D)
Fanout Package w/ Embedded Chiplet (2.3D-BT2)
For $25 addition
$4~$6 packaging process adder
$20 256MB SRAM of N6, SF4 or N4P
1¢/µF optional DTC or ISC for PDN
For $25 addition:
$7~$8 packaging process adder
$10~$20 Interposer & MiM of P1227
For > $150 addition
$7~$8 packaging process adder
$150~$200 Interposer, MiM & 400MB SRAM of I3FV

## Slide 3: Base Die (Advanced Packaging) Technology: 2.5D (Si Interposer)  2.3D (Fan-out)
Capability
2.3D provides flexible low parasitic interconnect of heterogenous technology integrating features for performance augmentation with TTM advantage
Cost
2.5D degrades feature utilization efficiency hence higher cost ~420mm2 I3FV (~$150) vs. ~120mm2 N6 (~$20)
Silicon interposer (TSV + BEOL) is 20% higher ($2~$3) in cost of making than Fanout packaging (TMV + RDL)
Additional 2.3D cost reduction opportunities in development
Capacity of 2.3D Family
TSMC’s InFO-3D and SPIL’s FO-3D are under development (Intel’s ODI ZBB’d)
Maturity of 2.3D Family
(maturity and roadmap)
Topics under evaluation in 2.3D
D2D IP design and performance difference between 2.5D and 2.3D (UCIe and beyond), including R/W latency, IO, ESD, power/thermal and PDN
Explore unknowns in Chip-Package Interaction using "Electric Pond" for 2.3D integration flow flushing
CPU-PX
Si Interposer / MiM / SRAM
CPU-PX
SRAM
DTC

## Slide 4: Disaggregated SRAM
256MB System Level Cache organization
  8MB channel: 32 banks in 8 bank groups, 256KB/bank 64B ECC Full Duplex DQ @ 1.6MT/s, 0.2pJ/b 102 MB/s for read/write @ 3ns latency
  32 channels deliver max BW 6.6TB/s @ 10~11W
  "Electric Pond": 2MB channel in FO-3D package for SV
Choices of technology and die capacity
  64MB/die yields the best cost due to yield
Emb. SRAM is estimated < 3˚C (∆T) higher than top die
  Feasibility in reducing ∆T with 25µm-Pitch bump/underfill optimization and “thermal chimney” design / TFM development
  Early Engagement between suppliers and design team to achieve STCO before design start
256MB SRAM | N6 | SF4 | N4P
Density [MB/mm2] | 2.16 | 2.57 | 2.77
Footprint [mm2] | 118 | 100 | 92
4x 64MB/die | $19.79 | $20.27 | $21.65
2x 128MB/die | $20.85 | $21.89 | $22.75
1x 256MB/die | $23.54 | $25.30 | $25.35

## Slide 5: 2.3D BT2 Chip-Last Mockup Flow (SPIL/FO-3D, TSMC/InFO-3D)
Discrete CPU-PX DTC not shown)
GPU-PX
PCD-PX (HBI DTC not shown)
Bridge
Bridge
Emb. 64MB
Emb. 64MB
Emb. 64MB
Emb. 64MB
A
A’
2
3
3
4
5
6
2
2
2
1
1
7
64M SRAM
GPU-PX N3P
Bridge
A
A’
N6/N4P
DTC
DTC
CPU-PX N3P/N3X/N2
Power Delivery
Small chiplet embedded in 2.3D-BT2 package enables flexibilities for PDN optimization for parasitic insertion loss (I·R, di/dt·L) reduction and noise de-coupling by effective capacitor placement within proximity of consumption.
TSMC DTC and SF ISC are the high-density de-cap choices for CPU/GPU in scaling path.
PCD
DTC
PCD
DTC
GPU
Carrier Prep
Top Die Attachment
Em. Chiplets Attachment
SRAM
Bridge
Mold, RDL
RDL, Cu Pillar
C4
1
6
5
2
3
Micro Bumping
9 µm HBI
25µm µB
80µm C4
Top Carrier Bond,
Back Carrier Debond.
Bumping
CPU
4
IPD not shown
7
25µm
Bumping

## Slide 6: Backup

## Slide 7: NVL-PX
LPDDR PHY
LPDDR PHY
Mem Controller (D-Unit)
System Agent
P-Core
P-Core
P-Core
E-Core Cluster
IDI
IDI
LLC (L3$)
MLC (L2$)
MLC (L2$)
MLC (L2$)
MLC (L2$)
MIPI PHY
TBT PHY
PCIe PHY
UART
CTRL
CTRL
MS IOSF Fabric
HS IOSF Fabric (PSF)
CTRL
CTRL
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate (UCIe-S)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
Si Interposer / MiM / i3FV SLC
MiP
MiP
EU
EU
EU
EU
VDEC
Display
LLC (L3$)
L1$
L1$
L1$
L1$
Slice
EU
EU
EU
EU
L1$
L1$
L1$
L1$
LPDDR PHY
LPDDR PHY
Mem Controller (D-Unit)
System Agent
MiP
MiP
L4/SLC/MSC
Lowest-Cost State (MCP)
POR passive interposer (2.5D)
Active interposer for eLLC / SLC (2.5D)
Embedded Die interposer (2.3D-BT2)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
i16 Si Interposer/MiM* (UCIe-A)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
SLC
DTC
SLC
eLLC

## Slide 8: Electric Pond - Summary
Top Die
(Controller)
Power & test signals to bottom die
Embedded Die
(SRAM)
Controller
SRAM
RDL layer
Substrate
Power & test signals to top die
Drivers
Drivers
SRAM
MUX
SRAM
SRAM
SRAM
SRAM
SRAM
SRAM
SRAM
(*) preliminary
Electric Pond Testchip
  Technology: TSMC N6
  Memory density: 2.25 MB/mm2
  Databus width: 64B cache line
  Die-to-die link (data, cmd, red): 1272 pads @ 1.6GT/s
Package Assembly
  Technology: SPIL FO-EB (Fan-Out, Embedded Bridge)
  Face-to-Face integration between top die and embedded die
  Micro-bump pitch @ 25µm, 1.78K bumps per mm2 in HCP
  RDL layer: 1 layer for routing test signals & power
Test Chip KPI | Test Chip | 32x Scaling | Notes
Memory capacity | 2MB (1 channel x 2MB) | 64MB (8 channels x 8MB) | 32x increase: 8x independent channels 4x more memory per channel
Channel capacity | 2MB | 8MB | 
Memory density | 2.25 MB/mm2 | 2.25 MB/mm2 | 
IO drivers (die-to-die) | 1,272 | 10,176 | IO drivers scaling w/ # channels
RD Bandwidth WR Bandwidth | 102 GB/s 102 GB/s | 816 GB/s 816 GB/s | Scaling with # of channels
RD Latency WR Latency | 4.375 ns 2.5 ns | 4.375 ns 2.5 ns | Datapath propagation delay remains 1 clk up to ~8MB channel capacity
RD energy per bit* WR energy per bit* | 0.22 pJ/bit 0.20 pJ/bit | 0.30 pJ/bit 0.28 pJ/bit | Datapath energy scaling with channel capacity: [pJ/bit]
Test Chip KPI | Test Chip | 32x Scaling | Notes
Memory capacity | 2MB (1 channel x 2MB) | 64MB (8 channels x 8MB) | 32x increase: 8x independent channels 4x more memory per channel
Channel capacity | 2MB | 8MB | 
Memory density | 2.25 MB/mm2 | 2.25 MB/mm2 | 
IO drivers (die-to-die) | 1,272 | 10,176 | IO drivers scaling w/ # channels
RD Bandwidth WR Bandwidth | 102 GB/s 102 GB/s | 816 GB/s 816 GB/s | Scaling with # of channels
RD Latency WR Latency | 4.375 ns 2.5 ns | 4.375 ns 2.5 ns | Datapath propagation delay remains 1 clk up to ~8MB channel capacity
RD energy per bit* WR energy per bit* | 0.22 pJ/bit 0.20 pJ/bit | 0.30 pJ/bit 0.28 pJ/bit | 

## Slide 9: ∆T between Embedded SRAM & Top Die
Base Line and experiment explored
Base Line ∆T: Emb. SRAM is <3˚C higher than Top Die at Full BW
25µm pitch µBump process change
  Upto 40% ∆T reduction with thickness, CD and Underfill material change
Layout effects:
  Upto 60% ∆T reduction by deploying Thermal Chimney (µBump dummification, method under development)
  Lower SRAM density to 1.66MB/mm2 (~25%) reduce ∆T by 20%
Other Design impact
  ½ Transfer Rate, ½ ∆T whereas +20% ∆T with Half Duplex @ constant BW
  ∆T inversely correlated with channel capacity
µBump Pitchw | µBump thicknes | µBump CD | KµBump | KUnderFill | Adding TS PDN Via µBump | Adding Thermal Chimney | SRAM Density | I/O Duplex | Transfer Rate | Capacity
µm | µm | µm | W/°C·m | W/°C·m |  |  | MB/mm2 |  | MT/s | MB/ch
25 | 26 | 12 | 8.8 | 0.55 | No | No | 2.25 | Full | 1.6 | 8
 | 25 | 14 |  | 1.1 | Yes | Yes | 1.66 | Half | 0.8~3.2 | 2~16
0.7˚C ∆T (76% reduction) can be achieved with process change and dummification
Embedded SRAM Chiplet
µBump connect to top die
TSVs connect to Substrate
CDµB
tµB
PitchµB
Early Engagement with Suppliers and Customer to achieve STCO before Design Start

## Slide 10
Chart: ’24 Adv. Fanout Packaging by Suppliers
| µB Pitch [µm] | TMV Pitch [µm] | C4 Bump Pitch [µm] | RDL Pitch [µm] | Number of RDL layers | Number of Embedded Die | Module Sizes [x reticle] | Package Sizes [mm] square
SPIL | 4 | 1.8301 | 2 | 1.6781 | 2.5 | 3 | 4 | 4
ASE | 3.1926 | 1.8301 | 1.5406 | 0.67807 | 2 | 1.3333 | 3 | 4
JCET | 3.415 | 1.8301 | 1.5406 | 4 | 3.5 | 1.3333 | 3 | 3
Amkor | 3.1926 | 1.8301 | 1.5406 | 0.67807 | 2 | 1.3333 | 3 | 4
TSMC'22 | 3.6781 | 1.8301 | 1.8301 | 3.8625 | 2 | 0.33333 | 1 | 2.7364
3
2
100
9
4
4
50
6
16
8
4
2
160
80
40
20
160
80
80
2
1
3
75
6
40
40
8
Chart: SRAM Benchmark by Mainstream Logic
| Cell Size [µm^2] | $/64MB | 2R1W Energy [pJ/b] | SRAM Fmax [GHz] | Static Leakage [nW/b] | Iso Power Speed [Normalized]
Intel 3 | 2.8 | 1.2632 | 1.6704 | 3.37 | 1.3552 | 3.6726
N6 | 1.792 | 3.3508 | 3.7048 | 3.0912 | 3.4395 | 2
N5 | 3.574 | 3.1091 | 3.9304 | 2.8289 | 3.4053 | 3.165
N4P | 3.9828 | 3.1958 | 3.9304 | 3.173 | 3.3248 | 3.835
SF5 | 2.14 | 3.6344 | 3.41 | 2.4867 | 0.86551 | 1.9157
SF4 | 3.1 | 3.3108 | 3.926 | 2.6178 | 1.708 | 3.2767
0.0200
0.0233
0.0267
0.0300
9
6
3
0.07
0.06
0.05
0.04
0.75
1.25
1.0
0.5
0.75
1
1.25
1.2
1.1
1.0

## Slide 11: Disaggregated SRAM
256MB System Level Cache organization
  8MB channel: 32 banks in 8 bank groups, 256KB/bank 64B ECC Full Duplex DQ @ 1.6MT/s, 0.2pJ/b 102 MB/s for read/write @ 3ns latency
  32 channels deliver max BW 6.6TB/s @ 10~11W
  "Electric Pond": 2MB channel in FO-3D package for SV
Choices of technology and die capacity
  64MB/die yields the best cost due to yield
Emb. SRAM is estimated < 3˚C (∆T) higher than top die
  Feasibility in reducing ∆T with 25µm-Pitch bump/underfill optimization and “thermal chimney” design (dummification TFM) development
  Early Engagement between suppliers and design team to achieve STCO before design start
256MB SRAM | N6 | SF4 | N4P
Density [MB/mm2] | 2.16 | 2.57 | 2.77
Footprint [mm2] | 118 | 100 | 92
4x 64MB/die | $19.79 | $20.27 | $21.65
2x 128MB/die | $20.85 | $21.89 | $22.75
1x 256MB/die | $23.54 | $25.30 | $25.35
CDµB
tµB
PitchµB
Embedded SRAM Chiplet
25µm Pitch
µBump connect to top die
9µm Pitch
TSVs connect to Substrate