## Slide 1: NVL-PX by courtesy of Mike Goldsmith
LPDDR PHY
LPDDR PHY
Mem Controller (D-Unit)
System Agent
P-Core
P-Core
P-Core
E-Core Cluster
IDI
IDI
LLC (L3$)
MLC (L2$)
MLC (L2$)
MLC (L2$)
MLC (L2$)
MIPI PHY
TBT PHY
PCIe PHY
UART
CTRL
CTRL
MS IOSF Fabric
HS IOSF Fabric (PSF)
CTRL
CTRL
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate (UCIe-S)
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
i16 Si Interposer/MiM
CPU-PX
GPU-PX
PCD-P
LPDDR
LPDDR
Substrate
Si Interposer / MiM / i3FV SLC
MiP
MiP
EU
EU
EU
EU
VDEC
Display
LLC (L3$)
L1$
L1$
L1$
L1$
Slice
EU
EU
EU
EU
L1$
L1$
L1$
L1$
LPDDR PHY
LPDDR PHY
Mem Controller (D-Unit)
System Agent
MiP
MiP
L4/SLC/MSC

## Slide 2: 2.5D  2.3D
Cost advantages
420mm2 of I3FV vs. 100mm2 of N6 ($20)
Silicon interposer is 20% higher in cost of making than Fanout packaging
Capability and Limitation
Besides thermal, there are many unknow in physical constraint
CPU-PX
Si Interposer / MiM / SRAM
CPU-PX
SRAM
DTC

## Slide 3: ∆T between Embedded SRAM & Top Die
Base Line and experiment explored
Base Line ∆T: Emb. SRAM is 4.4˚C higher than Top Die at Full BW
25µm pitch µBump process change
  Upto 40% ∆T reduction with thickness, CD and Underfill material change
Layout effects:
  Upto 60% ∆T reduction by deploying Thermal Chimney (µBump dummification, method under development)
  Lower SRAM density to 1.66MB/mm2 (~25%) reduce ∆T by 20%
Other Design impact
  ½ Transfer Rate, ½ ∆T whereas +20% ∆T with Half Duplex @ constant BW
  ∆T inversely correlated with channel capacity
µBump Pitchw | µBump thicknes | µBump CD | KµBump | KUnderFill | Adding TS PDN Via µBump | Adding Thermal Chimney | SRAM Density | I/O Duplex | Transfer Rate | Capacity
µm | µm | µm | W/°C·m | W/°C·m |  |  | MB/mm2 |  | MT/s | MB/ch
25 | 26 | 12 | 8.8 | 0.55 | No | No | 2.25 | Full | 1.6 | 8
 | 25 | 14 |  | 1.1 | Yes | Yes | 1.66 | Half | 0.8~3.2 | 2~16
1.1˚C ∆T (76% reduction) can be achieved with process change and dummification
Embedded SRAM Chiplet
µBump connect to top die
TSVs connect to Substrate
CDµB
tµB
PitchµB
Early Engagement with Suppliers and Customer to achieve STCO before Design Start

## Slide 4: Embedded Features impede Effective Power Delivery
CPU-PX
Si Interposer / MiM / SRAM
CPU-PX
SRAM
DTC
design requirement vs. physical constraint
Yet another example of pathfinding engagement for product leadership
CPU-PX
SRAM
DTC
DTC
CPU-PX
SRAM
DTC
DTC
t

## Slide 5: NVL-PX with 256MB embedded SRAM
CPU-PX
Discrete DTC not shown)
Embedded 256MB
GPU-PX
PCD-PX
(HBI DTC not Shown)
Bridge
Bridge
CPU-PX
Discrete DTC not shown)
Emb. 128MB
GPU-PX
PCD-PX
Bridge
Bridge
Emb. 128MB
CPU-PX
Discrete DTC not shown)
GPU-PX
PCD-PX
Bridge
Bridge
Emb. 64MB
Emb. 64MB
Emb. 64MB
Emb. 64MB
10mm
17.5mm
10.5mm
5.25mm
9.84~
10.91mm
4.87mm
5.46mm
9.75mm

## Slide 6: 2.3D BT2 Chip-Last Mockup Flow (SPIL/FO-3D, TSMC/InFO-3D)
Discrete CPU-PX DTC not shown)
GPU-PX
PCD-PX (HBI DTC not shown)
Bridge
Bridge
Emb. 64MB
Emb. 64MB
Emb. 64MB
Emb. 64MB
A
A’
2
3
3
4
5
6
2
2
2
1
1
7
PCD
DTC
PCD
DTC
GPU
Carrier Prep
Top Die Attachment
Em. Chiplets Attachment
SRAM
Bridge
Mold, RDL
RDL, Cu Pillar
C4
1
6
5
2
3
Micro Bumping
9 µm HBI
25µm µB
80µm C4
Top Carrier Bond,
Back Carrier Debond.
Bumping
CPU
4
IPD not shown
7
64M SRAM
GPU-PX I18A
Bridge
A
A’
N6/N4P
DTC
DTC
CPU-PX N3P

## Slide 7: Is 2.3D BT2 superior?
2.5D Foveros
  Si interposer with RDL and IPD addresses interconnect scalability and power/signal integrity
  Base die CMOS enables IP-folding thru stacking
  Combining them simplify assembly logistics but reduces feature utilization efficiency; increase BOM cost
2.3D-BT2
  2.3D-BT: RDL, bridge die for high density shore connectivity; IPD chiplets w/ TSV for PI/SI
  T: Si Chiplets w/ TSV for IP-folding
  What is design requirement vs. physical constraint
Holistic Co-pathfinding with SiFO/OSAT/Design for successful new product-technology deployment

## Slide 8: Rumsfeld Matrix known knowns, known unknowns, and unknown unknowns
“… there are known knowns; there are things we know we know. We also know there are known unknowns; that is to say we know there are some things we do not know. But there are also unknown unknowns—the ones we don't know we don't know…”
Known and Unknown: A Memoir by Donald Rumsfeld

## Slide 9: Why ELP
Inspired by Client PX processor
  Medium Power (~50W/package), High BW SLC (~TB/s/core)
"2.3D is superior"; is it?
  One of CCG’s interests but no resources/bandwidth assess it.
"Si is smarter"
  Learnings comes from entire cycle (design to tests)
2.3D is system pathfinding priority
  Pick ELP for System Integration learning
  Beyond known knowns/unknowns, exploring unknown unknowns
  Afterall, pathfinding is only useful if “It works”

## Slide 10: Scratchpad

## Slide 11
CPU-PX
Si Interposer / MiM / SRAM
CPU-PX
SRAM
DTC
CPU-PX
GPU-PX
PCD-PX
10mm
17.5mm
10.5mm
5.25mm
I3FV
Upto 420MB
~1MB/mm2
CPU-PX
Discrete DTC not shown)
Embedded 256MB
GPU-PX
PCD-PX
(HBI DTC not Shown)
Bridge
Bridge
10mm
17.5mm
10.5mm
5.25mm
9.84~
10.91mm
9.75mm