## Slide 1
Speaker Name Title Goes Here

## Slide 2
 | HD Bitcell Area (um2) | Bit Density Mb/mm2 | Byte Density MB/mm2
N3E | 0.0212 | 47.1 | 
N5 | 0.0214 | 46.7 | 
N6 | 0.0274 | 36.5 | 
N7 | 0.0274 | 36.5 | 

## Slide 3: SRAM M3 Pinout Patterning
 | N3E | N5 | N6 | N7
Fin | EUV | ArFi | ArFi | ArFi
Gate | EUV | 3ArFi | 3ArFi | 3ArFi
Epi | 2 | 4 | 2 | 2
CPO | EUV | EUV | 2ArFi | 2ArFi
MD/MP | 2EUV | 2ArFi + EUV | 7ArFi | 7ArFi
VGVD | 3EUV | 3EUV | EUV | 4ArFi
M0 | 3EUV | 2EUV+3ArFi | EUV | 5ArFi
M1 | EUV | 2EUV | EUV | 4ArFi
V0 | EUV | EUV | EUV | 3ArFi
M2 | 2EUV | 2EUV | EUV | 3ArFi
V1 | 2EUV | EUV | EUV | 2ArFi
M3 | EUV | 2ArFi | 2ArFi | 2ArFi
V2 | EUV | EUV | ArFi | ArFi
FEOL

## Slide 4: SRAM-Only Patterning
 | N3E | N5 | N6 | N7
Fin | EUV | ArFi | ArFi | ArFi
Gate | EUV | 3ArFi | 3ArFi | 3ArFi
Epi | 2 | 4 | 2 | 2
CPO | EUV | EUV | 2ArFi | 2ArFi
MD/MP | 2EUV | 2ArFi + EUV | 7ArFi | 7ArFi
VGVD | 3EUV | 3EUV | EUV | 4ArFi
M0 | EUV | EUV | EUV | 5ArFi
M1 | EUV | EUV | EUV | 4ArFi
V0 | EUV | EUV | EUV | 3ArFi
M2 | EUV | EUV | EUV | 3ArFi
V1 | EUV | EUV | EUV | 2ArFi
M3 | 2ArFi | 2ArFi | 2ArFi | 2ArFi
V2 | ArFi | ArFi | ArFi | ArFi
Bitcell is
FEOL limited
thus FEOL
cannot change
BEOL for
periphery can be
simplified to
lowest cost, N6

## Slide 5: Thank You!

## Slide 6: Decision making methodology
Metric: seeking lowest (cell size) · (patterning cost) product
Patterning cost :
Patterning tool exchange rate: 1 · EUV = 3 · 193i
6T patterning (Fin to VDVG) based on Technology node
Cell patterning ( M0 to M3): Simplify for Cell construct
Array patterning : upto 9ML is required
(Cell Size) · (Patterning Cost)
N5 is the best up to M3 and, will be the best for 9ML given everything equal form M4 and up with N5 cell size.
N4 share the same patterning cost of N5 with xx% optical shrink

## Slide 7: TSMC POR process for SRAM process cost assessment
 | N3E | N5 | N6 | N7 |  |  | N3E | N5 | N6 | N7
Fin | EUV | ArFi | ArFi | ArFi |  | Fin | 3 | 1 | 1 | 1
Gate | EUV | 3ArFi | 3ArFi | 3ArFi |  | Gate | 3 | 3 | 3 | 3
Epi | 2 | 4 | 2 | 2 |  | Epi | 2 | 4 | 2 | 2
CPO | EUV | EUV | 2ArFi | 2ArFi |  | CPO | 3 | 3 | 2 | 2
MD/MP | 2EUV | 2ArFi + EUV | 7ArFi | 7ArFi |  | MD/MP | 6 | 5 | 7 | 7
VGVD | 3EUV | 3EUV | EUV | 4ArFi |  | VGVD | 9 | 9 | 3 | 4
M0 | 3EUV | 2EUV+3ArFi | EUV | 5ArFi |  | M0 | 9 | 9 | 3 | 5
M1 | EUV | 2EUV | EUV | 4ArFi |  | M1 | 3 | 6 | 3 | 4
V0 | EUV | EUV | EUV | 3ArFi |  | V0 | 3 | 3 | 3 | 3
M2 | 2EUV | 2EUV | EUV | 3ArFi |  | M2 | 6 | 6 | 3 | 3
V1 | 2EUV | EUV | EUV | 2ArFi |  | V1 | 6 | 3 | 3 | 2
M3 | EUV | 2ArFi | 2ArFi | 2ArFi |  | M3 | 3 | 2 | 2 | 2
V2 | EUV | EUV | ArFi | ArFi |  | V2 | 3 | 3 | 1 | 1
 |  |  |  |  |  | 6T Patterning | 26 | 25 | 18 | 19
 |  |  |  |  |  | Cell patterning | 59 | 57 | 36 | 39
 |  |  |  |  |  | Array Patterning |  |  |  | 
 |  |  |  |  |  | cell size | 0.0212 | 0.0214 | 0.0274 | 0.0274
 |  |  |  |  |  | 6T product | 0.5512 | 0.535 | 0.4932 | 0.5206
 |  |  |  |  |  | Cell product | 1.2508 | 1.2198 | 0.9864 | 1.0686
 |  |  |  |  |  | Array Product |  |  |  | 

## Slide 8: SRAM Optimized process
 | N3E | N5 | N6 | N7 |  |  | N3E | N5 | N6 | N7
Fin | EUV | ArFi | ArFi | ArFi |  | Fin | 3 | 1 | 1 | 1
Gate | EUV | 3ArFi | 3ArFi | 3ArFi |  | Gate | 3 | 3 | 3 | 3
Epi | 2 | 4 | 2 | 2 |  | Epi | 2 | 4 | 2 | 2
CPO | EUV | EUV | 2ArFi | 2ArFi |  | CPO | 3 | 3 | 2 | 2
MD/MP | 2EUV | 2ArFi + EUV | 7ArFi | 7ArFi |  | MD/MP | 6 | 5 | 7 | 7
VGVD | 3EUV | 3EUV | EUV | 4ArFi |  | VGVD | 9 | 9 | 3 | 4
M0 | EUV | EUV | EUV | 5ArFi |  | M0 | 3 | 3 | 3 | 5
M1 | EUV | EUV | EUV | 4ArFi |  | M1 | 3 | 3 | 3 | 4
V0 | EUV | EUV | EUV | 3ArFi |  | V0 | 3 | 3 | 3 | 3
M2 | EUV | EUV | EUV | 3ArFi |  | M2 | 3 | 3 | 3 | 3
V1 | EUV | EUV | EUV | 2ArFi |  | V1 | 3 | 3 | 3 | 2
M3 | 2ArFi | 2ArFi | 2ArFi | 2ArFi |  | M3 | 2 | 2 | 2 | 2
V2 | ArFi | ArFi | ArFi | ArFi |  | V2 | 1 | 1 | 1 | 1
 |  |  |  |  |  | 6T Patterning | 26 | 25 | 18 | 19
 |  |  |  |  |  | Cell patterning | 44 | 43 | 36 | 39
 |  |  |  |  |  | Array Patterning |  |  |  | 
 |  |  |  |  |  | cell size | 0.0212 | 0.0214 | 0.0274 | 0.0274
 |  |  |  |  |  | 6T product | 0.5512 | 0.535 | 0.4932 | 0.5206
 |  |  |  |  |  | Cell product | 0.9328 | 0.9202 | 0.9864 | 1.0686
 |  |  |  |  |  | Array Product |  |  |  |