## Slide 1: A 1Gb 2GHz Embedded DRAM in 22nm Tri-Gate CMOS Technology
Fatih Hamzaoglu, Umut Arslan, Nabhendra Bisnik, Swaroop Ghosh, Manoj B. Lal, Nick Lindert, Mesut Meterelliyoz, Randy B. Osborne, Joodong Park, Shigeki Tomishima, Yih Wang, Kevin Zhang
Intel Hillsboro, OR

## Slide 2: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 3: Motivation
Need for High Capacity and Low Energy/bit high-BW Memory increases
  SRAM is not dense enough, and DDR Energy/bit is high
  A high-density, high-BW In Package Memory is needed
Intel IvyTown Xeon®, ISSCC’14, Paper#5.4
25MB LLC
12.5MB LLC
Memory BW Trend (GB/s)
Shih-Lien Lu, ISSCC’14, Forum2, 2-socket Dell DP Systems
120 GB/s

## Slide 4: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 5: eDRAM Process in 22nm Tri-Gate
9 Metal Layers and 7-layers self-aligned Vias with ULK ILD
Wordline [N]
Wordline [N+1]
BL
COB
BL
COB
1T-1C eDRAM: 0.029mm2
Key features of eDRAM Tech.:
0.029m2 eDRAM bitcell
  3.2x smaller than SRAM (ISSCC’12)
17.5Mb/mm2 density for a 128Mb Macro
High-k, Metal Tri-Gate transistors supporting both low leakage and high performance
MIM Capacitor-Over-Bitline (COB) embedded in interconnect stack

## Slide 6: eDRAM Access Transistor
Vds = 1V @ 95C
Storage
Node
(Drain)
Wordline
(Gate)
Bitline
Contact
(Source)
Optimized Tri-Gate transistors for Latency, BW and Power
  <<1pA/cell leakage with Gate Underdrive
  Fifth-generation strained Si
Drain Current (A/cell)

## Slide 7: eDRAM Capacitor
  Median 14.2fF/cell, <<0.1pA/cell
14.2fF/cell
Capacitor
Fully integrated MIM Trench Capacitor
  Aggressive aspect ratio and compatible with logic process

## Slide 8: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 9: Subarray Architecture and Operation
Sense
Write-Back
WLoff
Pch
Subarray also includes Row and Column Redundancies, as well as local ½-VCC Generator
eDRAM
Timer
Prec+Sense+Mux
WL Dec
128 rows
tBL[i]
Row Redundancy
Column Redundancy
64b*8 columns
64b
64b
½ VCC Gen
256Kbit Subarray
bBL[i]
65% Array efficiency is achieved at 256Kbit Subarray
Random Cycle Time of 6 Array-Clock

## Slide 10: WordLine Driver for Power and Vmax
  None of the transistors’ gate is exposed to >VCC_WL
VCC_WL
Sleep
Sleep_b
VSS_WL
WL [N:0] (VSS_WL  VCC_WL)
(VSS  VCC_WL)
(VSS  VCC)
(VSS_WL  VCC)
(VSS_WL  VCC)
  Dynamic Sleep/Wakeup between VCC/VCC_WL
VSS_WL < VSS
Plate
Bitline
Access
Transistor
MIM
COB
VCC_WL > VCC
Adr [i:0]
WLen [j:0]
NOR Wordline Driver is used for simplicity and Reliability

## Slide 11: Area Efficient Column-IO
½-VCC Small Signal Sensing at Local Bitline
GBL[j]
rGBL[j]
Sense
Sense_b
Csel_b [7:0]
column mux
8
8
½-VCC
precharge
WL[i]
x128+
bBL[i]
tBL[i]
WL[j]
x128+
2nd Stage Small Signal Sense at Global Bitline
  Shared among Subarrays
8:1 Column-Mux to Read/Write 128bits per Subarray

## Slide 12: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 13: Integrated Programmable Charge Pumps
WL-ON Voltage is generated through Voltage Doubler
WL-OFF Voltage is drived from –VCC/2
Both Voltages are Regulated for Vmax and GIDL
  Programmable
Separate Pumps for Leakage and Activity Charge Loss

## Slide 14: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 15: 1Gb Die Floorplan
77mm2 1Gbit die, with 128 Independent Banks
Charge Pumps & Regulators
256Kb Subarray
2Mbit ¼ Bank
High Frequency OPIO
Low Freq. Test IO
eFuse
Test Access Port
Thermal Sensor
On-die Positive and Negative Charge Pumps with 2% Area Overhead
Thermal Sensor for Tjmax

## Slide 16: 1Gb Die Operation and Bandwidth
IO transmition rate is 4x of eDRAM Array to save IO area
  2x Frequency and samples at both rising & falling edges of IOclk
Eclk
IOclk
RD
64bx2
64bx8
64bx2
64bx2
64bx2
RD
WR
64bx8
64bx2
64bx2
64bx2
64bx2
WR
REF
REF
A Refresh can be issued every cycle in parallel
Array supports back to back Read/Write to different Banks
  Completely decoupled Read and Write Datapaths

## Slide 17: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 18: Integrated Programmable Charge Pumps
Tight VCC_WL control is achieved to avoid VCCmax
VCC_WL (V)
UnRegulated
Hot
Regulated-1
2*VCC
Cold
Regulated-2
Cum Prob
VSS
VSS_WL (V)
Cum Prob
Hot
Cold
UnRegulated
Regulated-1
Regulated-2
Similarly, tight VSS_WL control helps to achieve good Retention Time
  Programmability allows optimizing Subthreshold leakage vs. GIDL

## Slide 19: Retention Time Testing
Retention Time tested at worst case Bitline Voltage of 0V/1V
Potential 2x lower Bit Fail with BL = VCC/2 in Self Refresh
VSS_WL < VSS
Plate
BitLine
1/0
Design Target
BL = 0.5*VCC
BL = 0/VCC
Isub
2x
Cum Prob
Bit Fail @100ms RT, 95C
0.5*VCC
0/VCC

## Slide 20: Retention Bit-Fail Optimization
Each die has different Subthreshold/Junction leakage trade-off
  Hence different optimal VSS_WL per die
Die-by-die VSS_WL setting achieves significantly improved bit-fail distribution
Design Limit
Different fixed VSS_WL settings
Cum Prob
Bit Fail @100ms RT, 95C
Die-by-Die VSS_WL setting

## Slide 21: 1Gbit Array Shmoo
0.7V/1GHz – 1.05C/2GHz operation @95C, 100ms RT
  3ns Random Cycle Time @1.05V
64GB/s Read + 64GB/s Write Bandwidth @1.05V
Clock Frequency (GHz)
Supply Voltage (V)
1.05V, 2GHz
0.7V, 1GHz

## Slide 22: Iris ProTM with 1Gbit MCP eDRAM
Iris ProTM with 1Gb eDRAM MCP is commercially available
up to 75% Graphics Performance improvement with 1Gbit eDRAM
75% speed up
20%
40%
60%
Performance Improvement (eDRAM ON vs. OFF)
eDRAM
1Gbit eDRAM
Processor
Graphics
Core
LLC
Core
Core
LLC
Core
LLC
System
Agent
DMI
PCI Express*
IMC
LLC
DDR
Display
IO
IO
N. Kurd, ISSCC’14, “Haswell: A Family of IA 22nm Processors”

## Slide 23: Outline
Motivation
eDRAM Process in 22nm Tri-Gate
Sub-Array Design
Integrated Charge Pumps
Die Architecture and Protocol
Silicon Data
Conclusions

## Slide 24: Conclusions
A record density eDRAM Technology is developed in 22nm Tri-Gate Technology to provide high-BW and low Power Memory access
1Gb eDRAM is packaged with high-end graphics processor to improve the performance up to 75% for wide spectrum of applications.
The product is commercially available as Iris ProTM

## Slide 25
Q&A