## Slide 1: GTM Device Physics
Ricky Tseng, Peter Chang, David Kencke

## Slide 2: Agenda
Introduction: Floating Body Gain Cells
Thyristor Action, Vfb (Steady State)
1T Gated Thyristor DRAM: Long Gate Length
Memory Operation (Transient State)
Evolution of Disturb “1” State
2T Scaling (DRAM Operation)
Summary

## Slide 3: “2T” FB Gain Cell (‘93 Berkeley)
Read
N++
P+
P+
N+
Gate
Program
Storage
Program charge through NMOS and read on PMOS.
Cell layout and scaling problematic.

## Slide 4: Thyristor Operation
Sweep Vanode >3V →break over middle junction→ snapback occurs
J1
J2
J3
+V1-
+V2-rev./for.
+V3-
P+
N+
N
P
Vfb
Vfb: forward breakover voltage
Anode (V)
Id (uA/cell)
Lg=300
Notes: 4

## Slide 5: Carriers
1
2
3
4
4
3
2
1
Breakover
All junctions on
Breakover
when reverse bias is large and starts to lower J1/J3
n
p
R
G
R
net doping

## Slide 6: Band Diagram
1
2
3
4
4
3
2
1
Breakover
when reverse bias is large and starts to lower J1/J3
Ec
Ev
Fn
Fp

## Slide 7: Vfb (w/o Gate)
Vfb=VB(1-α1-α2 )1/n, VB is the reverse breakdown voltage, n is constant, α1, α2 is the current gain of pnp, npn transistors.
Ln=√Dτ , α~sech(W/Ln), τ↑, α↑, Vfb↓ (Ln~2um)
When α1+α2~1, the thyristor breaks over, and J2 is in the saturation state.
Anode
Cathode
P
P
N
N
P
N
IE1
IB1=IC2
IE2
IC1=IB2

## Slide 8: Vfb vs. Gate Voltages
Gate voltages modulate the P body potential thus for breakover (Vfb) effect. In contrast no-gated thyristor relys on doping for Vfb.
Anode (V)
J1
J2
J3
+V1-
+V2-
+V3-
P+
N+
N
P
G
VG= -0.4
0.2
0.3
0.4
0.5
VG
(P-metal gate)
1.1

## Slide 9: 1T Thyristor DRAM (T-RAM ‘05)
It appears that Vfb > Vdd is still needed for DRAM.
Our finding: Vfb is a steady state characteristics, OK to be small for DRAM.
2T GTM is scalable to Lg=28nm.

## Slide 10: Simulation Model
Tram, IEDM’05
TRAM dimensions adjusted to fit
p+ n p n+
Lg=300nm | dId, 125C (uA/cell) | dId 25C (uA/cell) | Ret (ms)
T-ram | 190 | 130 | 24
Intel SIM | 183 | 142 | 17
FBC Device Model calibrated w/ Intel bipolar FBC data.
Estimated and compared results vs. T-ram’s long Lg data.
Use this model for device design and array operations

## Slide 11: Memory Operation W1/W0
J1
J2
J3
P+
N+
N
P
1.05
J1
J2
J3
P+
N+
N
P
0.6
W1
W0
w1
w0
SRH
e-
h+
P+
N
P
N+
Rate, doping, e/h conc. (cm-3)
Mechanism only involves SRH Rec/Gen.
I hole →
←I elec
+1.05
+1.05
0
No holes
0
+1.05
+1.05
h+
Notes: 11

## Slide 12: Memory Operation R1/R0
J1
J2
J3
P+
N+
N
P
1.05
J1
J2
J3
P+
N+
N
P
1.05
R1
R0
r1
r0
e-
h+
P+
N
P
N+
Rate, doping, e/h conc. (cm-3)
I hole →
←I elec
0
0.3
0.3
I hole →
←I elec
0
0.3
0.3

## Slide 13: 1T Disturb/Hold Retention
Median retention (disturb “1”, hold “0”) ~4ms.
Disturb settles at “0” , Hold settles at “1”.
Time (sec)
Holes
“1”
“0”
hold
dist
Time (sec)
Id (uA/cell)
“1”
“0”
DG, Lg = 40nm.
1T Lg=40 | BL (anode) | WL (P-Gate) | SL (cathode)
Write1 | 1.05 | 1.05 | 0
hold | 1.05 | 0.3 | 0.9
Read | 1.05 | 0.4 | 0
Write0 | 0.6 | 1.05 | 0
Disturb | 0.6 | 0.3 | 0.9
hold
dist
Notes: 13

## Slide 14: Evolution of Dist “1”
10ms
1us
Anode (V)
Id (uA/cell)
Time (sec)
40 holes
120 holes
Long read after Dist “1” for 1s
1s
5 holes
Transient state evolves into the steady state condition.
Transient state does not correspond to a steady state point.
Vfb is needed for read operation not retention.
Read condition @ VG=0.3
Dist: BL=0.6 WL=0.3 SL=0.9V

## Slide 15: 2T Gated Thyristor SRAM (Stanford ’98, ’99, T-RAM ‘04)
2T is needed for solving the BL disturb issue in 1T.

## Slide 16: 2T Cell Scaling
P1270
Cell: 270x80 nm2
P1274
Cell:170x40 nm2
P1272
Cell: 216x56 nm2
0.8X0.7
0.8X0.7
Lg=40
Lg=40
Lg=32
Lg=32
Lg=25
Lg=25

## Slide 17: 2T Lg=40 (P1270)
Time (sec)
Holes
Median retention ~25ms
Tail retention ~14ms
med
tail
med
tail
Median dId ~13.5uA @85C
Tail dId ~6.3uA @-5C
Id (uA/cell)
DG, Lg=40
Tail conditions (± 2nm Tsi, ±4.7s RDF)
Notes: 17

## Slide 18: 2T Scaling to Lg=25nm (P1274)
Lg=25 is functional, continue investigating shorter Lg.
Time (sec)
med
tail
med
tail
1, 0 # of holes
Id/cell (uA)
Median dId ~15.6 uA @85C
Tail dId ~6 uA @-5C
Median retention ~1.5ms
Tail retention ~0.5ms

## Slide 19: Vfb Scaling
As device scaled, proper gate voltages and Tox are needed to maintain Vfb.
(Tails have condition of 4.7s RDF, +2nm Tsi)
Lg (nm)
Vfb (V)
@ 85C
VG=0.9
VG=0.3 tails
VG=0.3 median
(ret~ 1.5ms)
(ret~ 0.5ms)
2T DRAM operation
Gate: P-metal gate

## Slide 20: Summary Table
 | Ox (nm) | Lg (nm) | Tsi (nm) | V range (V) | Results/Comments
Tram |  |  |  |  | 
1T | ? | 300 | 90 | 3 | Device data, DRAM operation, retention 27ms
2T | ? | 300 | 90 | 3.6 | 1.1MB Array, Claimed SRAM operation (restore).
 |  |  |  |  | Our finding: restore has no operating window given intrinsic 4.7s RDF and ± 2nm Tsi tail condition.
Intel Simulation |  |  |  |  | Matched cells shows comparable dId and retention.
1T | 6 | 300 | 90 | 3 | 
1T DG | 2.4 | 40 | 26 | 1.1 | Lg=40 shows median retention 4ms Cannot scale to Lg=32 due to BL low disturb
2T DG | 2.4 | 40 | 26 | 1.8 | Isolate the floating node, which can eliminate the disturb issue in 1T Scalable to Lg=25
Tox scaling is the key to generate scaled device.
Tox scaling is the key for scaling down to 40nm Lg device.

## Slide 21: Backup

## Slide 22: Transient (Hold “0”) vs. Steady State
10ms
Short Read 6ns after Hold “0”
Anode (V)
Id (uA/cell)
Time (sec)
27 holes
66 holes
10ns
Long read after write0
5 holes

## Slide 23: Erase Hold 4ms

## Slide 24: 1T FB Gain Cell (ISi ‘01, Toshiba ’02, Berkeley ‘02)
Front channel for both program and read, back channel for storage.
Impact Ionization requires moderately high voltage.
Hole storage in back channel requires a BG coupling.
  Pillar BG or -20V voltage for 150nm BOX

## Slide 25: IDG 1T FBC (Intel ‘06)
BOX
FG
BG
Si
Low voltage operation with thin BG oxide.
But asymmetric FB/BG needed for optimal memory performance.